ɤ-TiAl alloy: Tensile creep deformation behaviour and creep life at 832 °C

Mainak Saha

Department of Metallurgical and Materials Engineering, Indian Institute of Technology (IIT) Madras-600036, Tamil Nadu, India

Abstract

Creep deformation in single phase ɤ-TiAl alloy manufactured using different processing techniques has been an extensively studied topic since the late 1970s. The present work revisits the original work on understanding the tensile creep deformation behaviour of wrought single-phase ɤ-TiAl alloy by Hayes and Martin [1] and is aimed to develop an understanding of steady state creep. Besides, it is also aimed to investigate the creep life for stress levels of 69.4 and 103.4 MPa at 832 ⁰C using Monkman-Grant [2] approach.

Keywords: ɤ-TiAl, Monkman-Grant parameter, Coble creep, Nabarro-Herring creep

- Introduction

A series of reports on the room temperature tensile deformation behaviour of ɤ-TiAl alloys (L10 structure) show that the near-ɤ, two phase compositions having ~ 48 at.% Al possess very high toughness (ultimate tensile strength~ 844-1010 MPa and tensile ductility~ 3-4.6% at room temperature) [1], [3]–[10]. Extensive creep deformation studies have been carried out on a number of two phase near- ɤ-TiAl alloys produced by various processing routes. In addition, compression creep based investigations have been performed on a number of single phase ɤ-TiAl alloys and a number of literatures have reported that minimum strain rates during creep testing at different regimes of temperature and stress, hugely influence the grain size of single phase ɤ-TiAl alloys (during creep testing) [11]–[24]. Minimum strain rate of such intermetallic-based alloys may be defined in terms of Mukherjee-Bird-Dorn (MBD) equation [19], [25], [26].

The work of Hayes and Martin [1] discusses an analysis of the minimum strain rate deformation of a wrought single phase ɤ -TiAl alloy within temperature range of 760-1000 ⁰C and stress range of 32–345 MPa. The work by Hayes and Martin [1] also predicts the main mechanism for creep rupture at different temperatures, in a given stress range, using Larson-Miller (L-M) [27] and Monkman-Grant (M-G) plots [2] and extensive microstructural characterisation using Optical microscope (OM) and the Transmission Electron Microscope (TEM). Besides, a recent report (from the author) on the tensile creep deformation behaviour of ɤ-TiAl has determined the stress exponent and creep activation energies between 760 ⁰C and 900 ⁰C at 69.4 and 103.4 MPa [28]. Moreover, based on creep activation energies and stress exponents, it has been reported that there is a transition from dislocation-glide to dislocation-climb controlled creep at very low creep stress levels (~ 66.68 MPa) [28] and that there is no steady-state creep observed for both interrupted and uninterrupted creep tests at 832 ⁰C [1]. However, there is limited understanding of creep behaviour and creep rupture life as a function of stress at 832 ⁰C. To this end, the present work is aimed towards determining creep behaviour and rupture life for stress levels of 69.4 and 103.4 MPa at 832 ⁰C using M-G approach.

- Theoretical analysis

Based on the single-phase ɤ-TiAl alloy composition and tensile creep test parameters used by Hayes and Martin [1], the minimum strain rate (εmin) vs strain (ε) and ln(εmin) vs ε plots have been determined at 832 °C for two different stress levels viz. 69.4 and 103.4 MPa for the purpose of understanding the influence of creep stress and temperature on the three creep regimes (viz. primary, secondary and tertiary) and the influence of the same on the creep life of the material. For creep life determination, M-G approach was used. For M-G approach, the governing equation is: [16], [29]

εstr=CMG                                                                          (2)

where, εsis the steady state creep rate (~ εmin based on the justification that many metallic materials may not exhibit steady-state creep (provided in Ref. [28])), tr is the rupture time (expressed in seconds) and  CMG (~1.40 at 832 °C) is the M-G constant (obtained from Ref. [28]).

- Results and Discussions

Figs. 1(a and b) show the variation of ε  with ε (in both linear and logarithmic scales respectively) for three cases viz. uninterrupted creep testing and interrupted creep testing with termination strains of 0.18 and 0.5%. Fig. 1(b) shows the creep regimes at 832 °C (for stress levels of 69.4 and 103.4 MPa respectively) with a higher simplicity. Based on Fig. 1, it is observed that the present material (45.9Ti-0.91Nb-52.9Al (at.%)) shows a very early onset of tertiary creep at 832 °C for uninterrupted creep test and for creep test terminated at 0.5% strain whereas there is no primary (or transient) creep observed during creep test interrupted at strain of 0.18% (Fig. 1) indicating that the material (used in the present work) does not exhibit resistance to creep deformation for the aforementioned deformation condition. Besides there is a limited regime of tertiary creep observed for creep tests terminated a 0.18% and 0.5% strain (Fig. 1). In addition, the material shows a dominant tertiary creep regime for the case of uninterrupted tensile creep testing (Fig. 1). Secondary (or steady-state creep) is not observed in any case (Fig. 1). In other words, the interrupted creep tests lead to a higher rate of vacancy formation at grain boundaries (GBs) normal to the tensile stress subsequently followed by void growth and coalescence leading to an intergranular fracture, as mentioned in Refs. [30]–[32]. Explanation of the above tendencies during interrupted and uninterrupted tensile creep test (at 832 °C) is subject to extensive microstructural investigations which is beyond the scope of the present discussion.

Fig. 1 Variation of (a)  ε  with ε, and (b) ln(ε) with ε. In parts (a) and (b), the plot uninterrupted creep test has been represented using black colour whereas the creep tests terminated at 0.18% and 0.5% have been represented using red and blue colours respecively. The inset images in parts in (a) and (b) represent the different creep regimes in both interrupted and uninterrupted creep tests with a high level of clarity.

For uninterrupted creep testing, there is a dominant tertiary creep regime (Fig. 1). Moreover, it has been reported that the extent of tertiary creep hugely influences the creep life of the material [31]. To this end, creep life determination has been performed for samples (with uninterrupted creep testing) at 832 °C. Fig. 2 shows the creep life plots (for uninterrupted creep testing) based on M-G approach for stress levels of 69.4 and 103.4 MPa at 832 °C. From Fig. 2, it is observed that tr decreases with increasing εmin at 832 °C (based on equation 2). Moreover, the slope (p) of the M-G curve (in Fig. 2) is calculated as -1.33 which suggests that the mechanism of creep rupture is power-law breakdown at 832 °C (using the criteria mentioned in Ref. [14], [16], [33]–[37]). Hayes and Martin [1] and Saha [28] have reported that εmin decreases with increasing stress levels (from 69.4-103.4 MPa) at 832 °C. Moreover, Saha [28] has reported that the creep mechanisms operating at different stress levels (69.4 and 103.4 MPa) at 832 °C are independent of each other and hence, are not sequential. Hence, combining the trend observed between εmin with tr (Fig. 2) with the aforementioned reports (Refs. [1], [28]), it may be inferred that M-G based approach to determine the creep life also predicts that tr decreases with increasing stress levels (from 69.4 to 103.4 MPa) at 832 °C.

Fig. 2 M-G plots for determining creep life for 69.4 MPa and 103.4 MPa at 832°C. εmin has been normalised with rupture strain (εr) determined from Fig. 1. A justification of the above normalisation (for M-G plots) has been provided in Ref. [27].

Based on the Ashby’s model [13], [14], [38], [39], the constitutive equation for NH (or lattice diffusion creep) is given as:

ε=9.3DlGbkTbd2σG                                                                     (3)

where, ε is the strain rate, Dl is the lattice diffusivity, b is the burgers vector, d is the grain size, k is the Boltzmann constant, σ is the creep stress and G is the shear modulus of the material. Similarly, using Ashby’s model, the constitutive equation for Coble creep (or GB diffusion creep) is given as:

ε=33.4DGBGbkTbd3σGδb                                                                     (4)

where, δ is the GB width and DGB is the activation energy for GB diffusion. Both DGB and Dl are highly temperature-dependent [14]. However, the magnitude of DGB is higher than that of Dl at lower homologous temperatures whereas the magnitude of Dl is higher than that of DGB at higher homologous temperatures [40], [41]. This is because GBs offer a higher pathway for diffusion at lower temperatures when compared with that of the lattice [42]. Moreover, a comparison of the equations (3) and (4) shows that Coble creep has a higher grain-size dependence as compared to that of NH creep. In other words, although both Coble and NH creep may operate simultaneously, Coble creep is the dominant diffusion creep mechanism for fine grain sizes at lower temperatures whereas NH creep dominates for comparatively coarser grains at higher temperatures. However, both these mechanisms show a similar sensitivity towards σ (as shown in equations (3) an (4)). Based on the previous reports [1], [28], d has minimal influence on ε. The direct proportionality between ε ad σ in equations (3) and (4) also explains the previous observations (in Refs. [1], [3], [28]) on the increasing magnitude of ε with increasing stress levels from 69.4-103.4 MPa. Besides, G, σ, T (~ 832 °C) and b are constant in the present work. Based on the values of NH and Coble creep activation energies (Ql and QGB respectively) reported for 69.4 MPa (QGB~ 210 kJ/mol and Ql~ 350 kJ/mol at 832 °C in Ref. [28]) and for 103.4 MPa (QGB~ 151.88 kJ/mol and Ql~ 253.13 kJ/mol at 832 °C in Ref. [28]), it may be inferred that a decrease in the creep activation energy (for both Coble and NH creep) significantly reduces the creep life of the material with increasing stress levels from 69.4-103.4 MPa.

- Conclusions

Based on the present work, the following may be concluded:

- At 832 °C, ɤ-TiAl alloy (45.9Ti-0.91Nb-52.9Al (at.%)) shows a dominant tertiary creep regime for uninterrupted creep testing at 69.4 MPa and 103.4 MPa whereas there is a limited tertiary creep regime for creep tests (under the same temperature and stresses) for creep tests interrupted at 0.18% and 0.5% indicating that during interrupted creep testing, there is a higher rate of vacancy formation along GBs normal to the applied tensile stress followed by void coalescence and growth leading to intergranular fracture.

- M-G approach (for creep life determination) shows that creep life (for uninterrupted creep testing) decreases with increase in stress levels from 69.4 to103.4 MPa. In addition, M-G plots indicate the mode of rupture (for uninterrupted creep test) at 832 °C (for stress levels of 69.4 MPa and 103.4 MPa) is power-law breakdown.

- A decrease in creep activation energy (for both Coble and NH creep) reduces the creep life of the material with increasing stress level from 69.4 to 103.4 MPa.

Acknowledgement

MS would like to acknowledge the Department of Metallurgical and Materials Engineering, NIT Durgapur, for detailed discussions during the preparation of the manuscript.

References

[1]        R. W. Hayes and P. L. Martin, “Tension creep of wrought single phase γ TiAl,” Acta Metallurgica Et Materialia, vol. 43, no. 7, pp. 2761–2772, Jul. 1995, doi: 10.1016/0956-7151(94)00486-2.

[2]        M. Menon, H. Fang, … D. W.-J. of the, and undefined 1994, “Creep and Stress Rupture Behavior of an Advanced Silicon Nitride: Part III, Stress Rupture and the Monkman–Grant Relationship,” Wiley Online Library, Accessed: Sep. 16, 2020. [Online]. Available: https://ceramics.onlinelibrary.wiley.com/doi/abs/10.1111/j.1151-2916.1994.tb05397.x.

[3]        R. W. Hayes and B. London, “On the creep deformation of a cast near gamma TiAl alloy Ti48Al1 Nb,” Acta Metallurgica Et Materialia, vol. 40, no. 9, pp. 2167–2175, 1992, doi: 10.1016/0956-7151(92)90134-Z.

[4]        S. C. Huang and E. L. Hall, “Plastic deformation and fracture of binary TiAl-base alloys,” Metallurgical Transactions A, vol. 22, no. 2, pp. 427–439, Feb. 1991, doi: 10.1007/BF02656810.

[5]        D. Holec, R. K. Reddy, T. Klein, and H. Clemens, “Preferential site occupancy of alloying elements in TiAl-based phases,” Journal of Applied Physics, vol. 119, no. 20, May 2016, doi: 10.1063/1.4951009.

[6]        S. Karthikeyan, G. B. Viswanathan, P. I. Gouma, V. K. Vasudevan, Y. W. Kim, and M. J. Mills, “Mechanisms and effect of microstructure on creep of TiAl-based alloys,” Materials Science and Engineering A, vol. 329–331, pp. 621–630, Jun. 2002, doi: 10.1016/S0921-5093(01)01659-8.

[7]        D. Shechtman, M. J. Blackburn, and H. A. Lipsitt, “PLASTIC DEFORMATION OF TiAl.,” Metall Trans, vol. 5, no. 6, pp. 1373–1381, 1974, doi: 10.1007/BF02646623.

[8]        P. L. Martin, M. G. Mendiratta, and H. A. Lipsitt, “Creep deformation of tial and tial + w alloys,” Metallurgical Transactions A, vol. 14, no. 10, pp. 2170–2174, Oct. 1983, doi: 10.1007/BF02662384.

[9]        S. A. Court, V. K. Vasudevan, H. L. Fraser, S. A. Court, V. K. Vasudevan, and H. L. Fraser, “Deformation mechanisms in the intermetallic compound TiAl,” Philosophical Magazine A: Physics of Condensed Matter, Structure, Defects and Mechanical Properties, vol. 61, no. 1, pp. 141–158, 1990, doi: 10.1080/01418619008235562.

[10]       C. T. Liu, J. H. Schneibel, P. J. Maziasz, J. L. Wright, and D. S. Easton, “Tensile properties and fracture toughness of TiAl alloys with controlled microstructures,” Intermetallics, vol. 4, no. 6, pp. 429–440, Sep. 1996, doi: 10.1016/0966-9795(96)00047-7.

[11]       X. Wang et al., “Creep-Induced Phase Instability and Microstructure Evolution of a Nearly Lamellar Ti–45Al–8.5 Nb–(W, B, Y) Alloy,” Springer, Accessed: Sep. 16, 2020. [Online]. Available: https://link.springer.com/content/pdf/10.1007/s40195-020-01108-x.pdf.

[12]       P. S. Phani and W. C. Oliver, “A direct comparison of high temperature nanoindentation creep and uniaxial creep measurements for commercial purity aluminum,” Acta Materialia, vol. 111, pp. 31–38, Jun. 2016, doi: 10.1016/j.actamat.2016.03.032.

[13]       A. C. F. Cocks and M. F. Ashby, “On creep fracture by void growth,” Progress in Materials Science, vol. 27, no. 3–4, pp. 189–244, 1982, doi: 10.1016/0079-6425(82)90001-9.

[14]       G. H. Edward and M. F. Ashby, “Intergranular fracture during power-law creep,” Acta Metallurgica, vol. 27, no. 9, pp. 1505–1518, 1979, doi: 10.1016/0001-6160(79)90173-1.

[15]       B. F. Dyson and D. McLean, “A new method of predicting creep life,” Metal Science Journal, vol. 6, no. 1, pp. 220–223, Jan. 1972, doi: 10.1179/030634572790446181.

[16]       M. E. Kassner, Fundamentals of Creep in Metals and Alloys: Third Edition. Elsevier Inc., 2015.

[17]       B. C. Ng, B. A. Simkin, M. A. Crimp, and T. R. Bieler, “The role of mechanical twinning on microcrack nucleation and crack propagation in a near-γ TiAl alloy,” Intermetallics, vol. 12, no. 12, pp. 1317–1323, Dec. 2004, doi: 10.1016/j.intermet.2004.03.015.

[18]       A. Mukherjee, R. Mishra, T. B.-M. S. Forum, and undefined 1997, “Some critical aspects of high strain rate superplasticity,” Trans Tech Publ, Accessed: Sep. 16, 2020. [Online]. Available: https://www.scientific.net/MSF.233-234.217.pdf.

[19]       T. R. Bieler, R. S. Mishra, and A. K. Mukherjee, “Superplasticity in hard-to-machine materials,” Annual Review of Materials Science, vol. 26, no. 1, pp. 75–106, 1996, doi: 10.1146/annurev.ms.26.080196.000451.

[20]       A. H. Chokshi, “Grain Boundary Processes in Strengthening, Weakening, and Superplasticity,” Advanced Engineering Materials, vol. 22, no. 1, p. 1900748, Jan. 2020, doi: 10.1002/adem.201900748.

[21]       T. G. Langdon, “Grain boundary sliding as a deformation mechanism during creep,” Philosophical Magazine, vol. 22, no. 178, pp. 689–700, 1970, doi: 10.1080/14786437008220939.

[22]       R. L. Coble, “A Model for Boundary Diffusion Controlled Creep in Polycrystalline Materials,” Journal of Applied Physics, vol. 34, no. 6, pp. 1679–1682, 1963, doi: 10.1063/1.1702656.

[23]       R. C. Gifkins, T. G. Langdon, and D. McLean, “Grain-Boundary Sliding and Axial Strain during Diffusional Creep,” Metal Science, vol. 9, no. 1, pp. 141–144, Jan. 1975, doi: 10.1179/030634575790444522.

[24]       A. G. Evans and T. G. Langdon, “Structural ceramics,” Progress in Materials Science, vol. 21, no. 1–2. Pergamon, pp. 171–425, Jan. 01, 1976, doi: 10.1016/0079-6425(76)90006-2.

[25]       A. K. Mukherjee, “An examination of the constitutive equation for elevated temperature plasticity,” Materials Science and Engineering A, vol. 322, no. 1–2, pp. 1–22, Jan. 2002, doi: 10.1016/S0921-5093(01)01115-7.

[26]       R. S. Mishra and A. K. Mukherjee, “On superplasticity in silicon carbide reinforced aluminum composites,” Scripta Metallurgica et Materiala, vol. 25, no. 2, pp. 271–275, Feb. 1991, doi: 10.1016/0956-716X(91)90177-3.

[27]       G. Sundararajan, “The Monkman-Grant relationship,” Materials Science and Engineering A, vol. 112, no. C, pp. 205–214, Jun. 1989, doi: 10.1016/0921-5093(89)90360-2.

[28]       M. Saha, “A brief discussion on the tensile creep deformation behaviour of wrought single-phase γ-TiAl,” Materials Today: Proceedings, Jan. 2021, doi: 10.1016/j.matpr.2020.11.189.

[29]       MONKMAN and F. C., “An Empirical Relationship between Rupture Life and Minimum Creep Rate in Creep Rupture Tests,” Proc. ASTM, vol. 56, pp. 91–103, 1956, Accessed: Sep. 16, 2020. [Online]. Available: https://ci.nii.ac.jp/naid/10006401917.

[30]       R. E. Smallman and A. H. W. Ngan, “Creep, Fatigue and Fracture,” in Modern Physical Metallurgy, Elsevier, 2014, pp. 571–616.

[31]       R. E. Smallman and R. J. Bishop, “Mechanical behaviour of materials,” in Modern Physical Metallurgy and Materials Engineering, Elsevier, 1999, pp. 197–258.

[32]       G. M. Gladysz and K. K. Chawla, “Intrinsic Voids, Ideal Materials, and Real Materials,” in Voids in Materials, Elsevier, 2015, pp. 13–35.

[33]       R. E. MISTLER and R. L. COBLE, “Rate‐Determining Species in Diffusion‐Controlled Processes in Al2O3,” Journal of the American Ceramic Society, vol. 54, no. 1, pp. 60–61, 1971, doi: 10.1111/j.1151-2916.1971.tb12175.x.

[34]       T. G. LANGDON, “Activation Energies for Creep of Pyrolytic and Glassy Carbon,” Nature Physical Science, vol. 236, no. 65, pp. 60–60, Mar. 1972, doi: 10.1038/physci236060a0.

[35]       J. Weertman, “Steady-State Creep through Dislocation Climb,” Journal of Applied Physics, vol. 28, no. 3, pp. 362–364, 1957, doi: 10.1063/1.1722747.

[36]       F. R. N. Nabarro, “Steady-state diffusional creep,” Philosophical Magazine, vol. 16, no. 140, pp. 231–237, 1967, doi: 10.1080/14786436708229736.

[37]       F. A. Mohamed and T. G. Langdon, “Deformation mechanism maps: Their use in predicting creep behavior,” Journal of Engineering Materials and Technology, Transactions of the ASME, vol. 98, no. 2, pp. 125–130, 1976, doi: 10.1115/1.3443352.

[38]       LANGDON TG, “Effect of surface configuration on grain boundary sliding,” Met Trans, vol. 3, no. 4, pp. 797–801, 1972, doi: 10.1007/bf02647651.

[39]       W. D. Kingery and E. D. Montrone, “Diffusional creep in polycrystalline sodium chloride,” Journal of Applied Physics, vol. 36, no. 8, pp. 2412–2413, 1965, doi: 10.1063/1.1714501.

[40]       T. G. Langdon, D. R. Cropper, and J. A. Pask, “Creep Mechanisms in Ceramic Materials at Elevated Temperatures,” in Ceramics in Severe Environments, Springer US, 1971, pp. 297–313.

[41]       V. Yamakov, D. Wolf, S. R. Phillpot, and H. Gleiter, “Grain-boundary diffusion creep in nanocrystalline palladium by molecular-dynamics simulation †,” 2002. Accessed: Sep. 30, 2020. [Online]. Available: www.elsevier.com/locate/actamat.

[42]       T. G. Langdon, “Grain Boundary Deformation Processes,” in Deformation of Ceramic Materials, Springer US, 1975, pp. 101–126.