Cyclic oxidation behaviour of ZrB2 -20 vol.%MoSi2 based ultra-high temperature ceramic matrix composite between 1100°C and 1300°C

Mainak Saha1, Sourajit Pramanik1, Rajdeep Banik1, Pooja Maurya1, Simrat Singh1, S. Vandan Raj1, D. Prem Madhur1, Tanay Rudra Paul1, Rahul Mitra2, Manas Kumar Mondal1, Manab Mallik1

1Department of Metallurgical and Materials Engineering, National Institute of Technology, Durgapur, India

2Department of Metallurgical and Materials Engineering, Indian Institute of Technology, Kharagpur, India

Abstract- While descending through different layers of atmosphere with tremendously high velocities, hypersonic re-entry nosecones fabricated using ultra-high temperature ceramic matrix composites (UHTCMCs) are subjected to repeated thermal shocks. This necessitates extensive investigations on the cyclic oxidation behaviour of UHTCMCs at temperatures ranging from 1100°C to 1300°C (service temperature of the nosecones). To this end, the present work is aimed at investigating the cyclic oxidation behaviour of ZrB2 -20 vol.%MoSi2 (ZM20) UHTCMC (a very widely investigated ZM CMC) by carrying out cycles for 6h, at 1cycle/h and estimating oxidation kinetic law. This has been followed by extensive characterisation using X-Ray Diffraction (XRD) to indicate the phases formed during oxidation and  Scanning  electron  microscopy-energy  dispersive  spectroscopy  (SEM-EDS), in order to determine the chemical composition of the oxides formed between 1100°C and 1300°C.

Keywords- Borides; ceramic composites; cyclic oxidation; kinetics; oxide layer

Among UHTCs, ZrB2-based ceramics have been reported to be potential candidates for the 
manufacture of reusable Thermal Protection Systems (TPS) in Hypersonic re-entry nosecones, 
due to very high thermal conductivity and relatively low density [1,2]. However, the low 
fracture toughness and poor thermal shock resistance of these ceramics pose major obstacles 
to their use in extreme environment [3]. 
Moreover, the poor oxidation resistance of ZrB2 at temperatures above 1200°C, due to 
formation of B2O3, and a non-protective porous scale of ZrO2 [4], poses restrictions to its use 
at elevated temperatures, especially above 1200°C. Thus, it becomes extremely important to 
find materials, which may highly enhance the oxidation resistance of ZrB2 [5-8]. A significant 
amount of work has already been done in that direction [8-12]. 
Besides, a significant amount of research has been done on reinforcing diborides like ZrB2, 
HfB2 and TiB2 with SiC, MoSi2, or ZrSi2 for enhanced oxidation resistance beyond 800C [3- 
20]. However, a limited amount of study has been made on cyclic oxidation of ZM20 at 
temperatures exceeding 1100C, which is not at all unlikely, in the context of Hypersonic 
nosecones, during a high velocity descent through different layers of atmosphere. Thus, the 
scope of the present study is to investigate the cyclic oxidation behaviour of ZM20 between 
1100 and 1300 C.

The important conclusions drawn form the results and discussions of this study have been 
elucidated. Cyclic oxidation behaviour of ZrB2-20 vol.% MoSi2 composite have been studied at 1100 C, 1200 C, 1250 C and 1300 C for 6hrs. Monitoring weight change and examining oxide scales draw following conclusions:

(i) Weight gain for both the composites increased with increasing temperature and time. 

(ii) Weight gain occurred due to formation of ZrO2 and SiO2, at elevated temperatures. 

(iii) The main oxidation products were ZrO2, MoO3 and SiO2. 

(iv) At 1200 C and above, the presence of SiC particles markedly improves the resistance to 
oxidation of the composite due to the formation of borosilicate glass.

(v) Due to formation of oxide layer on the surface, the hardness of the samples i.e. its 
mechanical properties decreased from center to surface.

(vi) The cyclic oxidation of the samples follow linear oxidation kinetics from 1100 to 1250 ºC 
while at 1300 ºC it follows parabolic oxidation kinetics due to the protective action of SiO2 
above 1250 ºC.

The results of the present study and their analyses lead to the following directions for future 
work: 
(i) The oxidation kinetics of the samples beyond 1300 ºC can be studied. 
(ii) Residual strain calculations can be carried out. 
(iii) Mathematical modelling study of the oxidation kinetics can be carried out. 
(iv) TEM study of the samples can be carried out for more precarious measurements. 
(v) Carrying out diffusion studies on oxide layer. 


Acknowledgement 

The authors are grateful to the Department of Metallurgical and Materials Engineering, NIT 
Durgapur and Central Research Facility(CRF), IIT Kharagpur, for their support to carry out 
the work and hereby declare no conflict of interest.

References

[1] Monteverde F, Bellosi A, Luigi S. Processing and properties of ultra-high temperature 
ceramics for space applications. Mater Sci Eng 2008;485:415–21. 
[2] Levine SR, Opila EJ, Halbig MC, Kiser JD, Singh M, Salem JA. Evaluation of ultra-high 
temperature ceramics for aeropropulsion use. J Eur Ceram Soc 2002;22:2757–67. 
[3] Pastor M. Metallic borides: preparation of solid bodies, sintering methods and properties 
of solid bodies. In: Matkovich VI, editor. Boron and refractory borides. New York: Springer; 
1977. p. 457–93. 
[4] Meeson GA, Gorbunow AF. Activated sintering of zirconium boride. Inorg Mater 
1968;4:267–70. 
[5] Kinoshita M, Kose S, Hamanos Y. Hot-pressing of zirconium diboride–molybdenium 
disilicide mixtures. Yogyo-Kyokai-Shi 1970;78:32–41. 
[6] Guo SQ, Yang JM, Tanaka H, Kagawa Y. Effect of thermal exposure on strength of ZrB2- 
based composites with nano-sized SiC particles. Compos Sci Technol 2008;68:3033–40. 
[7] Niihara K, Nakahira A. In: Vincentini P, editor. Advanced structural inorganic composites.

[8] Mallik M, Roy S, Ray KK, Mitra R. Effect of SiC content, additives and process parameters 
on densification and structure–property relations of pressureless sintered ZrB2–SiC 
composites. Ceram Int 2013;39:2915–32. 
[9] Zhang SC, Hilmas GE, Fahrenholtz WG. Mechanical properties of sintered ZrB2–SiC 
ceramics. J Eur Ceram Soc 2011;31:893–901. 
[10] Liu Q, Han W, Zhang X, Wang S, Han J. Microstructure and mechanical properties of 
ZrB2–SiC composites. Mater Lett 2009;63:1323–5. 
[11] Ikegami M, Guo S, Kagawa Y. Densification behavior and microstructure of spark plasma 
sintered ZrB2-based composites with SiC particles. Ceram Int 2012;38:769–74. 
[12] Cao M, Wang S, Han W. Influence of nanosized SiC particle on the fracture toughness of 
ZrB2-based nanocomposite ceramic. Mater Sci Eng A 2010;527:2925–8. 
[13] Patel M, Singh V, Reddy JJ, Bhanu Prasad VV, Jayaram V. Densification mechanisms 
during hot pressing of ZrB2–20 vol% SiC composite. Scr Mater 2013;69:370–3. 
[14] Quo SQ. Densification of ZrB2-based composites and their mechanical and physical 
properties: a review. J Eur Ceram Soc 2009;29:995–1011. 
[15] Zhu M, Wang Y. Pressureless sintering ZrB2–SiC ceramics at low temperatures. Mater 
Lett 2009;63:2035–7. 
[16] Zhang X, Liu Q, Han W, Han J. Microstructure and mechanical properties of ZrB2–SiC 
nanocomposite ceramic. Scr Mater 2009;61(7):690–2. 
[17] Tripp WC, Davis HH, Graham HC. Effect of an SiC addition on the oxidation of ZrB2. 
Am Ceram Soc Bull 1973;52(8): 612–6. 
[18] Rezaie A, Fahrenholtz WG, Hilmas GE. Oxidation of zirconium diboride-silicon carbide 
at 1500 ◦C at a low partial pressure of oxygen. J Am Ceram Soc 2006;89(10): 3240–5. 
[19] Mashhadi M, Khaksari H, Safi S. Pressureless sintering behavior and mechanical 
properties of ZrB2–SiC composites: effect of SiC content and particle size. J Mater Res Technol 
2015;4(4):416–22. 
[20] Sciti D, Guicciardi S, Bellosi A. Properties of a pressureless-sintered ZrB2–MoSi2 ceramic 
composite. J Am Ceram Soc 2006; 89(7):2320–2