Biaxial estimation of biomechanical constitutive parameters of passive porcine sclera soft tissue

Zwelihle Ndlovu1,2, Dawood Desai2, Thanyani Pandelani1,3, Harry Ngwangwa1, Fulufhelo Nemavhola1*,

1Unisa Biomedical Engineering Research Group, Department of Mechanical Engineering, School of Engineering, College of Science Engineering and Technology, University of South Africa, Pretoria, 0001, South Africa

2Department of Mechanical and Mechatronics Engineering, Faculty of Engineering and Built Environment, Tshwane University of Technology

3Council for Scientific and Industrial and Research, Defence and Security Cluster, Brummeria, Pretoria, 0001

*Correspondence: masitfj@unisa.ac.za ; Tel.: (+27 (011) 471 2765)

Abstract

This study assesses the modelling capabilities of four constitutive hyperplastic material models to fit the experimental data of the porcine sclera soft tissue. It further estimates the material parameters and discusses their applicability to a finite element model by examining the statistical dispersion measured through the standard deviation. Fifteen sclera tissues were harvested from porcine’ slaughtered at an abattoir and were subjected to equi-biaxial testing. The results show that all the four material models yielded very good correlations at correlations above 96 %. The polynomial (anisotropic) model gave the best correlation of 98 %. However, the estimated material parameters varied widely from one test to another such that there would be needed to normalise the test data to avoid long optimisation processes after applying the average material parameters to finite element models. However, for application of the estimated material parameters to finite element models, there would be needed to consider normalising the test data to reduce the search region for the optimisation algorithms. Although the polynomial (anisotropic) model yielded the best correlation, it was found that the Choi-Vito had the least variation in the estimated material parameters thereby making it an easier option for application of its material parameters to a finite element model and also requiring minimum effort in the optimisation procedure. For the porcine sclera tissue, it was found that the anisotropy more influenced by the fiber-related properties than the background material matrix related properties.

Keywords: Soft tissue mechanics; sclera tissue; porcine eye; biaxial testing; biomechanical analysis; constitutive hyperplastic material models; constitutive parameters

- Introduction

It is reported that majority of the vision impairment may be prevented or treated if caught early and correct therapies are implemented. Globally, 86.1 million cases leading to the moderate and severe vision impairment were caused by under corrected refractive error.  Due to increase in aging population in many countries across the globe, vision impairment including uncorrected refractive error, glaucoma and contract were reported to be in the rise. The rise in vision impairment is due to rising sociodemographic status and life expectancy witnessed in number of countries globally [1-4]. It is reported that 4.8 million and 21.4 million people are blind and visually impaired in 48 countries of sub-Saharan Africa [5]. In addition, Africa has been reported to be carrying approximately 19 % of the global blindness [6]. Blindness prevalence rates vary widely but the evidence suggests that approximately 1 % of people in sub-Saharan Africa are blind [7]. Visual impairment is a significant health problem in the sub-Saharan Africa. The major eye conditions include cataracts, uncorrected refractive errors, glaucoma, age-related macular degeneration, corneal opacities, diabetic retinopathy, trachoma, and onchocerciasis [8, 9]. In addition, Glaucoma is labelled as world-wide problem of the eye diseases where 111 million of individuals projected to be affected in 2040 [10]. Therefore, it is vital that the biomechanical properties and computational models of the eye soft tissues are developed with the view to understand the mechanisms of various diseases of the eye. Biomechanical properties of eye soft tissues are vital in improving insight into how eye diseases progresses [11].

Biomechanical properties of the soft tissues have been utilised previously to study mechanical behaviour [12-14]. The progression of the diseases was also studied by developing accurate and reliable computational models [15, 16]. The detailed computational models of the eye request a thorough study of mechanical properties including the fitting of constitutive hyperelastic models. Previously, different biomechanical properties of the different ocular tissues including sclera [17-19], orbital connective tissue and fat [20, 21], cornea [22-24], and extraocular muscles [25, 26]. Sclera is normally associated with Near-sightedness (myopia) and therefore there is considerable amount of work done on the investigating the biomechanical of sclera [27, 28].  In particular, the mechanical properties of the sclera are critical for the development of synthetic materials for the replacement of eye tissues. This is even so because globally, there has been the rise of accident where organ such as eye maybe lost due to accidents. In our previous studies, we presented the biaxial mechanical characterisation of the sheep sclera soft tissue [28]. In this study, the Fung and Choi-Vito hyperelastic constitutive models were fitted on the biaxial tensile data. Finite Element Modelling has been previously utilised in studying how soft tissues behave under mechanical loading [29-36]. These constitutive parameters generated by fitting biaxial tensile data may be utilized for detailed study of the diseases progression in the eye as well as understanding pain dissemination based on the needle injection in the sclera for treatment [37, 38].

In this paper, we present the biaxial biomechanical properties of the porcine sclera soft tissue. The porcine anatomy has been reported to be like that of human being, therefore, it is believed that the biaxial mechanical data presented in this study will be useful for studying human eye diseases.  Therefore, the aim of this study is to generate constitutive parameters of the porcine sclera soft tissues subjected to equi-biaxial loading. Fung, Choi-Vito, Holzapfel (200) and Polynomial (Anisotropic) hyperelastic constitutive models are fitted in the equi-biaxial tensile data to estimate the constitutive materials parameters. To our knowledge, there is no study that looked at utilising and comparing the Fung, Choi-Vito, Holzapfel (200) and Polynomial (Anisotropic) hyperelastic constitutive models in estimating the materials (porcine sclera soft tissue) parameters.

- Methods and materials

2.1 Sample preparation

The sample consists of 15 sclera soft tissue harvested from the local abattoir. To preserve the mechanical properties of the sclera soft tissue, the specimen was collected within 4 to 6 hours after slaughter as discussed [39]. The detailed tissue preparation of the Porcine sclera is like what we have previously presented [28]. To avoid possible deterioration of the sclera tissue including dehydration, specimen was placed in ice bag on the way to the Biomechanics Lab. During further processing, the unwanted ocular tissues was removed from the porcine eye using surgical blades. Two square samples of 12 x 12 mm (Fig. 1) were cut from each eye roughly 4 to 6 mm away from the optic nerve head and corneal limbus to reduce thickness variation. Vernier caliper was then utilized to measure the thickness of the sclera tissue. Randomly, the thickness of the sclera tissue was measured in four different places and the average thickness was taken for further processing of the data. Specimen were subjected to visual inspection before individually subjected to biaxial testing equipment. Reason for visual inspection was to ensure that there is no physical damage on the tissue that may influence the mechanical data. Samples were dipped and kept in isotonic solution 9.0 g/l at pH of 5.5 for about 15 to 20 minutes before testing.

Figure 1. Porcine sclera tissue samples (a) cut from each eye immediately after the delivery from the abattoir to the Unisa Biomechanics Laboratories with a sketch showing how the tissue was excised from the Porcine eye (b). The reference axis where define in such a way that the longitudinal direction is from the cornea to the base while circumferential direction is 90o with the longitudinal direction.

2.2 Mechanical testing

Biaxial mechanical properties of the porcine sclera soft tissue were captured using custom-built biaxial testing device, Bio-Tester 5000 from Cellscale (Waterloo, Canada) with load capacity of 23000 mN and accuracy of 5000 µN (Fig.2). Custom made tines were utilized to clamp the sclera soft tissue on all sides when eqi-biaxial force is applied. Strain rate of between 0.0133 to 0.89 mm/s was applied during biaxial testing of each sample. To mimic the body temperature, the water bath was heated to 37 oC. the temperature sensor is integrated in the custom-built biaxial device to ensure that the temperate is kept constant through testing. X and y directions were considered as circumferential and longitudinal directions, respectively. Four (4) CellScale BioRakes were used to mount the specimens to develop mechanical properties. On both x and y direction, all fourteen (15) specimens were subjected to 25% strain.

Figure 2. Experimental set-up of porcine sclera tissue subjected to biaxial tensile loading (Bio-Tester 5000 from Cellscale) (Waterloo, Canada). The hooks (BioRakes) were utilised in securing the sclera tissue and were punched thoroughly before they are inserted in the warm (37oC) of isotonic solution 9.0 g/l at pH of 5.5

- Theoretical framework

  - Tissue stress-strain analysis

In this study the stresses were calculated through the first Piola-Kirchoff stress T in the two-directions using the equation:

Tii=FiiLi0h0											(1)

Where F is the load vector in directions i=1,2 and for the current study these indices represent longitudinal (cross-fiber-direction) and circumferential (fiber-direction) direction. The index 0 denotes the undeformed state. L represents tissue length, and h represents tissue thickness.

The finite strains were calculated by the formula:

εi=Li-Li0Li0											(2)

These stress results however are noisy therefore they were further filtered with an 8-point moving average filter in Excel. The data were resampled and further smoothened using a quadratic function.

3.2	Constitutive modelling

The passive response of a biological soft tissue is more complex than the response of elastic solids due to the fact that they undergo finite deformations under mechanical loads [40, 41]. Thus, the passive phases of the tissues’ deformations are considered using the nonlinear theory of hyperelasticity. The most useful quantity in deriving the expressions for the passive response of materials that undergo finite deformation is the strain energy function [41]. There is a huge number of variations of its implementation in the literature depending on different cases. In this study, we assume that the tracheal tissue is anisotropic and incompressible, therefore we apply and study the material parameters from six models namely the Fung, Choi-Vito, Holzapfel (2000), and Polynomial (Anisotropic) models. In the following sections, these models are presented in terms of their strain energy functions.

3.2.1 The Fung model

The Fung model is a hyperelastic anisotropic material model for stress-strain description of arterial wall. It is phenomenological in nature and its incompressible form is given by [42].

W=c2eQ-1										(3)

Where Q=b1Eθθ2+b2EZZ2+b3ERR2+2b4EθθEZZ+2b5EZZERR+2b6ERREθθ; and  bi are the material parameters.

3.2.2	Choi-Vito model

Choi-Vito model is hyperelastic anisotropic material model developed for canine pericardium. The model is fully phenomenological and formulated through the components of Green-Lagrange strain tensor. The model is implemented in an exponential format and its strain-energy function is expressed as [43].

W=b0expb1E112+expb2E222+exp2b3E11E22-3				(4)

Where bi are the material parameters.

3.2.3	The Holzapfel (2000) model

This model is hyperelastic anisotropic material model for stress-strain description of arterial layers. It is constituted by forms of the strain energy function that represent isotropy and anisotropy. Thus, its strain energy function is given by [44].

W=c12c2expc2I4-12-1								(5)

Where ci are the material parameters. The model is implemented in an exponential format.

3.2.4	The polynomial (anisotropic) model

Like its name, this model is hyperelastic anisotropic material model whose strain energy function is expressed as a polynomial series of isotropic and anisotropic strain invariants given as [45].

W=i=13aiI1-3i+j=13bjI2-3j+k=26ckI4-1k+m=26emI6-1m	(6)

Where ai,bj,ck, and em are material parameters.

The four material models are classified further according to the type of material parameters that they represent in Table 1. From the table, the models can be grouped into two main classes: those that model the soft tissue as layers of general material matrix, and those that model the soft tissue as composite material with embedment of fiber structures within the layers of material matrix.

Table 1. The classification of the four hyperelastic anisotropic material models according to the material properties they represent. The Fung and Choi-Vito are classified as the models that that model the soft tissue as layers of general material matrix, while the Polynomial (anisotropic) and Holzapfel 2000 models are those that model the soft tissue as composite material with embedment of fiber structures within the layers of material matrix.

| Model |  | Stress-like material parameter |  | Dimensionless material parameter |  | Stress-like material parameter referred to material matrix property |  | Stress-like material property referred to fiber property |  | Dimensionless material property referred to fiber property |  | Material parameter referred to fiber angle orientation |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polynomial (anisotropic) |  |  |  |  |  | ✔ (ai, bj) |  | ✔ (ck) |  |  |  | ✔ (ϕ) |
| Fung |  | ✔ (c) |  | ✔ (bi, i =1…6) |  |  |  |  |  |  |  |  |
| Choi-Vito |  | ✔ (b0) |  | ✔ (bi, i =1…3) |  |  |  |  |  |  |  |  |
| Holzapfel 2000 |  |  |  |  |  | ✔ (μ) |  | ✔ (k1) |  | ✔ (k2) |  | ✔ (ϕ) |

3.3	Data analysis

In this study, we use the constrained optimisation by linear approximation algorithm (COBYLA (3rd party: SciPy)) implemented in Hyperfit software for fitting the equi-biaxial tensile experimental data of Fung, Choi-Vito, Holzapfel (2000), and Polynomial (Anisotropic) hyperelastic constitutive models given in Equations (3)-(6). The coefficient of determination, R2 which measure the correlation of one variable with another is evaluated for each model. The coefficient of determination (R2) (also known as Nash-Sutcliffe coefficient) is defined as follows [46-48]:

R2=1-i=1nye-ym2i=1nye-ye2       								 (7)

Where ye is the experimental data,  ym is the model predicted data, ye is the average value of the experimental data, the indices i, …, n denote the data points, and R2ϵ〈-∞,1〉, where a perfect fit is defined for R2=1.

- Results

Stress-strain curves for the porcine sclera soft tissue subjected to equi-biaxial tensile loading are plotted in Figure 2. The stress-strain curves for porcine sclera soft tissue show the tissue has a well-defined nonlinear behaviour as the tissue gets stretched from the toe region to 25% strain.

Figure 2. Porcine sclera soft tissue (N=18) subjected to equi-biaxial mechanical forces showing stress (kPa) vs strain mechanical properties up to 25 % strain (a) Circumferential and (b) Longitudinal. Test 4 and Test 3 showing highest and lowest tress in the circumferential direction, respectively. Additionally, Test 1 showing the highest stress and Test 15 showing the lowest stress in the longitudinal direction, respectively.

This study is aimed at estimating the biomechanical material parameters of a porcine sclera using four different constitutive material models namely Fung, Choi-Vito, Holzapfel 2000, and polynomial (anisotropic) models. All the above materials models are hyperelastic anisotropic models which employ different modelling frameworks as presented in Equations (3) - (6) in Section 3.2. The material parameters for each model for all the fifteen tests are given in Tables (3) - (5). The tabulated results show that all the models yield very good correlations at greater than 96% with standard deviations of less than 3.2%. This implies that the model predictions were very close to the mean stress-strain curves for all the four models in this study.

Table 2: Estimated material parameters of porcine sclera soft tissue loaded biaxially using Polynomial (anisotropic) hyperelastic constitutive model including the coefficient of determination (R2) of each specimen (N =15). The average constitutive (a1, a2, a3, b1, b2, b3, c2, c3, c4, c5, c6,  φ and R2) parameters are also included.

|  | R2 | a1 | a2 | a3 | b1 | b2 | b3 | c2 | c3 | c4 | c5 | c6 | φ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | 0.953 | 0.045 | 0.014 | 0.035 | -0.002 | -0.003 | -0.002 | -0.027 | -0.007 | -0.018 | -0.010 | 0.994 | 0.944 |
| S2 | 0.976 | 0.023 | 0.048 | 0.039 | 0.000 | 0.001 | -0.005 | -0.015 | 0.001 | 0.006 | 0.010 | 0.022 | 0.003 |
| S3 | 0.983 | -0.011 | 0.102 | -0.072 | -0.220 | -0.089 | -0.133 | -0.005 | 0.074 | 0.201 | 0.174 | -0.259 | 0.268 |
| S4 | 0.954 | 0.018 | 0.055 | -0.051 | 0.035 | 0.031 | 0.021 | 0.011 | -0.022 | -0.041 | -0.040 | 1.217 | 0.911 |
| S5 | 0.948 | 0.006 | 0.216 | -0.302 | -0.095 | -0.042 | 0.007 | -0.039 | 0.150 | 0.035 | 0.050 | -0.011 | 0.016 |
| S6 | 0.990 | 0.010 | -0.016 | 0.074 | 0.233 | -0.158 | 0.186 | -0.008 | -0.018 | 0.247 | 0.394 | -0.825 | -0.083 |
| S7 | 0.997 | 0.014 | 0.007 | 0.298 | -0.118 | -0.285 | -0.112 | -0.038 | 0.245 | -0.217 | -0.004 | -0.019 | 0.199 |
| S8 | 0.998 | 0.003 | 0.225 | 0.206 | -0.305 | 0.319 | -0.283 | 0.006 | -0.096 | 0.195 | -0.325 | 0.310 | -0.089 |
| S9 | 0.991 | 0.004 | 0.087 | 0.039 | 0.012 | -0.082 | 0.026 | -0.005 | -0.006 | 0.024 | 0.016 | 0.015 | -0.056 |
| S10 | 0.993 | 0.015 | 0.093 | 0.006 | -0.043 | 0.008 | -0.004 | 0.000 | -0.046 | 0.154 | 0.048 | -0.147 | -0.085 |
| S11 | 0.998 | 0.008 | 0.201 | -0.061 | -0.425 | 0.155 | 0.060 | -0.012 | 0.020 | 0.081 | -0.155 | 0.180 | 0.216 |
| S12 | 0.989 | 0.028 | -0.011 | 0.075 | -0.289 | -0.477 | -0.220 | -0.004 | 0.003 | 0.465 | 0.198 | -0.928 | 0.460 |
| S13 | 0.989 | 0.028 | -0.011 | 0.075 | -0.289 | -0.477 | -0.220 | -0.004 | 0.003 | 0.465 | 0.198 | -0.928 | 0.460 |
| S14 | 0.992 | -0.013 | 0.081 | -0.707 | 0.254 | -0.952 | 0.325 | 0.031 | -0.058 | 0.762 | 0.610 | -4.150 | 0.592 |
| S15 | 0.991 | -0.001 | 0.375 | -0.293 | 0.335 | -0.371 | 0.014 | -0.003 | -0.032 | -0.166 | 0.269 | 0.152 | 0.081 |
| Average | 0.983 | 0.012 | 0.098 | -0.043 | -0.061 | -0.161 | -0.023 | -0.007 | 0.014 | 0.146 | 0.096 | -0.292 | 0.256 |
| STD | 0.017 | 0.015 | 0.108 | 0.233 | 0.215 | 0.301 | 0.152 | 0.017 | 0.082 | 0.250 | 0.217 | 1.185 | 0.337 |

However, the polynomial (anisotropic) model yielded the best correlation at an average of 98.3% and an average standard deviation of approximately 1.73%, while the Fung model yielded the lowest average correlation of 96.4% with an average standard deviation of 3.2%. The Choi-Vito and Holzapfel models had similar average correlations of 97.2% with average standard deviations of 1.65% and 2.98%, respectively.

Table 3. Estimated material parameters of porcine sclera soft tissue loaded biaxially using Fung hyperelastic constitutive model including the coefficient of determination (R2) of each specimen (N =15). The average constitutive (c, b1, b2, b3, b4, b5, b6 and R2) parameters are also included.

| Test # | R2 | c | b1 | b2 | b3 | b4 | b5 | b6 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | 0.985 | 1.527 | 1.264 | 1.228 | -0.655 | 0.375 | 0.243 | 0.329 |
| S2 | 0.959 | 1.533 | 0.952 | 1.139 | -0.420 | 0.460 | 0.569 | -0.027 |
| S3 | 0.993 | 1.050 | 1.200 | 1.178 | -0.118 | 0.533 | 0.379 | 0.628 |
| S4 | 0.900 | 0.137 | 3.965 | 1.971 | -1.625 | 2.864 | 1.851 | -1.999 |
| S5 | 0.971 | 0.500 | 1.924 | 2.824 | -0.643 | 1.242 | 1.147 | 0.739 |
| S6 | 0.907 | 0.791 | 1.293 | 0.801 | -0.345 | 1.038 | 0.630 | 0.289 |
| S7 | 0.915 | 0.822 | 3.911 | 1.877 | 1.002 | 2.527 | 2.473 | 0.068 |
| S8 | 0.957 | 0.929 | 1.299 | 0.902 | -0.388 | 1.071 | 0.563 | 0.513 |
| S9 | 0.993 | 0.558 | 2.701 | 3.301 | 1.488 | 3.039 | 2.612 | 2.439 |
| S10 | 0.983 | 0.158 | 4.686 | 3.439 | -0.125 | 2.827 | 1.727 | 2.578 |
| S11 | 0.960 | 0.960 | 1.102 | 0.808 | -0.130 | 0.298 | 0.297 | 0.260 |
| S12 | 0.983 | 1.286 | 1.000 | 0.857 | -0.335 | 0.390 | 0.265 | 0.283 |
| S13 | 0.990 | 1.286 | 1.671 | 0.601 | -0.280 | 1.123 | 0.507 | 0.614 |
| S14 | 0.983 | 1.026 | 0.976 | 1.200 | -0.374 | 1.074 | 0.635 | 0.465 |
| S15 | 0.984 | 0.910 | 1.517 | 0.679 | -0.318 | 1.111 | 0.442 | 0.546 |
| Average | 0.964 | 0.898 | 1.964 | 1.520 | -0.218 | 1.331 | 0.956 | 0.515 |
| STD | 0.031 | 0.413 | 1.202 | 0.921 | 0.679 | 0.949 | 0.783 | 1.002 |

Table 4. Estimated material parameters of porcine sclera soft tissue loaded biaxially using Choi-Vito hyperelastic constitutive model including the coefficient of determination (R2) of each specimen (N =15). The average constitutive (c, b1, b2 and b3 and R2) parameters are also included.

| Test # | R2 | c | b1 | b2 | b3 |
| --- | --- | --- | --- | --- | --- |
| S1 | 0.979 | 0.004 | 3.180 | 11.421 | 39.018 |
| S2 | 0.956 | 0.006 | -2.627 | 10.015 | 21.673 |
| S3 | 0.967 | 0.011 | 21.724 | 26.703 | 11.276 |
| S4 | 0.985 | 0.017 | 39.952 | 17.770 | 9.632 |
| S5 | 0.981 | 0.024 | 23.364 | 27.074 | 17.790 |
| S6 | 0.935 | 0.011 | 47.858 | 17.579 | 6.936 |
| S7 | 0.974 | 0.012 | 40.348 | 14.985 | 14.470 |
| S8 | 0.976 | 0.018 | 36.901 | 25.357 | 14.662 |
| S9 | 0.990 | 0.022 | 29.680 | 34.177 | 23.643 |
| S10 | 0.983 | 0.029 | 17.587 | 16.756 | 15.163 |
| S11 | 0.981 | 0.015 | 27.327 | 19.054 | 2.194 |
| S12 | 0.985 | 0.039 | 20.816 | 18.381 | 13.656 |
| S13 | 0.969 | 0.036 | 34.998 | 18.118 | 15.893 |
| S14 | 0.994 | 0.093 | 14.175 | 14.101 | 13.318 |
| S15 | 0.946 | 0.024 | 31.969 | 14.387 | 2.134 |
| Average | 0.972 | 0.023 | 26.141 | 20.467 | 15.324 |
| STD | 0.016 | 0.021 | 13.494 | 6.348 | 8.741 |

Table 5: Estimated material parameters of porcine sclera soft tissue loaded biaxially using Holzapfel (2000) hyperelastic constitutive model including the coefficient of determination (R2) of each specimen (N =15). The average constitutive (c, b1, b2, b3 and R2) parameters are also included.

| Test # | R2 | μ | k1 | k2 | φ |
| --- | --- | --- | --- | --- | --- |
| S1 | 0.982 | 0.000 | 0.039 | 9.303 | 0.814 |
| S2 | 0.972 | 0.000 | 0.036 | 5.250 | 2.240 |
| S3 | 0.984 | 0.000 | 0.098 | 6.017 | -0.389 |
| S4 | 0.974 | 0.000 | 0.059 | 7.572 | 0.856 |
| S5 | 0.864 | 0.068 | 0.048 | 7.676 | 0.311 |
| S6 | 0.976 | 0.000 | 0.052 | 6.142 | -0.362 |
| S7 | 0.980 | 0.000 | 0.081 | 6.658 | 0.630 |
| S8 | 0.983 | 0.000 | 0.077 | 8.141 | 0.854 |
| S9 | 0.975 | 0.000 | 0.042 | 5.971 | 0.755 |
| S10 | 0.978 | 0.000 | 0.078 | 3.696 | 0.649 |
| S11 | 0.978 | 0.000 | 0.091 | 4.981 | 0.723 |
| S12 | 0.980 | 0.000 | 0.116 | 7.329 | 0.457 |
| S13 | 0.980 | 0.000 | 0.078 | 7.284 | 0.778 |
| S14 | 0.982 | 0.013 | 0.083 | 8.418 | 0.549 |
| S15 | 0.990 | 0.000 | 0.101 | 3.848 | 0.854 |
| Average | 0.972 | 0.005 | 0.074 | 6.767 | 0.654 |
| STD | 0.029 | 0.017 | 0.024 | 2.263 | 0.562 |

In terms of statistical dispersion in the estimated material parameters by the four models, the polynomial (anisotropic) model had the largest variance with the widest scatter in the material parameters over the fifteen different tests. An evaluation of the standard deviation percentage yielded deviations from 110 % to 660 % for the polynomial (anisotropic) model. On the other hand, the Choi-Vito model had the smallest variance in the material parameters with deviations between 31 % and 91 %. This result might not be surprising considering that the Choi-Vito model was originally formulated for the pericardium tissue [43, 49, 50] which, in much respect, may be similar in functionality to the sclera tissue. The implications of such deviations in terms of applying the estimated average material parameters directly to finite element (FE) models is problematic and this has been discussed in the next section. Form Figure 3, Polynomial (Anisotropic) constitutive model showing the highest R2 of 0.983 and the lowest R2 of 0.964 shown for Fung constitutive model. On the other hand, Figure 4 shows that the Porcine sclera soft tissue was found to be much stiffer in the circumferential direction with stress values taken at 15% strain.

Figure 3. Average Coefficient of Determination (R2) (with standard error) of the Porcine soft tissue sclera calculated for Holzapfel (2000) , Choi-Vito, Fung and Polynomial (Anisotropic) Model hyperelastic constitutive models, with Polynomial (Anisotropic) constitutive model showing the highest R2 of 0.983 and the lowest R2 of 0.964 observed for Fung constitutive model.

(a)                                                                                           (b)

Figure 4. First Piola-Kirchhhoff Stress (kPa) values taken at 15 % engineering strain of the Porcine soft tissue subjected to biaxial tension in two laoding directions (a) Longitutidnal and (b) Circumferencial

Table 6. Fitting of hyperelastic models (N =15) showing box plot properties of the coefficient of determination (R2) showing Q1, Median and Q3

|  | Polynomial Model | Fung Model | Choi-Vito Model | Holzapfel (2000) Model |
| --- | --- | --- | --- | --- |
| Min | 0.948 | 0.900 | 0.935 | 0.864 |
| Q1 | 0.980 | 0.958 | 0.968 | 0.976 |
| Median | 0.990 | 0.983 | 0.979 | 0.980 |
| Q3 | 0.993 | 0.985 | 0.984 | 0.982 |
| Max | 0.998 | 0.993 | 0.994 | 0.990 |
| IQR | 0.013 | 0.027 | 0.016 | 0.006 |

- Discussion

The results of correlations between model predictions and tests presented in Section 4 should never be taken at face value. It should be noted that a model is applied to a given set of experimental data from which the material parameters are estimated. Thus, each material model is optimised for each fresh set of experimental data with totally different target values, and therefore it is likely to yield material parameters that are different from those obtained from the other tests. This is where some form of calibration may become necessary to eliminate huge variances in the model parameters from one test to another [51-54]. Dubuis et al. [55] employed a calibration technique in which the FE itself was calibrated using 3D CT scans.

Therefore, in applying the average material parameters obtained here to an FE model, one may need to consider implementing an optimisation procedure in which these average values may be used as seed values [56]. Kollmann et al. [56] applied such methods for optimisation of the parameters used in FE modelling of asphalt mixtures. For models with large numbers of material parameters such as the polynomial (anisotropic) model in this study, it might be prudent to conduct an initial sensitivity analysis to determine the most influential material parameters. Biaxial tensile testing has been utilised in understanding the mechanical properties of soft tissues. Additionally, hyperelastic constitutive models have also been presented by fitting the constitutive models of the various soft tissues including heart myocardium [57-60] and omasum [61].

Despite the highest correlation obtained for the polynomial (anisotropic) model, the direct application of its parameters to an FE model can yield huge errors due to the wide scatter of its material parameters. One may need to prescribe huge range of its parameter space within which the optimisation algorithm can search for the optimal material parameters to give accurate correlation for any given random test. Among the four material models in this study, the Choi-Vito model offers the best chance for attaining accurate correlations when directly applied to an FE model with minimal effort of optimisation. For the Choi-Vito model, only the stress-like material parameter may take more time in searching for optimal material parameter at 91 % deviation from the mean value. Apart from the average value given in Table 4, the other best value from which to start the search for the stress-like material parameter for the Choi-Vito may be the gradient of the linear elastic portion of the stress-strain curve.

In terms of general material matrix anisotropy, both the Fung and Choi-Vito models do not show that the porcine sclera tissue is heavily anisotropic between the circumferential and longitudinal direction. However, the tissue seems to be different in material matrix in the radial direction from the Fung model. The values of ai and bj which also represent the material matrix properties in the polynomial (anisotropic) model show that there is no significant anisotropy between the circumferential and longitudinal directions. On the other hand, the ck material parameters in the polynomial (anisotropic) model and the ki parameters in the Holzapfel 2000 model, all of which represent material parameters related with fiber properties, exhibit significant anisotropy in Tables 2 and 5. This implies that the anisotropy in the porcine sclera tissue is mainly due to different fiber properties between the circumferential and longitudinal directions and not the background material matrix properties. It is difficult to establish in this study if the fiber orientation angle had any influence at the accuracy of the correlations in the polynomial (anisotropic) and Holzapfel 2000 models. This can be better investigated through the sensitivity analysis. Table 6 showing the showing box plot properties of the coefficient of determination (R2) showing Q1, Median and Q3, where it is clear that Fung model has larger range when compared to Holzapfel (2000) that has much lower range of the coefficient of determination (R2).

- Conclusion

The study applies four different hyperelastic material models to estimate the material parameters for the computational modelling of porcine sclera tissue. It is found that all the four material models produce very good correlations higher than 96 % with the polynomial (anisotropic) model yielding the highest correlation of 98 %. However, the variation of the material parameters from one test to another is a challenge as far as their direction application to FE models is concerned. For example, the polynomial (anisotropic) model has the minimum standard deviation of its material parameters from one test to another as 110%. Thus, the average material parameters obtained in this paper may result in inaccurate correlations in the FE predicted results. One way to deal with this challenge is to implement an optimisation routine which uses these material parameters as seed values. However, with such large spread in the parameter space, the search algorithm may take too long to converge especially with material models that have large numbers of estimated material parameters. Therefore, it is proposed that the test data should also be normalised r calibrated before application of the constitutive material models to reduce the variation in the estimated parameters thereby reducing the search region. In this study it is also found that the Choi-Vito model has the least variation in its material parameters. Thus, it might offer much better chance than the other models of convergence to material parameters that can yield very good correlations for the FE model. In terms of the models that are based on fiber-property formulation as identified in Table 1, the Holzapfel 2000 model offers a better option as compared to the polynomial (anisotropic) model for faster convergence as its material variation is much lower between the two models. As far as anisotropy in the porcine sclera tissue is concerned, both the polynomial (anisotropic) model and the Holzapfel 2000 model show that the fiber properties have more influence than the background material matrix. It is not clear if the angle of fiber orientation has any influence in the results. This might require more investigation.

Limitation

- This experiment did not segment porcine sclera per region. This may lead to unclear results since it was reported that some regions in the sclera exhibit anisotropic while others do not

- No imaging was done in this experiment, hence the fiber direction can be determined with certainty

Author contributions

F.N, H.N, Z.N, D.D and T.P contributed to conception, design, and interpretation, drafted the manuscript, Z.N, T.P and F.N contributed to the interpretation of the data and critically revised the manuscript, and finally D.D, F.N, H.N and T.P contributed to conception, design, data analysis, and interpretation, drafted and critically revised the manuscript. Z.N and F.N contributed to data acquisition and analysis. All authors gave final approval and agree to be accountable for all aspects of the work.

Competing interests

The authors declare no competing interests.

Additional information

Correspondence and requests for materials should be addressed to F.N.

Reprints and permissions information is available at www.nature.com/reprints.

Acknowledgments

Support from the National Research Foundation (NRF) Grant number (129380) is gratefully acknowledged. Unisa CAPEX Programme supported the acquisition of biaxial testing machine in the Department of Mechanical Engineering, School of Engineering, College of Science Engineering and Technology.

Corresponding author

Correspondence to Fulufhelo Nemavhola

References

1.	Steinmetz, J.D., et al., Causes of blindness and vision impairment in 2020 and trends over 30 years, and prevalence of avoidable blindness in relation to VISION 2020: the Right to Sight: an analysis for the Global Burden of Disease Study. The Lancet Global Health, 2021. 9(2): p. e144-e160.

2.	Flaxman, S.R., et al., Global causes of blindness and distance vision impairment 1990–2020: a systematic review and meta-analysis. The Lancet Global Health, 2017. 5(12): p. e1221-e1234.

3.	Pezzullo, L., et al., The economic impact of sight loss and blindness in the UK adult population. BMC health services research, 2018. 18(1): p. 1-13.

4.	Reddy, P.A., et al., Effect of providing near glasses on productivity among rural Indian tea workers with presbyopia (PROSPER): a randomised trial. The Lancet Global Health, 2018. 6(9): p. e1019-e1027.

5.	Stevens, G.A., et al., Global prevalence of vision impairment and blindness: magnitude and temporal trends, 1990–2010. Ophthalmology, 2013. 120(12): p. 2377-2384.

6.	Naidoo, K., Poverty and blindness in Africa. Clinical and Experimental Optometry, 2007. 90(6): p. 415-421.

7.	Lewallen, S. and P. Courtright, Blindness in Africa: present situation and future needs. British Journal of Ophthalmology, 2001. 85(8): p. 897-903.

8.	Buhrmann, R.R., et al., Prevalence of glaucoma in a rural East African population. Investigative ophthalmology & visual science, 2000. 41(1): p. 40-48.

9.	Dastjerdi, S., B. Akgöz, and Ö. Civalek, On the shell model for human eye in Glaucoma disease. International Journal of Engineering Science, 2021. 158: p. 103414.

10.	Tham, Y.-C., et al., Global prevalence of glaucoma and projections of glaucoma burden through 2040: a systematic review and meta-analysis. Ophthalmology, 2014. 121(11): p. 2081-2090.

11.	Ferrara, M., et al., Biomechanical properties of retina and choroid: a comprehensive review of techniques and translational relevance. Eye, 2021: p. 1-15.

12.	Ngwangwa, H.M. and F. Nemavhola, Evaluating computational performances of hyperelastic models on supraspinatus tendon uniaxial tensile test data. Journal of Computational Applied Mechanics, 2021. 52(1): p. 27-43.

13.	Nemavhola, F., Biaxial quantification of passive porcine myocardium elastic properties by region. Engineering Solid Mechanics, 2017. 5(3): p. 155-166.

14.	Nemavhola, F., Study of biaxial mechanical properties of the passive pig heart: material characterisation and categorisation of regional differences. International Journal of Mechanical and Materials Engineering, 2021. 16(1): p. 1-14.

15.	Nemavhola, F., Fibrotic infarction on the LV free wall may alter the mechanics of healthy septal wall during passive filling. Bio-medical materials and engineering, 2017. 28(6): p. 579-599.

16.	Nemavhola, F., Detailed structural assessment of healthy interventricular septum in the presence of remodeling infarct in the free wall–A finite element model. Heliyon, 2019. 5(6): p. e01841.

17.	Karimi, A., et al., Mechanical properties of the human sclera under various strain rates: elastic, hyperelastic, and viscoelastic models. Journal of Biomaterials and Tissue Engineering, 2017. 7(8): p. 686-695.

18.	Ji, F., et al., Mechanical properties of scleral collagen fibers obtained using a new fiber-based specimen-specific model of sclera microstructure. Investigative Ophthalmology & Visual Science, 2021. 62(8): p. 1652-1652.

19.	Bronte-Ciriza, D., et al., Estimation of scleral mechanical properties from air-puff optical coherence tomography. Biomedical Optics Express, 2021. 12(10): p. 6341-6359.

20.	Yoo, L., et al., Viscoelastic properties of bovine orbital connective tissue and fat: constitutive models. Biomechanics and modeling in mechanobiology, 2011. 10(6): p. 901-914.

21.	Schoemaker, I., et al., Elasticity, viscosity, and deformation of orbital fat. Investigative ophthalmology & visual science, 2006. 47(11): p. 4819-4826.

22.	Mahdian, M., et al., Characterization of the transient mechanical properties of human cornea tissue using the tensile test simulation. Materials Today Communications, 2021. 26: p. 102122.

23.	Yazdi, A.A., et al., Characterization of non-linear mechanical behavior of the cornea. Scientific reports, 2020. 10(1): p. 1-10.

24.	Branislav, H., et al., Glaucoma vs. biomechanical properties of cornea. Strojnícky časopis-Journal of Mechanical Engineering, 2019. 69(2): p. 111-116.

25.	Eckhardt, J., et al., Biochemical and Mechanical Properties of Murine Extraocular Muscles. Biophysical Journal, 2017. 112(3): p. 101a-102a.

26.	ZHANG, X., et al., Mechanical Properties of Porcine Extraocular Muscles in Vitro. Journal of Taiyuan University of Technology, 2017: p. 02.

27.	Tanaka, K., K. Yamamoto, and T. Katayama, Evaluation of mechanical properties of porcine sclera, in Recent Advances in Structural Integrity Analysis - Proceedings of the International Congress (APCF/SIF-2014), L. Ye, Editor. 2014, Woodhead Publishing: Oxford. p. 311-315.

28.	Ndlovu, Z., F. Nemavhola, and D. Desai, BIAXIAL MECHANICAL CHARACTERIZATION AND CONSTITUTIVE MODELLING OF SHEEP SCLERA SOFT TISSUE. Russian Journal of Biomechanics/Rossijski Zurnal Biomehaniki, 2020. 24(1).

29.	Masithulela, F. The Effect of Over-Loaded Right Ventricle During Passive Filling in Rat Heart: A Biventricular Finite Element Model. in ASME 2015 International Mechanical Engineering Congress and Exposition. 2015.

30.	Masithulela, F. Analysis of passive filling with fibrotic myocardial infarction. in ASME international mechanical engineering congress and exposition. 2015. American Society of Mechanical Engineers.

31.	Zhang, Y., et al., Finite-element based optimization of left ventricular passive stiffness in normal volunteers and patients after myocardial infarction: Utility of an inverse deformation gradient calculation of regional diastolic strain. Journal of the Mechanical Behavior of Biomedical Materials, 2021. 119: p. 104431.

32.	Sáez, P. and E. Kuhl, Computational modeling of acute myocardial infarction. Computer methods in biomechanics and biomedical engineering, 2016. 19(10): p. 1107-1115.

33.	Masithulela, F. The effect of over-loaded right ventricle during passive filling in rat heart: A biventricular finite element model. in ASME International Mechanical Engineering Congress and Exposition. 2015. American Society of Mechanical Engineers.

34.	Masithulela, F., Bi-ventricular finite element model of right ventricle overload in the healthy rat heart. Bio-medical materials and engineering, 2016. 27(5): p. 507-525.

35.	Masithulela, F.J., Computational biomechanics in the remodelling rat heart post myocardial infarction. 2016.

36.	Nemavhola, F., Mechanics of the septal wall may be affected by the presence of fibrotic infarct in the free wall at end-systole. International Journal of Medical Engineering and Informatics, 2019. 11(3): p. 205-225.

37.	Hans, S.A., S.Y. Bawab, and M.L. Woodhouse, A finite element infant eye model to investigate retinal forces in shaken baby syndrome. Graefe's Archive for Clinical and Experimental Ophthalmology, 2009. 247(4): p. 561-571.

38.	Dwyer, K.D. and K.L. Coulombe, Cardiac mechanostructure: Using mechanics and anisotropy as inspiration for developing epicardial therapies in treating myocardial infarction. Bioactive Materials, 2021. 6(7): p. 2198-2220.

39.	Nemavhola, F., Pig sclera stress-strain dataset under biaxial tensile testing. Mendeley Data, 2020. V1.

40.	Fung, Y., Structure and stress-strain relationship of soft tissues. American Zoologist, 1984. 24(1): p. 13-22.

41.	Fung, Y.-C., Mechanical properties of living tissues. Vol. 547. 1993: Springer.

42.	Chuong, C. and Y. Fung, Three-dimensional stress distribution in arteries. Journal of biomechanical engineering, 1983. 105(3): p. 268-274.

43.	Choi, H.S. and R. Vito, Two-dimensional stress-strain relationship for canine pericardium. Journal of biomechanical engineering, 1990. 112(2): p. 153-159.

44.	Holzapfel, G.A., T.C. Gasser, and R.W. Ogden, A new constitutive framework for arterial wall mechanics and a comparative study of material models. Journal of elasticity and the physical science of solids, 2000. 61(1): p. 1-48.

45.	Bursa, J., et al. Implementation of hyperelastic models for soft tissues in FE program and identification of their parameters. in Proceedings of the Sixth IASTED International Conference on Biomedical Engineering. 2008.

46.	Huang, L.-S. and J. Chen, Analysis of variance, coefficient of determination and F-test for local polynomial regression. The Annals of Statistics, 2008. 36(5): p. 2085-2109.

47.	Montgomery, D.C. and G.C. Runger, Applied statistics and probability for engineers. 2010: John Wiley & Sons.

48.	Barrett, J.P., The coefficient of determination—some limitations. The American Statistician, 1974. 28(1): p. 19-20.

49.	Feng, Y., et al., Computational Modeling for Surgical Reconstruction of Aortic Valve by Using Autologous Pericardium. IEEE Access, 2020. 8: p. 97343-97352.

50.	Rabkin, S.W. and P. Hsu, Mathematical and mechanical modeling of stress-strain relationship of pericardium. American Journal of Physiology-Legacy Content, 1975. 229(4): p. 896-900.

51.	Zeinali-Davarani, S., J. Choi, and S. Baek, On parameter estimation for biaxial mechanical behavior of arteries. Journal of biomechanics, 2009. 42(4): p. 524-530.

52.	Huang, J., et al., A comparison of calibration methods based on calibration data size and robustness. Chemometrics and Intelligent Laboratory Systems, 2002. 62(1): p. 25-35.

53.	Taylor, D.C., et al., Methods of model calibration. Pharmacoeconomics, 2010. 28(11): p. 995-1000.

54.	Mohan, N., et al., A review on composite materials and process parameters optimisation for the fused deposition modelling process. Virtual and Physical Prototyping, 2017. 12(1): p. 47-59.

55.	Dubuis, L., et al., Identification of the material parameters of soft tissues in the compressed leg. Computer Methods in Biomechanics and Biomedical Engineering, 2012. 15(1): p. 3-11.

56.	Kollmann, J., et al., Parameter optimisation of a 2D finite element model to investigate the microstructural fracture behaviour of asphalt mixtures. Theoretical and Applied Fracture Mechanics, 2019. 103: p. 102319.

57.	Ngwangwa, H., et al., Determination of Cross-directional and Cross-Wall Variations of Passive Biaxial Mechanical Properties of Rat Myocardium. Preprints, 2021. 2021090244.

58.	Nemavhola, F., et al., Understanding regional mechanics of rat myocardia by fitting hyperelatsic models. Research Square, 2021.

59.	Nemavhola, F., et al., Understanding regional mechanics of rat myocardia by fitting hyperelatic models. Research Square, 2021. DOI: https://doi.org/10.21203/rs.3.rs-957393/v1.

60.	Nemavhola, F., et al., Passive Biaxial Tensile Dataset of Three Main Rat Heart Myocardia: Left Ventricle, Mid-Wall and Right Ventricle. Preprints, 2021. 2021080153(Version 1).

61.	Lebea, L., et al., Biomechanical behaviour and hyperelastic model parameters identification of sheep omasum. Research Square, 2021. DOI: https://doi.org/10.21203/rs.3.rs-1015547/v1.