Effect of Injection System on Filling Time of Mold in VARTM Process to Manufacture Glass/Epoxy Composite Laminates

P.Ghabezi*1, S.Rajabi Jalall2

1 Mechanical Engineering, University of Galway, Ireland,

2 Department of Mechanical Engineering, University of Tarbiat Modares, Tehran, Iran.

Corresponding author’s E-mail address: pouyan.ghabezi@universityofgalway.ie

Abstract

The objective of this paper is to determine the optimized dimensions of the inlet tube to produce composite parts using VARTM method. Afterward, some samples with various diameters and lengths are produced using VARTM method while keeping the Vertical length of inlet tube on resin tank constant and also some samples were made by holding the length constant and changing the vertical images of inlet tube with various vertical distances. In both cases, experimental results are compared with simulation. The outcomes demonstrate that thicker inlet tube leads to lower ratio of energy drop to flow rate. Progression of the flow front will increase the length of movement route and the ratio of energy drop in different diameters to filled mold length will decrease and the velocities become closer. Also pressure drop and process duration will increase by increasing the length and the Vertical length of the inlet tube. In this paper the simulation gives a good agreement to experiments.

Keywords: Inlet tube dimensions, VARTM, velocity of flow front, Composites.

1. Introduction

Composite materials have been widely used in marine, automotive, aerospace, etc. industries because of their unique properties such as high strength; high modulus; low density; excellent resistance to fatigue, therefore many researchers have investigated their mechanical properties [, , ], their behavior in different environments [, ], their application in 3D printing [], and their behavior in presence of nanoparticles [, ]. Massive studies have been carried out so far investigating the impacts of effective parameters on resin motion velocity since, using this method; it is possible to achieve a proper design for producing large scale parts while confronting minimum complications. However, the influence of inlet tube has never been specifically analyzed. This paper theoretically and empirically inspects the effects of inlet tube on injection dies filling time to determine appropriate inlet tube dimensions. So far, carried out researches emphasizes on the importance of correctly estimating the inlet tube and injection location in different parts. Moreover, sample length, density and permeability along with vacuum pressure affect the position of the inlet tube. Placing the injection location to increase the resin conveying route increases the filling time and the possibility of incomplete part due to the less permeability resulted from lower pressure. Furthermore, substitution of groove injection, tube (Figure1 bottom-right) with typical injection tube has led to better results [, , , , , , , ]. Similarly, groove injection tube was used in this paper for performing the injection process. The studies of the inlet tube dimension effects can be stated as follows:

Nala et al. present an idea to use multi-segment injection line and omega tubes catch acceptable results in laboratory size molds [10]. In the last years, Owens [11], Vaidya [] and Yenilmez [], in their works present some of advantage using spiral tube(diagonal shear tube). Also Mack [] presents terms about energy drops in the injection tube. Lopatnikov [] and yoon [] investigated the filling time and variety of thickness of final parts through a closed-form solution effects of injection tube.

In this study, an injection tube with groove shears in cross of the die (see Figure 1, bottom-right) has been used. This makes uniform distribution of resin in die and lead to regular flow front. Permeability in cross section due to linear injection has insignificant effect on velocity and filling time. This case can be simulated in 2-dimension(X-Y) and third dimension (thickness) can be neglected.

2 Experimental and Simulation

2.1. Materials

In this research plain woven fabric E-glass were used with surface density 200 g/cm2 and the epoxy resin is from Axson (table 1). Thicknesses of preform and distribution layer are 2.55 and 1.4 mm respectively. Preform permeability factors are listed in table 2.

Table 1: Properties of used resin in tests [].

| resin | Resin density (g/cm3) | Viscosity at 25 oC (mPas) |
| --- | --- | --- |
| Epoxy (Epolam 2002) | 1.17 | 950 |

Table 2: Preform permeability factors.

| K2y (cm2) *10-6 | K2x (cm2) *10-6 | K1x (cm2) *10-6 |
| --- | --- | --- |
| 0.25 | 5.2 | 776 |

2.2. Experiments

In this work, 12 layers were provided from 200-gram (surface density) woven E-glass fibers in dimensions 300*500 mm with porosity 51.4% for each sample. Then sheet of distribution media was placed with thickness 1.4 mm and porosity 0.8 on top of the release ply. Attach plastic sheet on top of layers to act as a vacuum bag. Sealing between die and vacuum bag by two-side adhesive tape and apply respective vacuum pressure -0.8 bar and open to injection resin. Four samples are produced with internal diameter of inlet tube, D, in 2, 5, 8 and 12 mm with constant vertical length, Lv, 50 cm. and length, Lt, 55 cm. Inlet tube length effects made in four samples with lengths 20, 40, 70 and 110 cm with D = 5mm and Lv =20cm. Three samples were produced in vertical length of tube 15, 35 and 70 cm. Time of flow front position in different points are detected, and by using interpolation velocity are estimated versus distance from inlet point curves. Finally experimental results are compared with simulation results.

Figure 1: Experimental tests to determine optimum dimensions of inlet tube

3.2. Simulation of VARTM

Simple geometry can be simulated by analytical solution with drops effects of resin transfers in the injection tube in VARTM process. Vacuum suction has an important role on resin transfer in the fibers preform as resin flow in a space same as distribution media and preform media follow Darcy’s law [].

| (1) |  |
| --- | --- |

In Darcy’s law Equation 1, u is resin velocity and K, permeability and μ, resin viscosity. Assumption, incompressible fluid and spot pressure drops in injection tube can combine Darcy’s law with momentum and continuity equations, and extract term of flow front velocity. Then by integration and assumption uniform resin flow in contact of tube and preform, by simplification, give filling time as follows [11]:

| (2) |  |
| --- | --- |

Where  is viscosity, , resin density, Lt, length of injection tube, Lv, vertical length, k, Kozeny-Carmen constant for permeability, ΔP, apply pressure, , fibers porosity, R, injection tube radius, W, die width, h0, die height, , suction pressure in outlet, E, preform material’s modulus and s, distance from die head   (Figure 2).

3. Results and discussion

3.1 Effect of diameter:

After running the simulation in MATLAB software, results were compared with the experimental results. Figure 3 indicates that the filling time decreases quickly in a diameter of inlet tube from 5mm to 8 mm. But for higher diameters (more than 8 mm) there are insignificant varieties in pressure drops. Because higher tube diameter in die front decrease the energy drops growth over flow rate. So primal resin velocity is increased, but by flow progress in the die resin flow is increased (figures 3,4). In this case affect of pressure drops in different diameters increase the filled length of die and close velocities. Increasing flow front length, pressure drops due fiber permeability and die dimensions has more effective than injection tube diameter. So with increasing injection tube diameter make change in filling time in end of die poorly. But average velocity in path length need to increase the tube length, cause to decrease product time in low length (less than 1 meter). In higher length, diameter of inlet tube misses its effect. To find optimum diameter consider the velocity and manufacturing cost, So recognize optimum length to place inlet tube can increase flow front velocity in large injected parts.

Generally, according to obtained experimental results optimum diameter in low thickness can be more than preform thickness (in range of 1.5 to 2 times of thickness). The best range for inlet tube diameter is between 5 to 8 mm. It means if inlet tube diameter is less than 5 mm, filling time of die increases extremely and if it is more than 8 mm, time variation is insignificantly (variation is less than 10 percent). In this case, to choose optimum diameter, other parameters should be considered: preform thickness (if diameter of inlet tube be high longer than preform thickness (more than 2 times), increases preform thickness variance surrounding inlet respect to outlet and thickness variation is nonlinear[1]), resin viscosity (viscosity addition in higher diameters decreases effect of flow front primary velocity), die dimensions and cost (by increasing diameter, increases primary cost include tubes and links and remainder resin lead to cost addition (table 3)). So according to investigations tube with 8 mm diameter is best choice to produce VARTM parts in this research.

Figure 2: Schematic of flow front in the die.

Table 3: Volume of resin in tubes.

| Lt (cm) | R (cm) | V add (cm3) |
| --- | --- | --- |
| 80 | 0.1 | 2.5133 |
| 80 | 0.25 | 15.7080 |
| 80 | 0.4 | 40.2124 |
| 80 | 0.6 | 90.4779 |

Figure 3: Simulation and experimental results for inlet tube diameter

Figure 4: Velocity versus position of flow front by changing diameter of inlet tube.

3.2 Effect of length of tube:

Depicting the curve of the filling time changing versus inlet tube length in two cases theory and experiment (Figure 5), can be found that increasing inlet tube length increased filling time, this change is caused by pressure drop increasing within the injection tube. Increasing injection tube length difference between experimental and theoretical values less than 10 percent. Pressure drops can be calculated using equation 3.

| (3) |  |
| --- | --- |
|  |  | for laminar flow; |

Where h, is head, Re, Reynolds number, v, mean velocity, g, gravity and Lt, length of tube.

3.3 Effect of vertical length:

Also, figure 6 shows that vertical length of inlet tube has no effect on experimental results. It means pressure drops scale due to height variation is negligible. It is considered in Figure 6 obviously. Vertical length of the inlet tube don’t change in experimental results. Whereas simulation results show increasing Vertical length of the inlet tube cause to decrease resin velocity and increase filling time (Figure 6), It can be realized from this challenge between experimental and simulation results that this simulation is proper in different diameters and lengths but it is not suitable to determine filling time in vertical images of the inlet tube and by increasing Vertical length of the inlet tube, large difference exist between experimental and simulation results.

| Figure 5: Simulation and experimental results for inlet tube length. | Figure 6: Simulation and experimental results for vertical images of inlet tube in filling time,(R = 2.5 mm) |
| --- | --- |

Figure 7: Experimental results for position-time of flow front due to changing, Lv (R = 2.5 mm)

3.4 Comparing effect of Lt and Lv on pressure drops:

By comparing the results of Figure 5 and Figure 6 can be concluded that the effect of Lt, on filling time is more than Lv effect. This phenomenon can be explained as follows. Pressure drops of the inlet tube is as follows:

|  | (4) |
| --- | --- |
|  | (5) |

h, is calculated from Equation 3.

|  | (6) |
| --- | --- |

ΔP1 can be neglected in comparing to ΔP2 where ΔP1, is pressure drops due to gravity, ΔP2, pressure drops due to friction forces and ΔP, total pressure drops.

Calculating the pressure drop due to friction forces and comparison with the pressure drop due to gravity(is shown in the Table 4), can be found pressure drops due to gravity is very less than pressure drops due to friction forces, and virtually it has little effect on the overall pressure drops in the tube. So we can say pressure drop inside the injection tube is more affected length of the injection tube. Thus filling time depends on the length of injection tube and is not affected by Lv. If assume that in a tube, Lv and Lt be equal. Depicting curves of pressure drops in an inlet tube(figure 8), as horizontal axis shows Lv and Lt changing and vertical axis shows  pressure drops due to gravity, friction forces and total drops. It is clear, total pressure is conformed pressure drops due to friction forces, and pressure drops due to gravity is negligible.

Table 4: Drop pressures

| g(m/s^2) | d(mm) | Viscosity(pa.s) | v(m/s) | Lv(m) | Lt(m) | Density(gr/cm^3) | Drop pressure(pa) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 9.81 | 5 | 950E-3 | 0.125 | 0.5 | 0.5 | 1.17 | 8.892E7 | ΔP1 |
| 9.81 | 5 | 950E-3 | 0.125 | 0.5 | 0.5 | 1.17 | 5.7389E3 | ΔP2 |
| 9.81 | 5 | 950E-3 | 0.125 | 0.5 | 0.5 | 1.17 | 8.8926E7 | ΔP |

4. Conclusion

Optimizing the effective parameters in VARTM method may lead to a proper design for manufacturing large parts while facing the least number of problems. In this paper, the effects of injection tube dimension on die filling time are investigated and its effectiveness on determining optimum dimension in various parts is demonstrated. According to the results, optimum diameter for inlet tube in VARTM method is between 1.5 to 2 times of thickness.

References

# Endnotes

Ghabezi P, Farahani M. Trapezoidal traction–separation laws in mode II fracture in nano-composite and nano-adhesive joints. Journal of Reinforced Plastics and Composites. 2018; 37 (11): 780-794. doi:10.1177/0731684418761001

Ghabezi, P. Rectangular and Triangular Corrugated Composite Skins. Fibers Polym 19, 435–445 (2018). https://doi.org/10.1007/s12221-018-7728-8

P. Ghabezi, M. Khoran, Optimization of drilling parameters in composite sandwich structures (PVC core), Indian J. Sci. Res 2 (1), 173-179.

Ghabezi, P., Harrison, N.M. Hygrothermal deterioration in carbon/epoxy and glass/epoxy composite laminates aged in marine-based environment (degradation mechanism, mechanical and physicochemical properties). J Mater Sci 57, 4239–4254 (2022). https://doi.org/10.1007/s10853-022-06917-2

Pouyan Ghabezi, Noel M. Harrison, Indentation characterization of glass/epoxy and carbon/epoxy composite samples aged in artificial salt water at elevated temperature, Polymer Testing, Volume 110, 2022, 107588,

Pouyan Ghabezi, Tomas Flanagan, Noel Harrison, Short basalt fibre reinforced recycled polypropylene filaments for 3D printing, Materials Letters, Volume 326, 2022, 132942

Ghabezi, P., & Farahani, M. (2019). A cohesive model with a multi-stage softening behavior to predict fracture in nano composite joints. Engineering Fracture Mechanics, 219, 106611. https://doi.org/10.1016/j.engfracmech.2019.106611

P. Ghabezi, M. Farahani, Effects of Nanoparticles on Nanocomposites Mode I and II Fracture: A Critical Review, Progress in Adhesion and Adhesives, https://doi.org/10.1002/9781119526445.ch12.

Golzar Mohammad, Ghabezi Pouyan, Mechanical Behavior of Quasi-sinusoidal Corrugated Composite sheets, Polymer of Journal Iranian Technology and Science, 389-379, 5. No, 24. Vol, 2012.

S. Rajabi Jalall, M. Golzar, ‘‘Effect Of Woven Fabric Density And Distribution Media On VARTM Filling Process’’, Experimental Techniques and Design in Composite Materials.Vicenza – Italy, 30 September-2 October 2009.

P. Ghabezi, Investigation on mechanical behavior (effective elastic constant) of corrugated composite tructures glass/epoxy and graphite/epoxy, Master's Thesis, Department of Mechanical Engineering, Tarbiat Modares University, Tehran, 2012.

C. Alfred, ‘‘Vacuum Assisted Resin Transfer Molding (VARTM):Model Development and Verification’’, Doctor of Philosophy in Materials Engineering Science, 2003.

Ajit R. Nalla, Michael Fuqua, James Glancey, Benoit Lelievre, “A multi-segment injection line and real-time adaptive,model-based controller for vacuum assisted resin transfer molding”, Department of Mechanical Engineering, University of Delaware, 126 Spencer Lab, Newark, Composites: Part A 38, 1058–1069, 2007.

Angela C. Owens ,Lieutenant, United States Navy ,B.S. “an experimental study of fluid structure interaction of carbon composites under low velocity impact”, 2009.

P. Ghabezi, M. Farahani, M. Hosseinifakhr, Investigation of Mechanical Behavior of Alfa and Gamma Nano- Alumina/Epoxy Composite Made by VARTM, International Journal of Advanced Biotechnology and Research (IJBR), 2016, 7(3): 731-736.

P. Ghabezi, M. Farahani, M. Hosseinifakhr, Experimental Investigation Of Nano-Alumina Effect On The Filling Time In VARTM Process, Journal of Fundamental and Applied Sciences, 2016, 8(2S): 925-940, doi: http://dx.doi.org/10.4314/jfas.v8i2s.146.

Uday K. Vaidya, Abhay R.S. Gautam, Mahesh Hosur, Piyush Dutta, “Experimental–numerical studies of transverse impact response of adhesively bonded lap joints in composite structures”, International Journal of Adhesion & Adhesives 26, 184–198, 2006.

Bekir Yenilmez, Murat Senan, E. Murat Sozer, “Variation of part thickness and compaction pressure in vacuum infusion process”, Composites Science and Technology 69, 1710–1719, 2009.

Patrick E. Mack, “vacuum source volumetric flow and the vacuum infusion process”, CCT,Verdant Technologies, Inc.,310 Bourne Avenue,Box 15 / Building 50, East Providence, RI 02916,

S. Lopatnikov, P. Simacek, J. Gillespie and S. G. Advani, “A Closed-Form Solution to Describe Infusion of Resin under Vcuum in Deformable Fibrous Porous Media”, Modeling and Simulation in Materials Science and Engineering, Vol. 12, pp. S191-S204, 2004.

M. K. Yoon, J. Baidoo, J.W. Gillespie and D. Heider, “Vacuum Assisted Resin Transfer Molding (VARTM) Process Incorporating Gravitational Effects: A Closed-form Solution”, Journal of Composite Materials, Vol. 39, pp. 2227-2242, 2005.

http://www.AXSON.com

J. Cook, S.M. Walsh, “Enhancing the Vacuum Assisted Resin Transfer Molding (VARTM) Process Through the Alteration of Variables”,Army Research Laboratory-WMRD, (2003).