Coefficient of Linear Thermal Expansion (CLTE) dataset of extruded composites from recycled wind turbine blade material

1*Seyed Hossein Mamanpush, 1Azadeh Tavousi Tabatabaei, 1Hui Li and 1 Karl Englund

1Composite Materials and Engineering Center, Washington State University, Pullman, WA 99163, USA

Contact email:

*Corresponding Author

s.mamanpush@wsu.edu

Hosseinmamanpush@gmail.com

Abstract

The coefficient of linear thermal expansion (CLTE often referred to as “α”) is a material property which characterizes the ability of a plastic to expand under the effect of temperature elevation. We determined CLTE of extruded fiber-reinforced composites manufactured from recycled wind turbine blade (rWTB) material by considering the influence of particle size, resin content and MAPE as a coupling agent [1].

Keywords: Recycling, Wind turbine blade, Polymer-matrix composite, CLTE

Value of the Data

- Fibers and other fillers significantly reduce thermal expansion. The degree of anisotropy of the filler and the filler orientation pose great impact on the linear coefficient of thermal expansion, therefore, characterizing CLTE is vital for fiber-reinforced composites.

- CLTE helps determine dimensional behavior of structures subject to temperature changes.

- CLTE is important for the economics of production as well as the quality and functioning of products.

- Data on CLTE of extruded composites manufactured from rWTB material gives the researchers clear vision about the potential utilization of this material.

- Data

For obtaining coefficient of linear thermal expansion (CLTE) of extruded fiber-reinforced composites manufactured from recycled wind turbine blade (rWTB) material, tests were performed based on ASTM D1037-12 [2]. Presented dataset include influence of mill screen size (MSS), resin content and coupling agent [3] on the CLTE of second-generation composites.

- Experimental Design, Materials, and Methods

  - Materials and method

rWTB material were mixed with high density polyethylene, non-metallic stearate lubricant, MAPE as a coupling agent were also added to the formulation (Table 1) [4].

Table 1. Extruded rWTB composite formulation

| Sample # | Pine (60 mech) (%) | 3.18 mm MSS rWTB (%) | 1.59 mm MSS rWTB (%) | Talc (%) | MAPE (%) | HDPE (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 |  | 50 |  | 6 |  | 41 |
| 2 |  | 55 |  | 6 |  | 36 |
| 3 |  | 60 |  | 6 |  | 31 |
| 4 |  | 50 |  |  |  | 47 |
| 5 |  | 55 |  |  |  | 42 |
| 6 |  | 60 |  |  |  | 37 |
| 7 | 55 |  |  |  |  | 42 |
| 8 | 55 |  |  | 6 |  | 36 |
| 9 | 55 |  |  |  | 2 | 40 |
| 10 |  |  | 50 |  |  | 47 |
| 11 |  |  | 55 |  |  | 42 |
| 12 |  |  | 60 |  |  | 37 |
| 13 |  |  | 50 |  | 2 | 45 |
| 14 |  |  | 55 |  | 2 | 40 |
| 15 |  |  | 60 |  | 2 | 35 |
| 16 | 13.75 |  | 41.25 |  |  | 42 |
| 17 | 27.5 |  | 27.5 |  |  | 42 |
| 18 | 41.25 |  | 13.75 |  |  | 42 |
| 19 |  |  | 65 |  | 2 | 30 |
| 20 |  |  | 70 |  | 2 | 25 |
| 21 |  |  | 65 |  |  | 32 |
| 22 |  |  | 70 |  |  | 27 |

  - Coefficient of Linear Thermal Expansion (CLTE)

Tables 2-3 presents CLTE data (two cycles). Data shows that increasing rWTB content decreased CLTE for both untreated composite and modified with MAPE composite. The addition of MAPE did not alter the behavior of the CLTE. CLTE data for rWTB blending with pine show that by increasing the rWTB content from 0 % to 75%, CLTE increased. However, when this increased to 100%, CLTE started to decrease. Data indicates that MSS had no significant influence on CLTE of composites, and that simply decreasing MSS increased CLTE slightly [1].

Table 2. CLTE data (first cycle) of extruded fiber-reinforced composites manufactured from recycled wind turbine blade material

| Sample | Freezer (inch) | Room Temp (inch) | 60C (inch) | Freezer (cm) | Room Temp (cm) | 60C (cm) | CLTE results | Ave ×E-5 | STD E-06 | COV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1--1 | 11.899 | 11.909 | 11.923 | 30.22346 | 30.24886 | 30.28442 | 2.1439E-05 | 3.0729 | 5.3046 | 0.172623 |
| 1--2 | 11.895 | 11.913 | 11.933 | 30.2133 | 30.25902 | 30.30982 | 3.3934E-05 |  |  |  |
| 1--3 | 11.875 | 11.899 | 11.91 | 30.1625 | 30.22346 | 30.2514 | 3.1292E-05 |  |  |  |
| 1--4 | 11.888 | 11.909 | 11.926 | 30.19552 | 30.24886 | 30.29204 | 3.3945E-05 |  |  |  |
| 1--5 | 11.885 | 11.915 | 11.922 | 30.1879 | 30.2641 | 30.28188 | 3.3035E-05 |  |  |  |
| 2--1 | 11.891 | 11.912 | 11.928 | 30.20314 | 30.25648 | 30.29712 | 3.3044E-05 | 3.2517 | 3.8858 | 0.1195 |
| 2--2 | 11.884 | 11.903 | 11.925 | 30.18536 | 30.23362 | 30.2895 | 3.6644E-05 |  |  |  |
| 2--3 | 11.886 | 11.906 | 11.926 | 30.19044 | 30.24124 | 30.29204 | 3.5741E-05 |  |  |  |
| 2--4 | 11.885 | 11.905 | 11.918 | 30.1879 | 30.2387 | 30.27172 | 2.9489E-05 |  |  |  |
| 2--5 | 11.891 | 11.92 | 11.922 | 30.20314 | 30.2768 | 30.28188 | 2.7667E-05 |  |  |  |
| 3--1 | 11.895 | 11.913 | 11.926 | 30.2133 | 30.25902 | 30.29204 | 2.7683E-05 | 3.2152 | 3.2193 | 0.100127 |
| 3--2 | 11.886 | 11.911 | 11.927 | 30.19044 | 30.25394 | 30.29458 | 3.6619E-05 |  |  |  |
| 3--3 | 11.89 | 11.919 | 11.927 | 30.2006 | 30.27426 | 30.29458 | 3.3024E-05 |  |  |  |
| 3--4 | 11.885 | 11.905 | 11.92 | 30.1879 | 30.2387 | 30.2768 | 3.1276E-05 |  |  |  |
| 3--5 | 11.889 | 11.909 | 11.925 | 30.19806 | 30.24886 | 30.2895 | 3.2159E-05 |  |  |  |
| 4--1 | 11.872 | 11.906 | 11.922 | 30.15488 | 30.24124 | 30.28188 | 4.4676E-05 | 3.8758 | 4.407 | 0.113715 |
| 4--2 | 11.879 | 11.904 | 11.924 | 30.17266 | 30.23616 | 30.28696 | 4.0215E-05 |  |  |  |
| 4--3 | 11.891 | 11.914 | 11.93 | 30.20314 | 30.26156 | 30.3022 | 3.4824E-05 |  |  |  |
| 4--4 | 11.899 | 11.929 | 11.944 | 30.22346 | 30.29966 | 30.33776 | 4.0131E-05 |  |  |  |
| 4--5 | 11.886 | 11.91 | 11.924 | 30.19044 | 30.2514 | 30.28696 | 3.3943E-05 |  |  |  |
| 5--1 | 11.875 | 11.907 | 11.925 | 30.1625 | 30.24378 | 30.2895 | 4.4672E-05 | 3.8229 | 5.4812 | 0.143377 |
| 5--2 | 11.883 | 11.906 | 11.918 | 30.18282 | 30.24124 | 30.27172 | 3.1273E-05 |  |  |  |
| 5--3 | 11.887 | 11.915 | 11.935 | 30.19298 | 30.2641 | 30.3149 | 4.2857E-05 |  |  |  |
| 5--4 | 11.89 | 11.909 | 11.93 | 30.2006 | 30.24886 | 30.3022 | 3.5732E-05 |  |  |  |
| 5--5 | 11.89 | 11.914 | 11.931 | 30.2006 | 30.26156 | 30.30474 | 3.661E-05 |  |  |  |
| 6--1 | 11.887 | 11.911 | 11.927 | 30.19298 | 30.25394 | 30.29458 | 3.5726E-05 | 3.6988 | 3.1457 | 0.085045 |
| 6--2 | 11.883 | 11.908 | 11.926 | 30.18282 | 30.24632 | 30.29204 | 3.8415E-05 |  |  |  |
| 6--3 | 11.89 | 11.91 | 11.926 | 30.2006 | 30.2514 | 30.29204 | 3.2156E-05 |  |  |  |
| 6--4 | 11.886 | 11.913 | 11.929 | 30.19044 | 30.25902 | 30.29966 | 3.8399E-05 |  |  |  |
| 6--5 | 11.871 | 11.895 | 11.916 | 30.15234 | 30.2133 | 30.26664 | 4.0246E-05 |  |  |  |
| 7--1 | 11.883 | 11.907 | 11.923 | 30.18282 | 30.24378 | 30.28442 | 3.5738E-05 | 3.252E | 2.868 | 0.088193 |
| 7--2 | 11.89 | 11.911 | 11.929 | 30.2006 | 30.25394 | 30.29966 | 3.4833E-05 |  |  |  |
| 7--3 | 11.883 | 11.904 | 11.918 | 30.18282 | 30.23616 | 30.27172 | 3.1279E-05 |  |  |  |
| 7--4 | 11.882 | 11.904 | 11.918 | 30.18028 | 30.23616 | 30.27172 | 3.2172E-05 |  |  |  |
| 7--5 | 11.893 | 11.912 | 11.925 | 30.20822 | 30.25648 | 30.2895 | 2.8578E-05 |  |  |  |
| 8--1 | 11.89 | 11.901 | 11.911 | 30.2006 | 30.22854 | 30.25394 | 3.0385E-05 | 3.1282 | 5.0106 | 0.160172 |
| 8--2 | 11.888 | 11.904 | 11.922 | 30.19552 | 30.23616 | 30.28188 | 3.0385E-05 |  |  |  |
| 8--3 | 11.876 | 11.893 | 11.909 | 30.16504 | 30.20822 | 30.24886 | 2.9519E-05 |  |  |  |
| 8--4 | 11.895 | 11.914 | 11.925 | 30.2133 | 30.26156 | 30.2895 | 2.6788E-05 |  |  |  |
| 8--5 | 11.882 | 11.901 | 11.925 | 30.18028 | 30.22854 | 30.2895 | 3.8438E-05 |  |  |  |
| 9--1 | 11.887 | 11.903 | 11.92 | 30.19298 | 30.23362 | 30.2768 | 2.9494E-05 | 2.9856 | 2.8661 | 0.095998 |
| 9--2 | 11.884 | 11.897 | 11.915 | 30.18536 | 30.21838 | 30.2641 | 2.772E-05 |  |  |  |
| 9--3 | 11.882 | 11.9 | 11.92 | 30.18028 | 30.226 | 30.2768 | 3.3971E-05 |  |  |  |
| 9--4 | 11.889 | 11.906 | 11.924 | 30.19806 | 30.24124 | 30.28696 | 3.1273E-05 |  |  |  |
| 9--5 | 11.885 | 11.9 | 11.915 | 30.1879 | 30.226 | 30.2641 | 2.6819E-05 |  |  |  |
| 10--1 | 11.864 | 11.892 | 11.914 | 30.13456 | 30.20568 | 30.26156 | 4.4729E-05 | 4.3621 | 2.4979 | 0.057263 |
| 10--2 | 11.874 | 11.905 | 11.921 | 30.15996 | 30.2387 | 30.27934 | 4.1999E-05 |  |  |  |
| 10--3 | 11.87 | 11.904 | 11.92 | 30.1498 | 30.23616 | 30.2768 | 4.4684E-05 |  |  |  |
| 10--4 | 11.882 | 11.909 | 11.927 | 30.18028 | 30.24886 | 30.29458 | 4.0198E-05 |  |  |  |
| 10--5 | 11.869 | 11.898 | 11.921 | 30.14726 | 30.22092 | 30.27934 | 4.6494E-05 |  |  |  |
| 11--1 | 11.878 | 11.903 | 11.925 | 30.17012 | 30.23362 | 30.2895 | 4.2006E-05 | 4.3647 | 5.5797 | 0.127838 |
| 11--2 | 11.876 | 11.892 | 11.919 | 30.16504 | 30.20568 | 30.27426 | 3.8467E-05 |  |  |  |
| 11--3 | 11.88 | 11.902 | 11.938 | 30.1752 | 30.23108 | 30.32252 | 5.1842E-05 |  |  |  |
| 11--4 | 11.836 | 11.864 | 11.888 | 30.06344 | 30.13456 | 30.19552 | 4.6628E-05 |  |  |  |
| 11--5 | 11.889 | 11.913 | 11.933 | 30.19806 | 30.25902 | 30.30982 | 3.9292E-05 |  |  |  |
| 12--1 | 11.88 | 11.904 | 11.922 | 30.1752 | 30.23616 | 30.28188 | 3.7534E-05 | 3.5373 | 5.4022 | 0.152721 |
| 12--2 | 11.879 | 11.899 | 11.923 | 30.17266 | 30.22346 | 30.28442 | 3.9338E-05 |  |  |  |
| 12--3 | 11.9 | 11.923 | 11.929 | 30.226 | 30.28442 | 30.29966 | 2.5875E-05 |  |  |  |
| 12--4 | 11.882 | 11.904 | 11.924 | 30.18028 | 30.23616 | 30.28696 | 3.7534E-05 |  |  |  |
| 12--5 | 11.899 | 11.923 | 11.94 | 30.22346 | 30.28442 | 30.3276 | 3.6582E-05 |  |  |  |
| 13--1 | 11.886 | 11.911 | 11.93 | 30.19044 | 30.25394 | 30.3022 | 3.9299E-05 | 4.2172 | 6.1732 | 0.146382 |
| 13--2 | 11.874 | 11.903 | 11.927 | 30.15996 | 30.23362 | 30.29458 | 4.7369E-05 |  |  |  |
| 13--3 | 11.88 | 11.905 | 11.923 | 30.1752 | 30.2387 | 30.28442 | 3.8425E-05 |  |  |  |
| 13--4 | 11.873 | 11.908 | 11.929 | 30.15742 | 30.24632 | 30.29966 | 5.0029E-05 |  |  |  |
| 13--5 | 11.878 | 11.907 | 11.918 | 30.17012 | 30.24378 | 30.27172 | 3.5738E-05 |  |  |  |
| 14--1 | 11.888 | 11.915 | 11.934 | 30.19552 | 30.2641 | 30.31236 | 4.1071E-05 | 3.3407 | 5.2293 | 0.156532 |
| 14--2 | 11.884 | 11.907 | 11.922 | 30.18536 | 30.24378 | 30.28188 | 3.3951E-05 |  |  |  |
| 14--3 | 11.876 | 11.902 | 11.915 | 30.16504 | 30.23108 | 30.2641 | 3.4859E-05 |  |  |  |
| 14--4 | 11.888 | 11.914 | 11.921 | 30.19552 | 30.26156 | 30.27934 | 2.9466E-05 |  |  |  |
| 14--5 | 11.89 | 11.911 | 11.921 | 30.2006 | 30.25394 | 30.27934 | 2.7688E-05 |  |  |  |
| 15--1 | 11.875 | 11.899 | 11.917 | 30.1625 | 30.22346 | 30.26918 | 3.755E-05 | 3.198E | 4.072E | 0.12733 |
| 15--2 | 11.895 | 11.92 | 11.932 | 30.2133 | 30.2768 | 30.30728 | 3.3022E-05 |  |  |  |
| 15--3 | 11.896 | 11.911 | 11.926 | 30.21584 | 30.25394 | 30.29204 | 2.6794E-05 |  |  |  |
| 15--4 | 11.882 | 11.904 | 11.915 | 30.18028 | 30.23616 | 30.2641 | 2.9491E-05 |  |  |  |
| 15--5 | 11.89 | 11.912 | 11.927 | 30.2006 | 30.25648 | 30.29458 | 3.3044E-05 |  |  |  |
| 16--1 | 11.868 | 11.897 | 11.925 | 30.14472 | 30.21838 | 30.2895 | 5.0969E-05 | 4.5967 | 3.4899 | 0.075921 |
| 16--2 | 11.868 | 11.89 | 11.914 | 30.14472 | 30.2006 | 30.26156 | 4.1157E-05 |  |  |  |
| 16--3 | 11.876 | 11.903 | 11.927 | 30.16504 | 30.23362 | 30.29458 | 4.5581E-05 |  |  |  |
| 16--4 | 11.866 | 11.893 | 11.917 | 30.13964 | 30.20822 | 30.26918 | 4.562E-05 |  |  |  |
| 16--5 | 11.865 | 11.895 | 11.917 | 30.1371 | 30.2133 | 30.26918 | 4.6506E-05 |  |  |  |
| 17--1 | 11.869 | 11.89 | 11.911 | 30.14726 | 30.2006 | 30.25394 | 3.7579E-05 | 4.2203 | 2.769E | 0.06561 |
| 17--2 | 11.873 | 11.897 | 11.92 | 30.15742 | 30.21838 | 30.2768 | 4.2027E-05 |  |  |  |
| 17--3 | 11.877 | 11.908 | 11.926 | 30.16758 | 30.24632 | 30.29204 | 4.3775E-05 |  |  |  |
| 17--4 | 11.873 | 11.899 | 11.923 | 30.15742 | 30.22346 | 30.28442 | 4.4702E-05 |  |  |  |
| 17--5 | 11.868 | 11.894 | 11.916 | 30.14472 | 30.21076 | 30.26664 | 4.2932E-05 |  |  |  |
| 18--1 | 11.878 | 11.898 | 11.917 | 30.17012 | 30.22092 | 30.26918 | 3.4871E-05 | 3.7196 | 2.9488 | 0.079277 |
| 18--2 | 11.884 | 11.906 | 11.922 | 30.18536 | 30.24124 | 30.28188 | 3.3954E-05 |  |  |  |
| 18--3 | 11.87 | 11.891 | 11.915 | 30.1498 | 30.20314 | 30.2641 | 4.0259E-05 |  |  |  |
| 18--4 | 11.874 | 11.9 | 11.919 | 30.15996 | 30.226 | 30.27426 | 4.0229E-05 |  |  |  |
| 18--5 | 11.88 | 11.896 | 11.921 | 30.1752 | 30.21584 | 30.27934 | 3.6665E-05 |  |  |  |
| 19--1 | 11.869 | 11.894 | 11.906 | 30.14726 | 30.21076 | 30.24124 | 3.3094E-05 | 3.6216 | 6.5554 | 0.18101 |
| 19--2 | 11.878 | 11.9 | 11.91 | 30.17012 | 30.226 | 30.2514 | 2.8607E-05 |  |  |  |
| 19--3 | 11.87 | 11.891 | 11.918 | 30.1498 | 30.20314 | 30.27172 | 4.2943E-05 |  |  |  |
| 19--4 | 11.879 | 11.903 | 11.924 | 30.17266 | 30.23362 | 30.28696 | 4.0219E-05 |  |  |  |
| 19--5 | 11.7 | 11.893 | 11.902 | 29.718 | 30.20822 | 30.23108 | 4.0219E-05 |  |  |  |
| 20--1 | 11.882 | 11.906 | 11.919 | 30.18028 | 30.24124 | 30.27426 | 3.306E-05 | 2.7537 | 3.4192 | 0.124166 |
| 20--2 | 11.877 | 11.896 | 11.909 | 30.16758 | 30.21584 | 30.24886 | 2.8617E-05 |  |  |  |
| 20--3 | 11.896 | 11.907 | 11.924 | 30.21584 | 30.24378 | 30.28696 | 2.5017E-05 |  |  |  |
| 20--4 | 11.873 | 11.892 | 11.902 | 30.15742 | 30.20568 | 30.23108 | 2.5943E-05 |  |  |  |
| 20--5 | 11.877 | 11.892 | 11.905 | 30.16758 | 30.20568 | 30.2387 | 2.5048E-05 |  |  |  |
| 21--1 | 11.884 | 11.9 | 11.916 | 30.18536 | 30.226 | 30.26664 | 2.8607E-05 | 2.9689 | 3.0797 | 0.103734 |
| 21--2 | 11.866 | 11.889 | 11.901 | 30.13964 | 30.19806 | 30.22854 | 3.1318E-05 |  |  |  |
| 21--3 | 11.881 | 11.89 | 11.918 | 30.17774 | 30.2006 | 30.27172 | 3.3105E-05 |  |  |  |
| 21--4 | 11.874 | 11.895 | 11.908 | 30.15996 | 30.2133 | 30.24632 | 3.0408E-05 |  |  |  |
| 21--5 | 11.89 | 11.912 | 11.918 | 30.2006 | 30.25648 | 30.27172 | 2.5006E-05 |  |  |  |
| 22--1 | 11.873 | 11.897 | 11.907 | 30.15742 | 30.21838 | 30.24378 | 3.0403E-05 | 3.2365 | 5.8128 | 0.179602 |
| 22--2 | 11.885 | 11.903 | 11.911 | 30.1879 | 30.23362 | 30.25394 | 2.3237E-05 |  |  |  |
| 22--3 | 11.881 | 11.903 | 11.922 | 30.17774 | 30.23362 | 30.28188 | 3.6644E-05 |  |  |  |
| 22--4 | 11.873 | 11.892 | 11.915 | 30.15742 | 30.20568 | 30.2641 | 3.7572E-05 |  |  |  |
| 22--5 | 11.878 | 11.901 | 11.916 | 30.17012 | 30.22854 | 30.26664 | 3.3968E-05 |  |  |  |

Table 3. CLTE data (second cycle) of extruded fiber-reinforced composites manufactured from recycled wind turbine blade material

| Sample | Freezer (inch) | Room Temp (inch) | 60C (inch) | Freezer (cm) | Room Temp (cm) | 60C (cm) | CLTE results | Ave ×E-5 | STD E-06 | COV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1--1 | 11.885 | 11.902 | 11.921 | 30.1879 | 30.23108 | 30.27934 | 3.2178E-05 | 3.79 | 1.21 | 0.31838 |
| 1--2 | 11.89 | 11.914 | 11.925 | 30.2006 | 30.26156 | 30.2895 | 3.1252E-05 |  |  |  |
| 1--3 | 11.861 | 11.89 | 11.927 | 30.12694 | 30.2006 | 30.29458 | 5.9052E-05 |  |  |  |
| 1--4 | 11.885 | 11.906 | 11.926 | 30.1879 | 30.24124 | 30.29204 | 3.6634E-05 |  |  |  |
| 1--5 | 11.886 | 11.904 | 11.92 | 30.19044 | 30.23616 | 30.2768 | 3.0385E-05 |  |  |  |
| 2--1 | 11.885 | 11.908 | 11.929 | 30.1879 | 30.24632 | 30.29966 | 3.9308E-05 | 3.36 | 5.84 | 0.173848 |
| 2--2 | 11.886 | 11.909 | 11.93 | 30.19044 | 30.24886 | 30.3022 | 3.9305E-05 |  |  |  |
| 2--3 | 11.884 | 11.907 | 11.916 | 30.18536 | 30.24378 | 30.26664 | 2.859E-05 |  |  |  |
| 2--4 | 11.885 | 11.903 | 11.915 | 30.1879 | 30.23362 | 30.2641 | 2.6812E-05 |  |  |  |
| 2--5 | 11.886 | 11.909 | 11.924 | 30.19044 | 30.24886 | 30.28696 | 3.3945E-05 |  |  |  |
| 3--1 | 11.887 | 11.91 | 11.929 | 30.19298 | 30.2514 | 30.29966 | 3.7515E-05 | 3.16 | 6.75 | 0.213569 |
| 3--2 | 11.886 | 11.915 | 11.927 | 30.19044 | 30.2641 | 30.29458 | 3.6607E-05 |  |  |  |
| 3--3 | 11.894 | 11.911 | 11.929 | 30.21076 | 30.25394 | 30.29966 | 3.126E-05 |  |  |  |
| 3--4 | 11.894 | 11.902 | 11.917 | 30.21076 | 30.23108 | 30.26918 | 2.0558E-05 |  |  |  |
| 3--5 | 11.887 | 11.909 | 11.923 | 30.19298 | 30.24886 | 30.28442 | 3.2159E-05 |  |  |  |
| 4--1 | 11.868 | 11.891 | 11.918 | 30.14472 | 30.20314 | 30.27172 | 4.4733E-05 | 4.29 | 3.28 | 0.076546 |
| 4--2 | 11.873 | 11.901 | 11.923 | 30.15742 | 30.22854 | 30.28442 | 4.4695E-05 |  |  |  |
| 4--3 | 11.881 | 11.909 | 11.928 | 30.17774 | 30.24886 | 30.29712 | 4.1985E-05 |  |  |  |
| 4--4 | 11.893 | 11.924 | 11.944 | 30.20822 | 30.28696 | 30.33776 | 4.5501E-05 |  |  |  |
| 4--5 | 11.881 | 11.908 | 11.923 | 30.17774 | 30.24632 | 30.28442 | 3.7522E-05 |  |  |  |
| 5--1 | 11.872 | 11.904 | 11.93 | 30.15488 | 30.23616 | 30.3022 | 5.1833E-05 | 4.02 | 7.38 | 0.183436 |
| 5--2 | 11.881 | 11.903 | 11.92 | 30.17774 | 30.23362 | 30.2768 | 3.4856E-05 |  |  |  |
| 5--3 | 11.889 | 11.914 | 11.931 | 30.19806 | 30.26156 | 30.30474 | 3.7503E-05 |  |  |  |
| 5--4 | 11.883 | 11.901 | 11.931 | 30.18282 | 30.22854 | 30.30474 | 4.2907E-05 |  |  |  |
| 5--5 | 11.889 | 11.909 | 11.927 | 30.19806 | 30.24886 | 30.29458 | 3.3945E-05 |  |  |  |
| 6--1 | 11.879 | 11.908 | 11.926 | 30.17266 | 30.24632 | 30.29204 | 4.1989E-05 | 3.63 | 3.6 | 0.09937 |
| 6--2 | 11.885 | 11.91 | 11.924 | 30.1879 | 30.2514 | 30.28696 | 3.4836E-05 |  |  |  |
| 6--3 | 11.885 | 11.908 | 11.927 | 30.1879 | 30.24632 | 30.29458 | 3.7522E-05 |  |  |  |
| 6--4 | 11.889 | 11.91 | 11.926 | 30.19806 | 30.2514 | 30.29204 | 3.3049E-05 |  |  |  |
| 6--5 | 11.875 | 11.899 | 11.913 | 30.1625 | 30.22346 | 30.25902 | 3.3974E-05 |  |  |  |
| 7--1 | 11.882 | 11.906 | 11.921 | 30.18028 | 30.24124 | 30.27934 | 3.4847E-05 | 3.36 | 3.26 | 0.097156 |
| 7--2 | 11.888 | 11.915 | 11.928 | 30.19552 | 30.2641 | 30.29712 | 3.5714E-05 |  |  |  |
| 7--3 | 11.883 | 11.903 | 11.924 | 30.18282 | 30.23362 | 30.28696 | 3.6644E-05 |  |  |  |
| 7--4 | 11.885 | 11.905 | 11.921 | 30.1879 | 30.2387 | 30.27934 | 3.217E-05 |  |  |  |
| 7--5 | 11.888 | 11.914 | 11.92 | 30.19552 | 30.26156 | 30.2768 | 2.8574E-05 |  |  |  |
| 8--1 | 11.891 | 11.909 | 11.917 | 30.20314 | 30.24886 | 30.26918 | 2.3226E-05 | 2.45 | 1.49 | 0.060788 |
| 8--2 | 11.89 | 11.91 | 11.92 | 30.2006 | 30.2514 | 30.2768 | 2.6797E-05 |  |  |  |
| 8--3 | 11.881 | 11.898 | 11.908 | 30.17774 | 30.22092 | 30.24632 | 2.4141E-05 |  |  |  |
| 8--4 | 11.895 | 11.921 | 11.923 | 30.2133 | 30.27934 | 30.28442 | 2.4987E-05 |  |  |  |
| 8--5 | 11.887 | 11.903 | 11.913 | 30.19298 | 30.23362 | 30.25902 | 2.3237E-05 |  |  |  |
| 9--1 | 11.885 | 11.902 | 11.924 | 30.1879 | 30.23108 | 30.28696 | 3.4859E-05 | 3.02 | 5.34 | 0.176771 |
| 9--2 | 11.886 | 11.903 | 11.915 | 30.19044 | 30.23362 | 30.2641 | 2.5919E-05 |  |  |  |
| 9--3 | 11.882 | 11.91 | 11.921 | 30.18028 | 30.2514 | 30.27934 | 3.4836E-05 |  |  |  |
| 9--4 | 11.89 | 11.915 | 11.926 | 30.2006 | 30.2641 | 30.29204 | 3.2143E-05 |  |  |  |
| 9--5 | 11.893 | 11.91 | 11.919 | 30.20822 | 30.2514 | 30.27426 | 2.3224E-05 |  |  |  |
| 10--1 | 11.866 | 11.89 | 11.916 | 30.13964 | 30.2006 | 30.26664 | 4.4736E-05 | 3.51 | 7.83 | 0.222906 |
| 10--2 | 11.864 | 11.899 | 11.923 | 30.13456 | 30.22346 | 30.28442 | 5.2749E-05 |  |  |  |
| 10--3 | 11.865 | 11.893 | 11.911 | 30.1371 | 30.20822 | 30.25394 | 4.1147E-05 |  |  |  |
| 10--4 | 11.87 | 11.896 | 11.921 | 30.1498 | 30.21584 | 30.27934 | 4.5608E-05 |  |  |  |
| 10--5 | 11.876 | 11.893 | 11.911 | 30.16504 | 30.20822 | 30.25394 | 3.1308E-05 |  |  |  |
| 11--1 | 11.875 | 11.902 | 11.919 | 30.1625 | 30.23108 | 30.27426 | 3.9328E-05 | 3.59 | 4.67 | 0.129839 |
| 11--2 | 11.874 | 11.898 | 11.909 | 30.15996 | 30.22092 | 30.24886 | 3.1294E-05 |  |  |  |
| 11--3 | 11.888 | 11.908 | 11.933 | 30.19552 | 30.24632 | 30.30982 | 4.0202E-05 |  |  |  |
| 11--4 | 11.844 | 11.868 | 11.878 | 30.08376 | 30.14472 | 30.17012 | 3.0477E-05 |  |  |  |
| 11--5 | 11.895 | 11.914 | 11.938 | 30.2133 | 30.26156 | 30.32252 | 3.8396E-05 |  |  |  |
| 12--1 | 11.88 | 11.901 | 11.934 | 30.1752 | 30.22854 | 30.31236 | 4.8271E-05 | 3.58 | 5.18 | 0.144575 |
| 12--2 | 11.883 | 11.903 | 11.937 | 30.18282 | 30.23362 | 30.31998 | 4.8262E-05 |  |  |  |
| 12--3 | 11.893 | 11.919 | 11.935 | 30.20822 | 30.27426 | 30.3149 | 3.7487E-05 |  |  |  |
| 12--4 | 11.886 | 11.912 | 11.934 | 30.19044 | 30.25648 | 30.31236 | 4.2868E-05 |  |  |  |
| 12--5 | 11.898 | 11.921 | 11.941 | 30.22092 | 30.27934 | 30.33014 | 3.8373E-05 |  |  |  |
| 13--1 | 11.872 | 11.905 | 11.929 | 30.15488 | 30.2387 | 30.29966 | 5.0935E-05 | 5.11 | 6.74 | 0.131787 |
| 13--2 | 11.869 | 11.897 | 11.922 | 30.14726 | 30.21838 | 30.28188 | 4.7393E-05 |  |  |  |
| 13--3 | 11.871 | 11.908 | 11.935 | 30.15234 | 30.24632 | 30.3149 | 5.7176E-05 |  |  |  |
| 13--4 | 11.866 | 11.905 | 11.931 | 30.13964 | 30.2387 | 30.30474 | 5.8084E-05 |  |  |  |
| 13--5 | 11.87 | 11.894 | 11.917 | 30.1498 | 30.21076 | 30.26918 | 4.2038E-05 |  |  |  |
| 14--1 | 11.885 | 11.915 | 11.925 | 30.1879 | 30.2641 | 30.2895 | 3.5714E-05 | 4 | 4.46 | 0.111285 |
| 14--2 | 11.877 | 11.904 | 11.924 | 30.16758 | 30.23616 | 30.28696 | 4.2003E-05 |  |  |  |
| 14--3 | 11.872 | 11.899 | 11.922 | 30.15488 | 30.22346 | 30.28188 | 4.4702E-05 |  |  |  |
| 14--4 | 11.873 | 11.897 | 11.921 | 30.15742 | 30.21838 | 30.27934 | 4.2922E-05 |  |  |  |
| 14--5 | 11.881 | 11.901 | 11.92 | 30.17774 | 30.22854 | 30.2768 | 3.4862E-05 |  |  |  |
| 15--1 | 11.875 | 11.9 | 11.921 | 30.1625 | 30.226 | 30.27934 | 4.1123E-05 | 3.75 | 4.86 | 0.129489 |
| 15--2 | 11.892 | 11.913 | 11.933 | 30.20568 | 30.25902 | 30.30982 | 3.6613E-05 |  |  |  |
| 15--3 | 11.886 | 11.916 | 11.932 | 30.19044 | 30.26664 | 30.30728 | 4.1068E-05 |  |  |  |
| 15--4 | 11.881 | 11.909 | 11.925 | 30.17774 | 30.24886 | 30.2895 | 3.9305E-05 |  |  |  |
| 15--5 | 11.895 | 11.913 | 11.928 | 30.2133 | 30.25902 | 30.29712 | 2.9469E-05 |  |  |  |
| 16--1 | 11.867 | 11.892 | 11.921 | 30.14218 | 30.20568 | 30.27934 | 4.8307E-05 | 4.24 | 3.56 | 0.083979 |
| 16--2 | 11.867 | 11.894 | 11.913 | 30.14218 | 30.21076 | 30.25902 | 4.1144E-05 |  |  |  |
| 16--3 | 11.874 | 11.89 | 11.922 | 30.15996 | 30.2006 | 30.28188 | 4.2947E-05 |  |  |  |
| 16--4 | 11.869 | 11.894 | 11.914 | 30.14726 | 30.21076 | 30.26156 | 4.0249E-05 |  |  |  |
| 16--5 | 11.871 | 11.896 | 11.915 | 30.15234 | 30.21584 | 30.2641 | 3.9348E-05 |  |  |  |
| 17--1 | 11.871 | 11.894 | 11.91 | 30.15234 | 30.21076 | 30.2514 | 3.4883E-05 | 3.9 | 6.16 | 0.158173 |
| 17--2 | 11.876 | 11.901 | 11.921 | 30.16504 | 30.22854 | 30.27934 | 4.0225E-05 |  |  |  |
| 17--3 | 11.88 | 11.907 | 11.935 | 30.1752 | 30.24378 | 30.3149 | 4.914E-05 |  |  |  |
| 17--4 | 11.879 | 11.906 | 11.92 | 30.17266 | 30.24124 | 30.2768 | 3.6634E-05 |  |  |  |
| 17--5 | 11.873 | 11.895 | 11.911 | 30.15742 | 30.2133 | 30.25394 | 3.3985E-05 |  |  |  |
| 18--1 | 11.879 | 11.901 | 11.914 | 30.17266 | 30.22854 | 30.26156 | 3.1286E-05 | 3.29 | 1.47 | 0.044819 |
| 18--2 | 11.884 | 11.907 | 11.922 | 30.18536 | 30.24378 | 30.28188 | 3.3951E-05 |  |  |  |
| 18--3 | 11.871 | 11.894 | 11.909 | 30.15234 | 30.21076 | 30.24886 | 3.3988E-05 |  |  |  |
| 18--4 | 11.881 | 11.907 | 11.916 | 30.17774 | 30.24378 | 30.26664 | 3.1271E-05 |  |  |  |
| 18--5 | 11.879 | 11.9 | 11.917 | 30.17266 | 30.226 | 30.26918 | 3.3971E-05 |  |  |  |
| 19--1 | 11.871 | 11.888 | 11.901 | 30.15234 | 30.19552 | 30.22854 | 2.6846E-05 | 3.33 | 4.78 | 0.143792 |
| 19--2 | 11.874 | 11.896 | 11.916 | 30.15996 | 30.21584 | 30.26664 | 3.756E-05 |  |  |  |
| 19--3 | 11.87 | 11.898 | 11.913 | 30.1498 | 30.22092 | 30.25902 | 3.8447E-05 |  |  |  |
| 19--4 | 11.881 | 11.907 | 11.917 | 30.17774 | 30.24378 | 30.26918 | 3.2164E-05 |  |  |  |
| 19--5 | 11.872 | 11.891 | 11.907 | 30.15488 | 30.20314 | 30.24378 | 3.1313E-05 |  |  |  |
| 20--1 | 11.88 | 11.899 | 11.914 | 30.1752 | 30.22346 | 30.26156 | 3.0398E-05 | 2.74 | 3.06 | 0.111958 |
| 20--2 | 11.875 | 11.895 | 11.908 | 30.1625 | 30.2133 | 30.24632 | 2.9514E-05 |  |  |  |
| 20--3 | 11.889 | 11.912 | 11.921 | 30.19806 | 30.25648 | 30.27934 | 2.8578E-05 |  |  |  |
| 20--4 | 11.871 | 11.893 | 11.897 | 30.15234 | 30.20822 | 30.21838 | 2.3257E-05 |  |  |  |
| 20--5 | 11.881 | 11.892 | 11.909 | 30.17774 | 30.20568 | 30.24886 | 2.5048E-05 |  |  |  |
| 21--1 | 11.88 | 11.899 | 11.912 | 30.1752 | 30.22346 | 30.25648 | 2.861E-05 | 2.65 | 1.62 | #DIV/0! |
| 21--2 | 11.871 | 11.889 | 11.899 | 30.15234 | 30.19806 | 30.22346 | 2.5054E-05 |  |  |  |
| 21--3 | 11.881 | 11.903 | 11.909 | 30.17774 | 30.23362 | 30.24886 | 2.5025E-05 |  |  |  |
| 21--4 | 11.875 | 11.906 | 11.906 | 30.1625 | 30.24124 | 30.24124 | 2.7699E-05 |  |  |  |
| 21--5 | 11.889 | 11.912 | 11.918 | 30.19806 | 30.25648 | 30.27172 | 2.5899E-05 |  |  |  |
| 22--1 | 11.876 | 11.902 | 11.908 | 30.16504 | 30.23108 | 30.24632 | 2.8602E-05 | 2.72 | 3.39 | 0.12472 |
| 22--2 | 11.88 | 11.901 | 11.906 | 30.1752 | 30.22854 | 30.24124 | 2.3241E-05 |  |  |  |
| 22--3 | 11.885 | 11.908 | 11.917 | 30.1879 | 30.24632 | 30.26918 | 2.8588E-05 |  |  |  |
| 22--4 | 11.873 | 11.893 | 11.908 | 30.15742 | 30.20822 | 30.24632 | 3.1308E-05 |  |  |  |
| 22--5 | 11.882 | 11.91 | 11.909 | 30.18028 | 30.2514 | 30.24886 | 2.4117E-05 |  |  |  |

Acknowledgments

The authors gratefully appreciate the financial support by Global Fiberglass Solutions Inc. Bothell, WA.

References

# [1] Mamanpush, Seyed Hossein, et al., Extruded fiber-reinforced composites manufactured from recycled wind turbine blade material, Waste and biomass valorization,2019, Accepted: In press. https://doi.org/10.1007/s12649-019-00659-0

[2] Standard Test Methods for Evaluating Properties of Wood-Base Fiber and Particle Panel Materials, ASTM D1037-12.

[3] Mamanpush, Seyed Hossein, et al. "Recycled wind turbine blades as a feedstock for second generation composites." Waste Management 76 (2018): 708-714.

https://doi.org/10.1016/j.wasman.2018.02.050

[4] Mamanpush, Seyed Hossein, et al. "Data on the mechanical properties of recycled wind turbine blade composites." Data in brief, 19 (2018): 230-235.

https://doi.org/10.1016/j.dib.2018.05.008