# Integrated Electrochemical Process Modelling and Techno-Economic Assessment of Micro-Mesh Alkaline Seawater Electrolysis for Green Hydrogen Production

Mahdi Amanipour *

Durham University, Durham, UK, mahdi.amanipour@durham.ac.uk, ORCID: 0000-0001-7713-0653

Venkatesan Venkata Krishnan *

Teesside University, Middlesbrough, UK, V.krishnan@tees.ac.uk, ORCID: 0000-0001-6901-3393

Karen Johnston

Durham University, Durham, UK, karen.johnston@durham.ac.uk, ORCID: 0000-0002-9125-4203

Tony Roskilly

Durham University, Durham, UK, Anthony.p.roskilly@durham.ac.uk, ORCID: 0000-0002-9356-3157

Nashwan Dawood

Teesside University, Middlesbrough, UK, N.N.Dawood@tees.ac.uk, ORCID: 0000-0002-4873-7576

Abstract

This study couples an experimentally calibrated electrochemical model with a techno-economic assessment of expanded nickel micro-mesh electrodes for alkaline electrolysis of seawater (M-SWELT). A zero-gap cell model with explicit thermodynamic, kinetic, bubble and ohmic terms is anchored to commercial alkaline performance, checked against published resistance measurements and calibrated to a like-for-like two-electrode comparison of micro-mesh and woven Ni-mesh cells in natural seawater with 5 M KOH. Because one operating point cannot separate kinetic from resistive contributions, the transferred voltage saving at 0.4 A cm⁻² and 80 °C is bounded at 20–187 mV (central 89 mV). The model is coupled to two seawater feed routes, reverse-osmosis (RO) desalination and direct feed with softening and a chloride bleed, and to a cost model of a 10 MW plant. The RO-fed micro-mesh plant reaches a levelised cost of hydrogen (LCOH) of £4.35 kg⁻¹, against £4.51 kg⁻¹ with woven mesh, and the micro-mesh breaks even at an electrode premium of up to £950 m⁻² (range £217–1,985 m⁻²). Even without chloride oxidation and with electrodes that last as long as the stacks, direct feed costs £4.95 kg⁻¹, because the chloride bleed discards KOH and forces a dilute electrolyte; crediting the chloride’s conductivity narrows the gap to RO feed without closing it, and short electrode life widens it. Across 10,000 Latin-hypercube Monte Carlo samples, the RO-fed micro-mesh plant averages £4.72 kg⁻¹ (P5–P95 £3.95–5.59 kg⁻¹); it is cheaper than woven mesh at equal electrode cost, and direct feed is dearer than RO feed, in every sample.

Keywords: Seawater electrolysis; Process modelling; Green hydrogen; Micro-mesh electrodes; Monte Carlo uncertainty analysis; LCOH

Nomenclature

| Symbol | Description (unit) | Symbol | Description (unit) |
| --- | --- | --- | --- |
| A; Ael, Astack | active area (m²); annual electrode and stack replacement cost (£ yr⁻¹) | p | pressure (bar) |
| aw | water activity (–) | pv | water vapour pressure (bar) |
| B | electrolyte bleed (L kg⁻¹ H₂) | r | discount rate (–) |
| Cset | chloride set-point of the loop (mol L⁻¹) | rres | electrode resistance ratio (–) |
| carea | stack cost per active area (£ m⁻²) | R | gas constant (J mol⁻¹ K⁻¹) |
| CF | capacity factor (–) | Rsep, Rpore, Rcont | area-specific resistances: separator, electrolyte in electrode openings, contacts (Ω m²) |
| fel | electrode replacement cost fraction (–) | SEC | specific energy consumption (kWh kg⁻¹) |
| CRF | capital recovery factor (yr⁻¹) | T | temperature (K, °C) |
| E0, Erev | standard and reversible cell voltage (V) | V, Vtn | cell and thermoneutral voltage (V) |
| Ea | activation energy (J mol⁻¹) | W | water consumption (kg kg⁻¹ H₂) |
| eBoP | balance-of-plant electricity (kWh kg⁻¹) | w | kinetic share of the micro-mesh advantage (–) |
| F | Faraday constant (C mol⁻¹) | xCl | chloride per kg of seawater water (mol kg⁻¹) |
| Fact | electrode activity factor (–) | α | charge-transfer coefficient (–) |
| FE, FECl | Faradaic efficiency, chloride factor (–) | δ | thickness (m) |
| j, j0 | current density, exchange current density (A m⁻²) | η | overpotential (V) |
| jx | crossover-equivalent current density (A m⁻²) | ηrect | rectifier efficiency (–) |
| kε | gas void fraction per unit bubble coverage (–) | θ | bubble coverage (–) |
| Lel, Lstack | electrode and stack life (h) | σ | electrolyte conductivity (S m⁻¹) |
| m | KOH molality (mol kg⁻¹) | τ | stack replacement interval (yr) |
| N, NM | plant life (yr), MacMullin number (–) | ρs | Spearman rank correlation coefficient (–) |

Abbreviations: AEM, anion exchange membrane; AWE, alkaline water electrolysis; BoP, balance of plant; CAPEX, capital expenditure; LCOH, levelised cost of hydrogen; LDH, layered double hydroxide; O&M, operation and maintenance; P5/P95, 5th/95th percentile; RO, reverse osmosis.

# 1. INTRODUCTION

The global transition toward low-carbon energy systems has intensified interest in hydrogen as a versatile and clean energy carrier capable of decarbonising hard-to-abate sectors such as heavy industry, transportation, and chemical production [1–3]. Among various hydrogen production pathways, water electrolysis powered by renewable energy has emerged as the most sustainable route for producing green hydrogen with near-zero greenhouse gas emissions [4–7]. Alkaline water electrolysis (AWE) remains one of the most mature and commercially viable technologies due to its relatively low capital cost, operational robustness, and scalability [8–10].

Recent studies have increasingly focused on improving the efficiency and system-level performance of electrolysis technologies [6,11,12]. Electrolyser modelling has evolved from simple thermodynamic descriptions to multi-scale frameworks integrating electrochemical kinetics, heat transfer, and system dynamics [10,13,14]. Classical models, such as that of Ulleberg [13], describe the cell voltage as the sum of the reversible voltage and activation, ohmic and mass-transport losses, and Sánchez et al. [14] fitted and validated such a semi-empirical model for a 15 kW alkaline electrolyser. For zero-gap cells, de Groot and Vreman [15] and Haverkort and Rajaei [16] analysed how the separator, gas bubbles and the electrolyte held in the electrode openings contribute to the ohmic loss, which makes the electrode structure a design variable in its own right.

In parallel, process simulation tools such as Aspen Plus have become widely adopted for modelling hydrogen production systems at the plant level [17]. These tools enable the integration of electrolyser units with balance-of-plant components, including gas separation, thermal management, and compression systems. System-level models have also been used to optimise the operation of alkaline electrolysers; Zheng et al. [18], for example, showed that the thermal–electric behaviour and state transitions of an alkaline electrolyser system affect its optimal day-ahead dispatch.

Beyond technical modelling, techno-economic analysis (TEA) has become a critical tool for evaluating the commercial viability of green hydrogen systems [3,19,20]. TEA frameworks typically assess capital expenditure (CAPEX), operational expenditure (OPEX), and the levelised cost of hydrogen (LCOH), which serves as a key metric for comparing hydrogen production pathways. Recent literature highlights that electricity cost is the dominant contributor to the LCOH of electrolytic hydrogen [4,7,21]. In addition, plant size, capacity factor, and system efficiency significantly influence economic performance, with larger-scale systems benefiting from economies of scale and improved asset utilisation [7]. Recent assessments also combine TEA with an environmental analysis of large-scale electrolysis under different electricity supply options [20]. Coupling electrolysis with variable renewable supply makes both the capacity factor and the electricity price uncertain, and flexible operation changes the economics of power-to-hydrogen plants [3]; single-point cost estimates are therefore of limited value unless their uncertainty is quantified.

Seawater is an attractive feedstock for coastal and offshore hydrogen production, but it introduces problems that are absent in pure-water electrolysis [22,23]. Chloride can be oxidised at the anode to hypochlorite or chlorine, which lowers the Faradaic efficiency and produces corrosive by-products; Dionigi et al. [24] showed that in alkaline media the oxygen evolution reaction stays selective as long as the anode overpotential remains below about 480 mV. Magnesium and calcium precipitate when seawater is made alkaline, fouling electrodes and separators, and chloride accelerates the corrosion of nickel and steel [22,23]. Two routes are therefore debated: desalination by reverse osmosis (RO) followed by conventional electrolysis, and direct electrolysis of seawater with chloride-tolerant catalysts, membranes or local reaction environments [25,26]. Techno-economic appraisals have argued that desalination adds only a small fraction to the cost of hydrogen, which questions the economic case for direct seawater splitting [27,28]. These appraisals compare the cost of desalination with the benefits claimed for direct splitting; to our knowledge, none couples an electrode model to the mass balance of the electrolyte loop, which sets how much KOH and chloride must be purged when seawater is fed directly.

In zero-gap cells the electrode structure governs both the ohmic resistance and gas management. Bubbles shield active sites and raise the local current density [29,30], and the separator and the electrolyte held in the electrode openings account for much of the ohmic resistance [15,16]. Structured electrodes that release bubbles quickly, such as superaerophobic nanoarray electrodes [31] or optimised electrode micro-structures [32], can therefore lower both kinetic and ohmic losses. Expanded-metal micro-meshes, produced by slitting and stretching a single sheet without joints, are a scalable substrate of this type and a support for NiFe layered double hydroxide (LDH) catalysts for seawater oxidation [33]; their benefit, however, has not been quantified at plant scale.

Despite these advancements, several critical research gaps remain. The first is the limited integration of advanced electrode architectures into system-level models. Most existing Aspen and system-level models treat the electrolyser as a lumped unit, without explicitly incorporating the impact of novel electrode structures (e.g., micro-mesh or porous electrodes) on performance metrics such as ohmic losses and mass transport. Another area of research gap is the insufficient coupling between electrochemical performance and economic evaluation. While TEA studies quantify LCOH, they often rely on simplified assumptions for electrolyser efficiency, without linking these to measured improvements in electrode design or cell architecture, and without asking whether an efficiency gain pays for a more expensive electrode. Moreover, process models of seawater electrolysis rarely represent the feed-water route: the chloride and hardness that enter with seawater, the purge they require and the corrosion they cause are usually discussed qualitatively rather than included in the mass balance and the cost. Finally, cost estimates are often reported as single values, although the inputs that determine them are uncertain; a probabilistic treatment with documented input distributions is needed to judge whether the differences between technology options are robust.

The Micro-Mesh Structured Seawater Electrolysis Technology (M-SWELT) system is a zero-gap alkaline electrolysis configuration developed within the Research England Hydrogen Innovation Project (REHIP) (Feb 2024 to Feb 2026). The micro-mesh electrodes are produced by The Expanded Metal Company, Hartlepool, a project partner with Teesside and Durham Universities in REHIP. The system integrates expanded nickel micro-mesh electrodes within a zero-gap cell architecture, where electrodes are positioned in close contact with the separator to minimise ionic transport resistance. Compared with the planar or woven electrodes of conventional alkaline electrolysers, the open micro-mesh structure is intended to increase the accessible active area, speed up bubble detachment and improve electrolyte access to the catalyst, thereby lowering both activation and ohmic losses.

To address the research gaps identified above, this work couples an experimentally calibrated cell model with feed-water and cost models of a seawater electrolysis plant. The specific contributions are: (i) an explicit zero-gap cell model (Eqs. (1)–(13)) in which the micro-mesh enters through two physically interpretable factors, an activity factor on the effective exchange current density and a ratio on the electrode-related resistance, calibrated to a like-for-like test of micro-mesh and woven Ni mesh in natural seawater with 5 M KOH; (ii) a mass balance of the KOH loop for direct seawater feed that quantifies the chloride bleed, KOH loss and softening demand, with chloride selectivity and electrode life bounded by published data, compared with RO-fed operation; (iii) the break-even electrode premium, which answers whether the efficiency gain of the micro-mesh pays for a more expensive electrode, together with the cost-optimal current density; and (iv) a comparative uncertainty analysis in which all configurations share the same 10,000 Latin-hypercube samples, so that the probability that one option is cheaper than another, and the inputs that decide it, follow directly; input distributions are documented and the model code is provided for reproduction.

# 2. METHODOLOGY

## 2.1. Scope, plant definition and model structure

The analysis couples four layers. A cell model gives the cell voltage of a zero-gap alkaline cell as a function of current density, temperature, pressure and electrolyte composition, and represents the micro-mesh through two calibrated factors (Sections 2.2 and 2.3). An energy model converts the cell voltage into the system specific energy consumption (SEC), including rectifier, balance-of-plant (BoP) and cooling loads (Section 2.2). A feed-water model describes the two seawater routes (Section 2.4), and a cost model gives the LCOH together with Monte Carlo, tornado and rank-correlation analyses (Sections 2.5 and 2.6).

Fig. 1 shows the process configuration of the electrolysis island, set up as an Aspen Plus flowsheet: the zero-gap stack, the lye recirculation loops, gas–liquid separators and gas traps on the hydrogen and oxygen trains, intercoolers served by an air-cooled cooling-water loop, and the make-up water pump. Make-up water enters from the feed-water route (Section 2.4). In the energy and cost model, the stack is represented by the explicit cell model of Section 2.2, the electricity demand of pumps, gas conditioning and controls by a lumped BoP term, and the cooling duty by a fan term (Eq. (13)). All relations used for the results are therefore stated in this paper and can be reproduced with the supplied code without the process simulator.

Fig. 1. Process configuration of the zero-gap alkaline electrolysis island (Aspen Plus flowsheet): stack, recirculation loops, gas–liquid separators and gas traps on the hydrogen and oxygen trains, intercoolers with an air-cooled cooling-water loop, and make-up water supply (H2O-IN).

The plant is sized by a reference design: woven Ni-mesh electrodes, RO-fed, 80 °C, 7 bar, 5 M KOH (≈23 wt%) and a nominal current density of 0.4 A cm⁻², drawing 10 MW of AC power and producing 177.5 kg h⁻¹ of hydrogen (Table 1). Every other configuration produces the same hydrogen flow; its active area and rated power follow from its own polarisation curve and Faradaic efficiency, so that configurations are compared at equal output. The base-case electrolyte, 5 M KOH, matches the concentration of the M-SWELT cell test (Section 2.3) and lies within the 20–30 wt% range typical of alkaline electrolysers [8]; concentrations from 1 M to 35 wt% (8.4 M) are examined for the direct-feed route.

All relations are implemented in Python (NumPy/SciPy). The code, input files and the data behind every figure are provided as Supplementary Material. The code was developed with the assistance of a generative AI tool and checked against 24 independent verification tests that are included with it, among them a hand calculation of the reference LCOH, closure of the water and chloride balances, and consistency of the active area with Faraday’s law.

Table 1. Base case and ranges studied.

| Parameter | Base case | Range studied | Unit |
| --- | --- | --- | --- |
| Stack temperature | 80 | 40–90 (cell); 30–90 (feed routes) | °C |
| Operating pressure (balanced) | 7 | 1–30 | bar |
| KOH concentration | 5 (≈23 wt%) | 1–8.4 (direct feed) | mol L⁻¹ |
| Nominal current density | 0.4 | 0.1–1.2 | A cm⁻² |
| Chloride in the electrolyte loop | 0 (RO feed) | set-point 0.75–2 (direct feed) | mol L⁻¹ |
| Separator | Zirfon-type diaphragm, 500 µm | – | – |
| AC input of the reference design | 10 | 1–200 (plant size) | MW |
| Hydrogen output | 177.5 | scales with plant size | kg h⁻¹ |
| Active area of the reference design | 1,189 | follows from Eq. (21) | m² |
| Capacity factor | 0.80 | 0.20–1.00 | – |

## 2.2. Electrochemical cell model

The cell voltage is the sum of the reversible voltage, the activation overpotentials of anode and cathode, and the ohmic losses across the separator, the electrolyte held in the electrode openings and the electronic contacts:

|  | V=Erev+ηa+ηc+jRsep+Rpore+Rcont | (1) |
| --- | --- | --- |

The reversible voltage accounts for temperature, gas pressure and water activity [34,35]:

|  | Erev=E0T+RT2Flnp-pv3/2aw | (2) |
| --- | --- | --- |
|  | E0T=1.5184-1.5421×10-3 T+9.523×10-5 TlnT+9.84×10-8 T2 | (3) |
|  | lnaw=-0.05192 m+0.003302 m2+3.177 m-2.131 m2T-2ϕMH2O mCl | (4) |
|  | pv=awexp37.043-6275.7T-3.4159lnT | (5) |

where T is in K, p in bar, m is the KOH molality and mCl the chloride molality; the last term of Eq. (4) is a dilute-solution osmotic correction for chloride with osmotic coefficient ϕ = 0.93. At 80 °C and 7 bar in 5 M KOH, Erev = 1.231 V; it decreases by about 0.72 mV K⁻¹ between 40 and 90 °C and rises by 38 mV between 5 and 25 bar (Section 3.4).

Gas bubbles cover part of each electrode. The fractional coverage is described by a power law of the form proposed by Vogt and Balzer [29],

|  | θ=θrefjjref0.3 | (6) |
| --- | --- | --- |

with θref = 0.15 at jref = 0.4 A cm⁻². The activation overpotentials follow the symmetric Butler–Volmer relation evaluated on the uncovered, effective area,

|  | ηx=RTαxF arsinhj2 j0,xT Fact 1-θ, x=a,c | (7) |
| --- | --- | --- |
|  | j0,xT=j0,x,ref exp-Ea,xR1T-1Tref | (8) |

with Tref = 353.15 K. Fact is the electrode activity factor: it equals 1 for the woven reference and, for the micro-mesh, lumps the gain in accessible active area and the reduction in bubble shielding (Section 2.3).

The separator resistance follows from the electrolyte conductivity and the MacMullin number NM of the diaphragm [36],

|  | Rsep=NM δsepσcKOH,T | (9) |
| --- | --- | --- |

with the conductivity of aqueous KOH from the correlation of Gilliam et al. [37] (M in mol L⁻¹, T in K, σ in S m⁻¹); the contribution of dissolved chloride is neglected, and Section 3.6 examines its effect:

|  | σ=100-2.041M-0.0028M2+0.005332 MT+207.2MT+0.001043M3-3×10-7M2T2 | (10) |
| --- | --- | --- |

The electrolyte held in the electrode openings contributes a resistance that scales with 1/σ and increases with the gas void fraction kεθ through a Bruggeman correction [38], while the electronic contact resistance does not depend on temperature:

|  | Rpore=Rpore,arres σaσ 1-kεθ-3/2, Rcont=Rcont,arres | (11) |
| --- | --- | --- |

where σa is the conductivity at the anchor condition and rres is the electrode resistance ratio (1 for woven mesh). The separator term is the same for both electrode types.

The Faradaic efficiency combines a chloride factor FECl (Section 2.4) with gas crossover, represented by an equivalent current density jx that scales with pressure,

|  | FE=FECl1-jx p/prefj | (12) |
| --- | --- | --- |

with jx = 30 A m⁻² at pref = 7 bar, i.e. a loss of 0.75% at 0.4 A cm⁻². Finally, the system specific energy consumption per kilogram of hydrogen is

|  | SEC=26.59 Vηrect FE+eBoP+ffan 26.59V-VtnFE | (13) |
| --- | --- | --- |

where 26.59 kWh kg⁻¹ V⁻¹ = 2F/(3.6×10⁶ MH2), ηrect is the AC–DC conversion efficiency, eBoP the BoP electricity, ffan = 0.02 the fan electricity per unit of heat rejected, and Vtn = ΔH(T)/2F the thermoneutral voltage, with ΔH = 285.83 kJ mol⁻¹ − 31.77 J mol⁻¹ K⁻¹ (T − 298.15 K). A voltage degradation rate d raises the lifetime-average voltage by d Lstack/2, and the lifetime-average SEC is used for the electricity cost.

Table 2 lists the parameters. The kinetic parameters are representative values for Ni-based alkaline electrodes and are not fitted individually. Instead, the electrode-related resistance Rpore,a+Rcont,a (split 2:1) is fitted so that the woven-mesh reference cell gives 1.95 V at 0.4 A cm⁻², 80 °C, 7 bar and 30 wt% KOH, within the operating window of commercial alkaline electrolysers (1.8–2.4 V at 0.2–0.4 A cm⁻²) [5,12]. The resulting area-specific resistance at the anchor is 0.28 Ω cm², of which the separator contributes 0.14 Ω cm². Both values agree with independent measurements on zero-gap cells with 500 µm Zirfon diaphragms: de Groot and Vreman [15] give a diaphragm resistance of 0.13 Ω cm² at 80 °C in 30 wt% KOH, a MacMullin number between 2.6 and 4.0, and cell resistances, normalised to the same conditions, mostly between 0.24 and 0.4 Ω cm². The uncertainty of the anchor (±0.10 V) is propagated in the Monte Carlo analysis.

Table 2. Parameters of the cell model.

| Parameter | Value | Source or status |
| --- | --- | --- |
| Reversible voltage, water activity, vapour pressure | Eqs. (2)–(5) | [34,35] |
| KOH conductivity | Eq. (10) | [37] |
| Anode exchange current density at 80 °C, j0,a,ref | 0.1 A m⁻² | representative, NiFe on Ni |
| Anode transfer coefficient, αa | 1.0 (Tafel slope 70 mV dec⁻¹ at 80 °C) | representative |
| Anode activation energy, Ea,a | 45 kJ mol⁻¹ | representative |
| Cathode exchange current density at 80 °C, j0,c,ref | 50 A m⁻² | representative, Ni |
| Cathode transfer coefficient, αc | 0.5 (Tafel slope 140 mV dec⁻¹ at 80 °C) | representative |
| Cathode activation energy, Ea,c | 30 kJ mol⁻¹ | representative |
| Bubble coverage at 0.4 A cm⁻², θref; exponent | 0.15; 0.3 | assumed; exponent after [29] |
| Void fraction per unit coverage, kε | 0.5 | assumed |
| Separator thickness, δsep; MacMullin number, NM | 500 µm; 4 | Zirfon-type diaphragm; NM within 2.6–4.0 [15] |
| Electrode resistances at the anchor, Rpore,a; Rcont,a | 0.083; 0.042 Ω cm² | fitted to the anchor |
| Crossover current density at 7 bar, jx | 30 A m⁻² | assumed |
| Anchor of the woven reference cell | 1.95 V at 0.4 A cm⁻², 80 °C, 7 bar, 30 wt% KOH | [5,12] |

## 2.3. Experimental basis and calibration of the micro-mesh electrode

### 2.3.1. Electrodes and measurements

The experimental data used in this work were obtained within the REHIP M-SWELT project (Table 3). Expanded Ni micro-meshes were supplied by The Expanded Metal Company in the geometries listed in Table 3, and the anodes were coated with a NiFe layered double hydroxide (LDH), a class of catalyst developed for seawater oxidation [33]. The preparation, characterisation and durability of these electrodes will be reported separately; only the cell comparison needed to calibrate the model is used here.

The comparison was carried out in a two-electrode cell with a commercial anion exchange membrane (AEM) as separator [11]. Configuration A used an LDH-coated micro-mesh anode and a bare micro-mesh cathode; configuration B replaced the micro-mesh with commercial woven Ni mesh, with otherwise identical assembly and operating conditions. The electrolyte was natural seawater to which KOH was added to 5 M; the precipitate formed on alkalisation was removed by filtration before use. At a constant cell voltage of 2.1 V, configuration A delivered 116 mA cm⁻² and configuration B 82 mA cm⁻² at the start of the test (Table 3; Fig. 2b), so the micro-mesh cell carried 41% more current at the same voltage.

Table 3. Two-electrode test from the M-SWELT project used for the calibration.

| Item | Value |
| --- | --- |
| Micro-mesh substrates | expanded Ni, The Expanded Metal Company |
| Long-way pitch × short-way pitch × strand width; open area | SAM-A 1.0 × 0.6 × 0.1 mm, 67%; SAM-B 1.0 × 0.7 × 0.2 mm, 43%; SAM-C 1.0 × 0.8 × 0.3 mm, 25%; SAM-E 1.5 × 0.9 × 0.2 mm, 56% |
| Anode catalyst | NiFe-LDH coating (catalyst class reviewed in [33]) |
| Two-electrode cell | AEM separator; A: coated micro-mesh anode and bare micro-mesh cathode; B: woven Ni mesh, otherwise identical |
| Electrolyte | natural seawater + 5 M KOH, filtered after alkalisation |
| Current density at 2.1 V, start of test | A: 116 mA cm⁻²; B: 82 mA cm⁻² (ratio A/B 1.41) |

### 2.3.2. Calibration procedure

The micro-mesh enters the plant-scale model through two factors, Fact in Eq. (7) and rres in Eq. (11). To calibrate them, the same kinetic model is applied to the laboratory cell at 1 bar with 5 M KOH and 0.55 M chloride, and all resistances of the laboratory cell are lumped into Rlab:

|  | Vlab=Erev+ηaj;Fact+ηcj;Fact+Rlab j | (14) |
| --- | --- | --- |

For configuration A the unknowns are Fact and Rlab; configuration B uses Fact = 1 and a resistance Rlab+ΔR. A cell temperature of 25 °C is used in the calibration. The two measured points give two equations for three unknowns, so the split of the micro-mesh advantage between a kinetic mechanism (larger Fact) and a resistive mechanism (smaller electrode-related resistance) cannot be identified from these data. We therefore define the kinetic share of the voltage advantage, evaluated at the current density jB of the woven-mesh cell,

|  | w=ΔVkinΔVkin+ΔR jB, ΔVkin=VkinjB;1-VkinjB;Fact | (15) |
| --- | --- | --- |

where Vkin = Erev+ηa+ηc, and solve for the family of calibrations with 0 ≤ w ≤ 1 (w = 0: purely resistive; w = 1: purely kinetic). At plant scale, Fact multiplies the effective exchange current densities of both electrodes, and rres=Rlab+ΔR/Rlab divides the electrode-related resistance, leaving the separator unchanged. The central case uses w = 0.5; the two limits bound the result, and w is sampled uniformly in the Monte Carlo analysis. Table 4 lists the calibrated factors and their effect at plant scale.

Table 4. Calibration to the two-electrode data and plant-scale effect at 0.4 A cm⁻², 80 °C, 7 bar and 5 M KOH.

| Case | w | Fact | rres | Rlab (Ω cm²) | ΔR (Ω cm²) | V at 0.4 A cm⁻² (V) | Saving (mV) | j at equal V (A cm⁻²) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Woven Ni mesh (reference) | – | 1.00 | 1.00 | – | – | 1.956 | – | 0.40 |
| Micro-mesh, resistive limit | 0.0 | 1.00 | 1.55 | 2.47 | 1.36 | 1.935 | 20 | 0.44 |
| Micro-mesh, central | 0.5 | 2.34 | 1.26 | 3.04 | 0.80 | 1.866 | 89 | 0.59 |
| Micro-mesh, kinetic limit | 1.0 | 7.78 | 1.00 | 3.84 | 0.00 | 1.769 | 187 | 0.79 |

## 2.4. Seawater feed routes

Water consumption is W = 9.12 kg per kg of hydrogen: 8.94 kg for the reaction plus 2% for evaporation and carry-over. The seawater composition follows the reference composition of Millero et al. [39]; per kilogram of seawater (salinity 35) it contains 0.9648 kg of water, 0.5459 mol Cl⁻, 0.0528 mol Mg²⁺, 0.0103 mol Ca²⁺ and 0.0023 mol HCO₃⁻. Two routes are compared (Table 5).

RO-fed route. Seawater is desalinated by reverse osmosis at 45% recovery (21.0 kg of seawater per kg of H₂) and polished to make-up quality. The all-in cost of demineralised water is taken as £1.0 m⁻³ (range £0.5–2.0 m⁻³), which includes the RO electricity of about 4 kWh m⁻³, i.e. about 0.04 kWh kg⁻¹ H₂. No chloride enters the KOH loop.

Direct-feed route. Seawater is softened with NaOH and Na₂CO₃ to remove Mg²⁺ and Ca²⁺, which precipitate when seawater is made alkaline [22,23], and filtered. Each kilogram of hydrogen then brings 5.2 mol of chloride into the electrolyte loop. At steady state, chloride is held at a set-point Cset by bleeding electrolyte, and the chloride balance gives the bleed volume per kilogram of hydrogen:

|  | B=xCl WCset-xCl wB | (16) |
| --- | --- | --- |

where xCl = 0.5658 mol kg⁻¹ is the chloride content of seawater per kilogram of water and wB is the water content of the loop electrolyte (kg L⁻¹); the seawater feed replaces both the water consumed and the water leaving with the bleed. The bleed discards B cKOH1-frec mol of KOH, where frec is the fraction recovered (zero in the base case), and must be neutralised with half that amount of H₂SO₄. Softening requires Fsw2Mg+HCO3 mol of NaOH and FswCa-HCO3 mol of Na₂CO₃ per kilogram of hydrogen, where Fsw is the seawater feed, and produces Mg(OH)₂ and CaCO₃ sludge. The set-point is limited to 2 M, the highest chloride concentration in the durability tests of NiFe-based anodes by Kuang et al. [40].

Chloride oxidation competes with oxygen evolution at the anode. In alkaline electrolytes, oxygen evolution remains selective as long as the anode overpotential stays below about 480 mV [24], and the modelled anode overpotential is 0.26–0.35 V at 0.4 A cm⁻² for every calibration case between 30 and 90 °C. Consistent with this criterion, NiFe-based anodes in 1 M KOH with 2 M NaCl at 0.4 A cm⁻² gave relative O₂ Faradaic efficiencies of 99–99.9% [40]. The chloride factor FECl in Eq. (12) is therefore 1 in the base case, and a loss ΔFECl of up to 1% is sampled in the Monte Carlo analysis.

Chloride also corrodes nickel electrodes. In 1 M KOH with 2 M NaCl at 0.4 A cm⁻² and room temperature, bare Ni foam failed within 20 min, NiFe hydroxide-coated Ni foam after 12 h and a NiFe anode protected by a sulfide interlayer after about 600 h; with 1.5 M NaCl the protected anode operated for more than 1,000 h, and in 6 M KOH with 1.5 M NaCl at 80 °C it sustained 0.4 A cm⁻² at 1.72 V for more than 1,000 h [40]. Durability over a stack life of several years has not, to our knowledge, been demonstrated. The electrode life Lel (operating hours) is therefore uncertain: in the deterministic base case the electrodes last as long as the stacks, the most favourable assumption for direct feed, and in the Monte Carlo analysis Lel is sampled log-uniformly between 1,000 h, of the order of the longest laboratory tests, and 60,000 h, the base-case stack life. When Lel is shorter than the stack life Lstack, the electrode sets are replaced at a cost equal to a fraction fel of the stack cost Cstack, which adds the annual cost

|  | Ael=fel Cstack8760 CFLel-8760 CFLstack, Lel<Lstack | (17) |
| --- | --- | --- |

The direct-feed route also carries treatment CAPEX for softening and bleed handling, taken as 3% of plant CAPEX.

Table 5. Feed-water flows and costs per kilogram of hydrogen.

| Quantity per kg H₂ | RO-fed | Direct, 1.5 M KOH, 2 M Cl⁻ | Direct, 5 M KOH, 2 M Cl⁻ |
| --- | --- | --- | --- |
| Seawater intake (kg) | 21.0 | 12.9 | 12.7 |
| Make-up water to the loop (kg) | 9.12 | 9.12 | 9.12 |
| Electrolyte bleed (L) | 0 | 3.53 | 3.47 |
| KOH lost in the bleed (kg) | 0 | 0.30 | 0.97 |
| H₂SO₄ for neutralisation (kg) | 0 | 0.26 | 0.85 |
| NaOH + Na₂CO₃ for softening (kg) | 0 | 0.067 | 0.066 |
| Sludge, dry (kg) | 0 | 0.053 | 0.052 |
| Water and chemicals cost (£) | 0.009 | 0.36 | 1.11 |

## 2.5. Techno-economic model

The LCOH is the ratio of annualised costs to annual hydrogen production:

|  | LCOH=CAPEX⋅CRF+CO&M+Astack+Ael+Celec+Cwater+CchemMH2 | (18) |
| --- | --- | --- |
|  | CRF=r1+rN1+rN-1 | (19) |

with r = 8% and N = 20 years. MH2 is the annual production (hydrogen flow × 8760 h × CF), CO&M is 2.5% of CAPEX per year, Celec = MH2 × SEC × electricity price, and Cwater and Cchem follow from Table 5. The CAPEX of a configuration is built from unit costs set by the reference plant (£1,100 kW⁻¹ installed, 10 MW, i.e. £11.0 million):

|  | CAPEX=carea A+cpower Prated+Cfixed+Ctreat | (20) |
| --- | --- | --- |
|  | A=2F nH2FE⋅j | (21) |

where nH2 is the molar hydrogen flow and Prated the rated AC power. The stack, 40% of the reference CAPEX, scales with active area, giving carea = £3,701 m⁻²; power electronics and BoP (45%) scale with rated power (cpower = £495 kW⁻¹); and fixed costs (15%) cover civil works, engineering and contingency. For other plant sizes, power-related costs scale with an exponent of 0.85, fixed costs with 0.6 and stacks linearly. Stacks are replaced every τ=Lstack/8760 CF years at a fraction frep of their initial cost Cstack, with a residual-value credit for the stack in service at the end of plant life:

|  | PVrep=kτ<N​frep Cstack1+r-kτ-f Cstack1-N-tlastτ1+r-N | (22) |
| --- | --- | --- |

where tlast is the time of the last replacement and f the cost fraction of the stack then in service, and Astack = PVrep × CRF. The credit keeps the LCOH continuous in capacity factor and stack life.

Break-even electrode premium. The micro-mesh cell is assigned the stack cost per unit area of the woven reference plus an extra electrode cost Δc (£ per m² of active area, both electrodes). The break-even premium is the value of Δc at which the LCOH of the RO-fed micro-mesh plant equals that of the woven reference. Because the premium enters stack CAPEX, O&M and replacements linearly, it follows from two evaluations of the LCOH.

Table 6 lists the economic inputs. The ranges were chosen to span recent estimates for installed alkaline systems and their operation [4,7,19]. The electricity-price range represents long-term renewable power purchase rather than grid supply; higher prices are examined separately (Section 3.8). Fixed values are the plant life (20 years), the fan electricity (0.02 kWh per kWh of heat rejected), Na₂CO₃ (£0.30 kg⁻¹), sludge disposal (£0.06 kg⁻¹) and the RO recovery (45%).

Table 6. Economic and uncertain inputs: base values and Monte Carlo distributions.

| Input | Base value | Distribution (minimum / mode / maximum) | Applies to |
| --- | --- | --- | --- |
| Electricity price (£ MWh⁻¹) | 55 | triangular 45 / 55 / 80 | all |
| Capacity factor, CF (–) | 0.8 | triangular 0.6 / 0.8 / 0.95 | all |
| Installed CAPEX of the reference plant (£ kW⁻¹) | 1,100 | triangular 800 / 1,100 / 1,500 | all |
| Stack share of CAPEX (–) | 0.4 | uniform 0.3 to 0.5 | all |
| Stack life, Lstack (h) | 60,000 | triangular 40,000 / 60,000 / 90,000 | all |
| Stack replacement cost fraction, frep (–) | 0.8 | uniform 0.6 to 1 | all |
| Fixed O&M (fraction of CAPEX per year) | 0.025 | triangular 0.015 / 0.025 / 0.04 | all |
| Discount rate, r (–) | 0.08 | triangular 0.05 / 0.08 / 0.1 | all |
| Rectifier efficiency, ηrect (–) | 0.96 | uniform 0.94 to 0.98 | all |
| BoP electricity, eBoP (kWh kg⁻¹) | 1.5 | triangular 1 / 1.5 / 3 | all |
| Voltage degradation, d (µV h⁻¹) | 2 | triangular 1 / 2 / 4 | all |
| Demineralised water (£ m⁻³) | 1 | triangular 0.5 / 1 / 2 | RO feed |
| Offset of the reference cell voltage (V) | 0 | uniform −0.1 to 0.1 | all |
| Kinetic share of the micro-mesh advantage, w (–) | 0.5 | uniform 0 to 1 | micro-mesh |
| KOH, 100% basis (£ kg⁻¹) | 1 | triangular 0.6 / 1 / 1.6 | direct feed |
| H₂SO₄ (£ kg⁻¹) | 0.12 | triangular 0.08 / 0.12 / 0.25 | direct feed |
| NaOH (£ kg⁻¹) | 0.45 | triangular 0.3 / 0.45 / 0.7 | direct feed |
| Chloride Faradaic-efficiency loss, ΔFECl (–) | 0 | uniform 0 to 0.01 | direct feed |
| Electrode life under direct feed, Lel (h) | 60,000 | log-uniform 1,000 to 60,000 | direct feed |
| Electrode replacement cost, fel (fraction of stack cost) | 0.25 | triangular 0.15 / 0.25 / 0.4 | direct feed |
| Treatment CAPEX (fraction of plant CAPEX) | 0.03 | triangular 0.01 / 0.03 / 0.06 | direct feed |

## 2.6. Uncertainty and sensitivity analysis

The Monte Carlo analysis draws N = 10,000 samples of the 21 uncertain inputs of Table 6 by Latin hypercube sampling [41] (SciPy, random seed 20260930) and evaluates three configurations for each sample: the RO-fed woven reference, the RO-fed micro-mesh plant and the direct-feed micro-mesh plant at its cost-optimal operating point. Using the same samples for all configurations (common random numbers) gives the distribution of the cost differences directly. The inputs are independent in the base case; a second run imposes a Spearman rank correlation of −0.5 between electricity price and capacity factor through a Gaussian copula, representing plants that run more when power is cheap. Convergence is checked by recomputing the mean and the 5th and 95th percentiles (P5, P95) for increasing N. Global sensitivity is measured by the Spearman rank correlation ρs between each input and the LCOH across the samples, and local sensitivity by a tornado diagram in which each input is moved from its P5 to its P95 with all other inputs at their base values.

# 3. RESULTS AND DISCUSSION

## 3.1. Anchoring and calibration of the cell model

Fig. 2a shows the polarisation curves at plant conditions. The woven-mesh reference passes through the anchor (1.95 V at 0.4 A cm⁻²) inside the commercial alkaline operating window, and the micro-mesh curves lie 19–187 mV lower at 0.4 A cm⁻², depending on the calibration case (20–187 mV at the 5 M KOH base case; Table 4).

Fig. 2. (a) Model polarisation curves at plant conditions (80 °C, 7 bar, 30 wt% KOH). The woven Ni-mesh reference is anchored to 1.95 V at 0.4 A cm⁻², inside the commercial alkaline operating window (shaded) [5,12]. The micro-mesh curve is the central calibration (w = 0.5); the band spans the resistive (w = 0) to kinetic (w = 1) limits. (b) Calibration against the M-SWELT two-electrode data (natural seawater + 5 M KOH, AEM separator, 2.1 V; 25 °C used in the calibration). Symbols: measured current densities at the start of the test. By construction, the model passes through both measured points for every w; the bands show the resulting range.

Fig. 2b compares the calibrated laboratory model with the M-SWELT data. By construction, every member of the calibration family passes through both measured points at 2.1 V, so the figure demonstrates consistency rather than independent validation. The data constrain the size of the micro-mesh advantage but not its mechanism: a purely resistive advantage (w = 0) and a purely kinetic one (w = 1) reproduce the same two points but diverge away from them, which full polarisation curves would distinguish. The fitted laboratory-cell resistance, 2.5–3.8 Ω cm², is about ten times the 0.28 Ω cm² of the industrial reference cell, consistent with the low current densities measured; only the relative advantage of the micro-mesh, not the absolute laboratory performance, is transferred to plant scale.

Two observations support this transfer. First, calibrating at 40 °C instead of 25 °C raises the central saving from 89 to 94 mV and the kinetic limit from 187 to 198 mV, so the result is not sensitive to the assumed cell temperature. Second, the calibrated factors are physically plausible: the central case (Fact = 2.34, rres = 1.26) corresponds to about twice the accessible catalytic area and a 21% lower electrode-related resistance. Expressed as capacity, the micro-mesh cell would carry 0.44–0.79 A cm⁻² (central 0.59 A cm⁻²) at the voltage at which the woven reference carries 0.40 A cm⁻².

The main limitation is that the calibration rests on one operating point in a laboratory cell with an AEM separator, whereas the plant model assumes a Zirfon-type diaphragm at 80 °C. Polarisation curves and impedance spectra of configurations A and B at 25–80 °C would identify w and narrow the 20–187 mV range (Section 3.10).

## 3.2. Voltage breakdown and electrode comparison

Fig. 3a shows the overpotentials of the micro-mesh cell (central case) at plant conditions, and Fig. 3b compares the breakdown at 0.4 A cm⁻² for the four electrode cases. For the woven reference, the cell voltage of 1.956 V comprises Erev = 1.231 V, anode and cathode activation overpotentials of 0.327 and 0.277 V, and ohmic losses of 0.063 V in the separator and 0.057 V in the electrodes and contacts. Activation therefore accounts for 83% of the overpotential at 0.4 A cm⁻² and still exceeds the ohmic loss at 0.8 A cm⁻² (Fig. 3a): the ohmic loss grows linearly with current density but does not become dominant within the range studied.

Fig. 3. (a) Overpotentials against current density for the micro-mesh cell (central case) at 80 °C, 7 bar and 5 M KOH. (b) Breakdown at 0.4 A cm⁻² for the woven reference and the three micro-mesh calibration cases; the cell voltage equals Erev (1.231 V) plus the bar.

The micro-mesh lowers the cell voltage to 1.935 V in the resistive limit, 1.866 V in the central case and 1.769 V in the kinetic limit. In the resistive limit only the electrode and contact term changes (from 0.057 to 0.037 V); in the kinetic limit the anode overpotential falls by 0.062 V and the cathode overpotential by 0.124 V, the larger cathodic reduction reflecting the smaller cathodic transfer coefficient. The anode overpotential of the coated micro-mesh (0.30 V) is well below the 480 mV threshold for chloride oxidation [24], which matters for any operation with residual chloride.

## 3.3. Effect of temperature

Fig. 4 shows the effect of temperature for the micro-mesh cell (central case) at 7 bar. At 0.4 A cm⁻², raising the temperature from 50 to 90 °C lowers the cell voltage from 1.976 to 1.834 V (Fig. 4a). Erev falls from 1.260 V at 40 °C to 1.224 V at 90 °C, while Vtn changes little (1.479 and 1.471 V; Fig. 4b). Between 40 and 90 °C the cathode activation overpotential falls from 0.270 to 0.214 V, the anode activation overpotential from 0.320 to 0.297 V, and the ohmic loss from 0.169 to 0.100 V, a factor of 1.7 that follows mainly from the rising conductivity of 5 M KOH (Fig. 4c). The benefit of temperature is therefore spread over all loss terms rather than concentrated in one.

Fig. 4. Effect of temperature (micro-mesh, central case, 7 bar, 5 M KOH). (a) Polarisation curves from 50 to 90 °C. (b) Reversible and thermoneutral voltages. (c) Overpotentials at 0.4 A cm⁻²; the ohmic loss falls by a factor of 1.7 between 40 and 90 °C, following the KOH conductivity [37].

For RO-fed operation the LCOH falls from £4.71 kg⁻¹ at 30 °C to £4.35 kg⁻¹ at 80 °C (Fig. 7d), so the stack should run as hot as separator and material stability allow. The same trend holds for direct feed (Fig. 7d), provided that electrode life does not shorten with temperature, which is not quantified here (Section 3.10).

## 3.4. Effect of pressure

At 80 °C and 0.4 A cm⁻², raising the balanced operating pressure from 1 to 7 bar increases the cell voltage by 53 mV, and raising it from 5 to 25 bar by 38 mV; the increase is entirely the Nernst term of Eq. (2) (Fig. 5a). In energy terms, operation at 7 bar raises the SEC of the electrolyser by 1.83 kWh kg⁻¹ relative to 1 bar, the sum of the Nernst term and a larger crossover loss that lowers the Faradaic efficiency from 99.9% to 99.25% (Fig. 5b). Producing hydrogen at 7 bar saves 1.13 kWh kg⁻¹ of multistage mechanical compression to 30 bar (isentropic efficiency 0.75), so the net penalty is 0.70 kWh kg⁻¹; at 30 bar the net penalty is 2.2 kWh kg⁻¹. Electrochemical compression is thermodynamically efficient, but it also compresses the oxygen, which is usually vented, and it increases gas crossover. Pressurised operation at 5–10 bar is therefore justified by smaller gas volumes and fewer compressor stages rather than by an energy saving.

Fig. 5. Effect of operating pressure (micro-mesh, 80 °C, 0.4 A cm⁻²). (a) Cell-voltage increase relative to 1 bar, which is entirely the Nernst term. (b) Change in electrolyser specific energy relative to 1 bar (Nernst term and crossover), energy for multistage mechanical compression of H₂ to 30 bar (isentropic efficiency 0.75), and their sum.

## 3.5. Cost-optimal current density

At fixed hydrogen output, the nominal current density sets the trade-off between stack CAPEX, which scales with active area and therefore with 1/j, and electricity cost, which rises with cell voltage. Fig. 6 shows the resulting LCOH curves. The optimum lies at 0.55 A cm⁻² for the woven reference (£4.47 kg⁻¹) and at 0.57 A cm⁻² for the central micro-mesh case (£4.30 kg⁻¹), £0.04–0.06 kg⁻¹ below the LCOH at 0.4 A cm⁻² across the calibration cases. The curves are flat near the optimum: the LCOH of the micro-mesh plant stays within 1% of its minimum between 0.42 and 0.80 A cm⁻². The micro-mesh lowers the whole curve. A resistive advantage also moves the optimum to a higher current density (0.59 A cm⁻² in the resistive limit), because it reduces the voltage penalty of running harder, whereas a kinetic advantage leaves the optimum at 0.55 A cm⁻².

Fig. 6. LCOH against nominal current density at fixed hydrogen output (RO-fed, 80 °C, 7 bar, £55 MWh⁻¹, capacity factor 80%). Markers show the optimum for the woven reference (0.55 A cm⁻²) and the central micro-mesh case (0.57 A cm⁻²); the band spans the micro-mesh calibration range.

## 3.6. Seawater feed routes: desalination versus direct feed

Fig. 7a compares the LCOH breakdown of the two feed routes, Table 5 lists the flows and Table 7 the cost components. For the RO-fed plant, desalinated water costs £0.009 kg⁻¹ H₂, 0.2% of the LCOH, which agrees with the conclusion of Khan et al. [27] and Hausmann et al. [28] that desalination adds little to the cost of hydrogen.

Fig. 7. Feed-water routes at 80 °C, 7 bar and 0.4 A cm⁻². (a) LCOH breakdown for the RO-fed woven reference; the RO-fed micro-mesh plant (central case); direct seawater feed at its cost-optimal point (1.5 M KOH, chloride held at 2 M) without chloride oxidation and with electrodes that last as long as the stacks; the same with the electrode sets replaced every 8,760 operating hours; and direct feed with 95% KOH recovery from the bleed (5 M KOH, 2 M chloride). (b) Chemical cost of direct feed (KOH lost in the bleed, neutralisation, softening) against the chloride set-point for four KOH concentrations; set-points above 2 M (shaded) exceed the highest chloride concentration in the durability tests of NiFe anodes by Kuang et al. [40]. (c) LCOH of direct feed against electrode life; shaded: range sampled in the Monte Carlo analysis. (d) LCOH against operating temperature; for direct feed, electrode life is assumed not to depend on temperature.

Direct feed adds three costs. First, every kilogram of hydrogen brings 5.2 mol of chloride into the loop, and this chloride can leave only with the bleed. Holding chloride at 2 M in 5 M KOH requires a bleed of 3.5 L kg⁻¹ H₂, which discards 0.97 kg of KOH and consumes 0.85 kg of H₂SO₄ for neutralisation, £1.11 kg⁻¹ H₂ in chemicals (Table 5). Fig. 7b shows the trade-off: a lower set-point multiplies the bleed, and set-points above 2 M exceed the chloride concentrations in which NiFe anodes have been tested [40]. Second, the KOH lost in the bleed favours a dilute loop: at 1.5 M KOH the chemicals cost £0.36 kg⁻¹, but the lower conductivity raises the cell voltage from 1.866 to 1.986 V, whereas a concentrated loop (35 wt%) raises the chemical cost to £1.79 kg⁻¹ at 2 M chloride. Third, electrodes that degrade faster in chloride than in pure alkaline electrolyte must be replaced between stack replacements (Eq. (17)).

A grid search over KOH concentration (1–6.9 M) and chloride set-point (0.75–2 M) at 80 °C places the cost optimum at 1.5 M KOH and 2 M chloride. Without chloride oxidation and with electrodes that last as long as the stacks, direct feed then costs £4.95 kg⁻¹, £0.60 kg⁻¹ more than the RO-fed micro-mesh plant (Fig. 7a; Table 7): £0.36 kg⁻¹ for chemicals, £0.19 kg⁻¹ for electricity and £0.06 kg⁻¹ for CAPEX and O&M, less £0.01 kg⁻¹ for the water that is no longer desalinated. The gap is £0.58–0.73 kg⁻¹ between 30 and 90 °C (Fig. 7d). The electrolyte conductivity of Eq. (10) counts only the KOH, which penalises the dilute loop. Crediting the chloride with half or all of the conductivity of KOH of the same molarity, the latter an upper bound because the hydroxide ion is far more mobile than the chloride ion, moves the optimum to 1 M KOH, the lowest concentration considered, and lowers the LCOH to £4.75 and £4.67 kg⁻¹; direct feed then remains £0.41 and £0.33 kg⁻¹ above RO feed.

Electrode life is the main open question. In 1 M KOH with 2 M NaCl, a NiFe anode lasted 12 h on bare Ni foam and about 600 h with a protective sulfide interlayer, and the protected anode exceeded 1,000 h at 1.5 M NaCl [40]; operation for years in alkaline chloride solutions has not, to our knowledge, been demonstrated. If the electrode sets last 8,760 operating hours, their replacement adds £0.60 kg⁻¹ and the LCOH rises to £5.55 kg⁻¹; at 2,000 h it reaches £7.94 kg⁻¹ and at 1,000 h £11.04 kg⁻¹ (Fig. 7c).

Recovering KOH from the bleed would remove most of the chemical cost and allow a concentrated loop. With 95% recovery, the optimum moves to 5 M KOH and the LCOH falls to £4.46 kg⁻¹, still £0.11 kg⁻¹ above RO feed (£0.09 kg⁻¹ with the chloride credited with the conductivity of KOH) before any cost of the recovery process is counted (Fig. 7a).

These results support the case for desalination made by Khan et al. [27] and Hausmann et al. [28], and they add a mechanism specific to alkaline electrolysis: the KOH loop cannot be operated once-through, so the chloride purge carries the electrolyte with it. Direct seawater feed to an alkaline loop would need near-complete KOH recovery from the bleed and electrodes that withstand concentrated chloride for years; neither has, to our knowledge, been demonstrated, and even both together would leave direct feed slightly dearer than RO feed at the conditions assessed here.

Table 7. Cell voltage, lifetime-average SEC, CAPEX and LCOH components per kilogram of hydrogen at the base case (0.4 A cm⁻², £55 MWh⁻¹, capacity factor 80%). Components may not add up exactly because of rounding.

| Quantity | RO-fed, woven Ni mesh (reference) | RO-fed, micro-mesh, resistive limit | RO-fed, micro-mesh, central | RO-fed, micro-mesh, kinetic limit | Direct feed, micro-mesh ᵃ | Direct feed, electrode life 8,760 h ᵇ | Direct feed, 95% KOH recovery ᶜ |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cell voltage at 0.4 A cm⁻² (V) | 1.956 | 1.935 | 1.866 | 1.769 | 1.986 | 1.986 | 1.868 |
| Lifetime-average SEC (kWh kg⁻¹) | 58.0 | 57.5 | 55.5 | 52.7 | 58.9 | 58.9 | 55.5 |
| CAPEX (£ million) | 11.00 | 10.95 | 10.78 | 10.53 | 11.41 | 11.41 | 11.10 |
| Electricity (£ kg⁻¹) | 3.19 | 3.16 | 3.05 | 2.90 | 3.24 | 3.24 | 3.05 |
| Capital recovery (£ kg⁻¹) | 0.90 | 0.90 | 0.88 | 0.86 | 0.93 | 0.93 | 0.91 |
| O&M (£ kg⁻¹) | 0.22 | 0.22 | 0.22 | 0.21 | 0.23 | 0.23 | 0.22 |
| Stack replacement (£ kg⁻¹) | 0.19 | 0.19 | 0.19 | 0.19 | 0.19 | 0.19 | 0.19 |
| Electrode replacement (£ kg⁻¹) | – | – | – | – | – | 0.60 | – |
| Water and chemicals (£ kg⁻¹) | 0.01 | 0.01 | 0.01 | 0.01 | 0.36 | 0.36 | 0.08 |
| LCOH (£ kg⁻¹) | 4.51 | 4.47 | 4.35 | 4.17 | 4.95 | 5.55 | 4.46 |

ᵃ Cost-optimal point at 80 °C: 1.5 M KOH, chloride held at 2 M; no chloride oxidation; electrodes last as long as the stacks. ᵇ As ᵃ, with the electrode sets replaced every 8,760 operating hours. ᶜ 5 M KOH, 2 M chloride and 95% of the KOH recovered from the bleed, without the cost of recovery; otherwise as ᵃ.

## 3.7. Break-even electrode premium

Fig. 8 answers whether the efficiency gain of the micro-mesh pays for a more expensive electrode. At £55 MWh⁻¹, the RO-fed micro-mesh plant matches the woven reference at an electrode premium of £950 m⁻² of active area in the central case, £217 m⁻² in the resistive limit and £1,985 m⁻² in the kinetic limit. The central value is 26% of the specific stack cost (£3,701 m⁻²). The break-even premium rises linearly with the electricity price, because the saving is mainly in electricity; at £100 MWh⁻¹ it reaches £1,619 m⁻² in the central case. Across the Monte Carlo samples, the break-even premium has a median of £1,028 m⁻² and a P5–P95 range of £303–2,148 m⁻², and it exceeds £300 m⁻² in 95% of the samples. The micro-mesh is therefore economically justified with high confidence if its extra cost, including the coating and for both electrodes, is below about £300 m⁻² of active area, and in the central case if it is below about £950 m⁻². A manufacturing cost of the micro-mesh relative to woven Ni mesh would complete this assessment.

Fig. 8. Break-even micro-mesh electrode premium against electricity price: the extra electrode cost per m² of active area (both electrodes) at which the RO-fed micro-mesh plant matches the LCOH of the woven reference. Solid line: central calibration; band: resistive to kinetic limits.

## 3.8. Electricity price, capacity factor and plant size

Fig. 9a shows the LCOH of the RO-fed micro-mesh plant against electricity price. The relation is linear, with a slope equal to the lifetime-average SEC (55.5 kWh kg⁻¹): at a capacity factor of 80% the LCOH rises from £2.96 kg⁻¹ at £30 MWh⁻¹ to £7.95 kg⁻¹ at £120 MWh⁻¹. Electricity accounts for 70% of the base-case LCOH. For comparison, the eleven projects awarded in the UK’s first Hydrogen Allocation Round had a weighted average strike price of £241 MWh⁻¹ of hydrogen [42], about £8–9.5 kg⁻¹ depending on the heating-value basis, which reflects smaller plants and higher electricity costs than the base case here.

Fig. 9. Deterministic sensitivities, RO-fed. (a) LCOH against electricity price at capacity factors of 50, 80 and 95% (micro-mesh, central case); the slope equals the lifetime-average SEC. (b) LCOH against capacity factor, which decreases monotonically. (c) LCOH against plant size (power-related CAPEX scaling exponent 0.85, fixed costs 0.6, stacks linear).

Fig. 9b shows that the LCOH decreases monotonically with capacity factor, from £7.33 kg⁻¹ at 20% to £4.15 kg⁻¹ at 100%, because the fixed costs are spread over more hydrogen while the electricity cost per kilogram is unchanged: running more hours does not change the operating point of the stack. An interior optimum in capacity factor would require time-varying electricity prices, so that additional operating hours are bought at higher prices [3]; with the constant price assumed here, the highest achievable capacity factor is always the cheapest.

Fig. 9c shows the effect of plant size. The LCOH falls from £4.80 kg⁻¹ at 1 MW to £4.35 kg⁻¹ at 10 MW and £4.05 kg⁻¹ at 200 MW, flattening above about 50 MW, where the specific cost of power electronics and fixed costs approaches its scale limit and electricity dominates. The micro-mesh advantage is £0.15–0.17 kg⁻¹ at all sizes.

## 3.9. Uncertainty analysis

Fig. 10a shows the LCOH distributions from the Monte Carlo analysis and Fig. 10b their convergence. The RO-fed micro-mesh plant has a mean LCOH of £4.72 kg⁻¹ (standard deviation £0.50 kg⁻¹; P5–P95 £3.95–5.59 kg⁻¹), the RO-fed woven reference £4.91 kg⁻¹ (P5–P95 £4.13–5.80 kg⁻¹) and the direct-feed plant £6.95 kg⁻¹ (P5–P95 £4.93–11.18 kg⁻¹). Because all configurations share the same samples, the differences are sampled directly: at equal electrode cost, the micro-mesh plant is cheaper than the woven reference in every sample, by £0.19 kg⁻¹ on average (P5–P95 £0.05–0.35 kg⁻¹), and direct feed is dearer than RO feed in every sample, by £2.23 kg⁻¹ on average (P5–P95 £0.68–6.35 kg⁻¹; minimum £0.50 kg⁻¹).

Fig. 10. Monte Carlo uncertainty analysis (Latin hypercube, N = 10,000, seed 20260930; input distributions in Table 6). (a) LCOH distributions for the three configurations, with the deterministic base cases as dotted lines; the axis ends at £13 kg⁻¹, above which lie 1.6% of the direct-feed samples. (b) Convergence of the mean, P5 and P95 for the RO-fed micro-mesh plant.

The distributions are slightly right-skewed (skewness 0.29 for the RO-fed micro-mesh plant) because several input distributions are, notably the electricity price (mean £60 MWh⁻¹, mode £55 MWh⁻¹); the deterministic base case therefore lies at the 24th percentile. The direct-feed distribution is strongly right-skewed (skewness 1.58) because electrode life is sampled log-uniformly down to 1,000 h; its deterministic case, with electrodes that last as long as the stacks, lies at the 5th percentile. With a rank correlation of −0.5 between electricity price and capacity factor, the mean is unchanged (£4.72 kg⁻¹) and the P5–P95 range widens slightly to £3.90–5.67 kg⁻¹. Beyond N = 5,000 the mean changes by less than £0.01 kg⁻¹ and the percentiles by less than £0.02 kg⁻¹ (Fig. 10b).

Fig. 11 ranks the inputs. Electricity price dominates (ρs = 0.82; a tornado swing of £1.34 kg⁻¹ between its P5 and P95), followed by installed CAPEX (ρs = 0.32; £0.56 kg⁻¹), the offset of the reference cell voltage (0.26; £0.40 kg⁻¹), capacity factor (−0.20; £0.31 kg⁻¹) and the micro-mesh mechanism w (−0.18; £0.27 kg⁻¹). The two electrochemical uncertainties, the anchor voltage and the mechanism of the micro-mesh advantage, thus rank third and fifth, ahead of the discount rate, O&M and stack life, and they are the ones that experiments can reduce. For the direct-feed plant, electrode life dominates (ρs = −0.84; a tornado swing of £4.92 kg⁻¹ between 1,230 and 48,900 h), well ahead of electricity price (ρs = 0.33; £1.43 kg⁻¹), whereas a chloride Faradaic-efficiency loss of up to 1% moves the LCOH by only £0.04 kg⁻¹ (Supplementary Material, results tables T11 and T13). Electrode life in concentrated chloride is therefore the measurement on which any case for direct feed depends.

Fig. 11. (a) Tornado diagram for the RO-fed micro-mesh plant (base £4.35 kg⁻¹): each input moves from its P5 to its P95 with the others at base values; blue bars lower and orange bars raise the LCOH, and the labels give the input values. (b) Spearman rank correlation of each input with the LCOH across the Monte Carlo samples.

## 3.10. Limitations and further work

The results rest on assumptions that further work should test. (i) The micro-mesh advantage is calibrated to one operating point in a laboratory cell with an AEM separator, with 25 °C used in the calibration; its transfer to a Zirfon-type zero-gap cell at 80 °C assumes that the advantage acts through the effective exchange current density and the electrode-related resistance. (ii) The kinetic parameters are representative rather than fitted, and the reference cell is anchored to a single commercial operating point; the ±0.10 V uncertainty of this anchor is the third most influential input. (iii) The kinetic parameters do not depend on KOH concentration, which favours the dilute direct-feed loop, and the electrolyte conductivity counts only the KOH, which penalises it; Section 3.6 bounds the second effect. (iv) Chloride leaves the loop only with the bleed, and its oxidation is limited to a Faradaic-efficiency loss of at most 1%, consistent with oxygen selectivities of 99–99.9% reported for NiFe anodes in 1 M KOH with 2 M NaCl [40]; set-points above 2 M are not considered. (v) Electrode life under direct feed is sampled between 1,000 h and the stack life. Laboratory tests have reached about 600 h at 2 M NaCl and more than 1,000 h at 1.5 M NaCl [40], so the lower end of this range is not pessimistic; life over years, and its dependence on temperature, chloride concentration and start–stop cycles, has not been established and is not modelled. (vi) The analysis is steady state; intermittent operation, hydrogen compression and storage, and oxygen revenue lie outside the system boundary. The measurements that would most reduce the remaining uncertainty are polarisation curves and impedance spectra of micro-mesh and woven-mesh cells at 25–80 °C, the life of electrodes in concentrated alkaline chloride solutions at operating temperature, and a manufacturing cost of the micro-mesh.

# 4. CONCLUSION

This study coupled an experimentally calibrated zero-gap cell model with feed-water and cost models to assess expanded Ni micro-mesh electrodes for alkaline electrolysis of seawater. A like-for-like two-electrode test of micro-mesh and woven Ni-mesh cells in natural seawater with 5 M KOH was used to calibrate the micro-mesh advantage. Transferred to a zero-gap cell at 80 °C and 0.4 A cm⁻², it corresponds to a voltage saving of 20–187 mV (central 89 mV); the range reflects the unidentified split between kinetic and resistive mechanisms. The ohmic resistance of the modelled reference cell agrees with published measurements on zero-gap cells with Zirfon diaphragms. For an RO-fed plant producing 177.5 kg h⁻¹ of hydrogen, the micro-mesh lowers the LCOH from £4.51 to £4.35 kg⁻¹ (range £4.17–4.47 kg⁻¹) and breaks even at an extra electrode cost of up to £950 m⁻² of active area (range £217–1,985 m⁻²; above £300 m⁻² in 95% of the Monte Carlo samples). Direct seawater feed is not competitive in an alkaline loop. Without chloride oxidation and with electrodes that last as long as the stacks, its cost-optimal point (80 °C, 1.5 M KOH, 2 M chloride) costs £4.95 kg⁻¹, £0.60 kg⁻¹ more than RO feed, because the chloride bleed discards KOH and forces a dilute, less conductive electrolyte; crediting the chloride with the conductivity of KOH narrows the gap to £0.33 kg⁻¹. Recovering 95% of the KOH from the bleed leaves direct feed £0.11 kg⁻¹ above RO feed, whereas electrode sets that last 8,760 operating hours add £0.60 kg⁻¹. The water for RO feed costs less than 1% of the LCOH. The cell voltage falls with temperature through all loss terms; balanced pressurisation to 7 bar costs a net 0.70 kWh kg⁻¹ relative to atmospheric operation with mechanical compression; the cost-optimal current density is 0.55–0.59 A cm⁻²; and the LCOH decreases monotonically with capacity factor. In the Monte Carlo analysis (10,000 Latin-hypercube samples), the RO-fed micro-mesh plant averages £4.72 kg⁻¹ (P5–P95 £3.95–5.59 kg⁻¹); it is cheaper than woven mesh at equal electrode cost, and direct feed is dearer than RO feed, in every sample. Electricity price dominates the uncertainty of the RO-fed plant (ρs = 0.82), followed by CAPEX, the anchor cell voltage, capacity factor and the micro-mesh mechanism; electrode life dominates that of direct feed (ρs = −0.84).

# DECLARATION OF COMPETING INTEREST

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

# ACKNOWLEDGMENT

The research outlined in this paper is part of REHIP project (Research England Hydrogen Innovation Project) and the authors acknowledge the financial contribution of UKRI, Durham and Teesside Universities. The authors also acknowledge the support of The Expanded Metal Company, Hartlepool, as the industrial partner of the project, for its valuable contributions and collaboration. The authors thank Dr Prasanth Prabhakaran, Dr Muhammad Maqbool and Dr Jiang Chulin (Teesside University) for the electrode preparation and electrochemical testing carried out within REHIP M-SWELT.

# DATA AVAILABILITY

The model code, input files and the data behind all figures can provided as Supplementary Material on reasonable demand. The two current densities used for the calibration are given in Table 3; the full experimental results of the M-SWELT project will be reported separately.

# Declaration of generative AI and AI-assisted technologies in the manuscript preparation process

During the preparation of this work the authors used Claude (Anthropic) to improve the clarity, grammar, and readability of the manuscript. All equations, inputs and results were checked by the authors. After using this tool/service, the authors reviewed and edited the content and take full responsibility for the content of the published article.

# REFERENCES

[1] IEA. The future of hydrogen: seizing today’s opportunities. Paris: International Energy Agency; 2019. https://www.iea.org/reports/the-future-of-hydrogen [accessed 6 October 2026].

[2] Staffell I, Scamman D, Velazquez Abad A, Balcombe P, Dodds PE, Ekins P, et al. The role of hydrogen and fuel cells in the global energy system. Energy Environ Sci 2019;12:463–91. https://doi.org/10.1039/C8EE01157E.

[3] Glenk G, Reichelstein S. Economics of converting renewable power to hydrogen. Nat Energy 2019;4:216–22. https://doi.org/10.1038/s41560-019-0326-1.

[4] IRENA. Green hydrogen cost reduction: scaling up electrolysers to meet the 1.5 °C climate goal. Abu Dhabi: International Renewable Energy Agency; 2020. https://www.irena.org/publications/2020/Dec/Green-hydrogen-cost-reduction [accessed 6 October 2026].

[5] Buttler A, Spliethoff H. Current status of water electrolysis for energy storage, grid balancing and sector coupling via power-to-gas and power-to-liquids: a review. Renew Sustain Energy Rev 2018;82:2440–54. https://doi.org/10.1016/j.rser.2017.09.003.

[6] Wang M, Wang Z, Gong X, Guo Z. The intensification technologies to water electrolysis for hydrogen production – a review. Renew Sustain Energy Rev 2014;29:573–88. https://doi.org/10.1016/j.rser.2013.08.090.

[7] IEA. Global hydrogen review 2023. Paris: International Energy Agency; 2023. https://www.iea.org/reports/global-hydrogen-review-2023 [accessed 6 October 2026].

[8] Zeng K, Zhang D. Recent progress in alkaline water electrolysis for hydrogen production and applications. Prog Energy Combust Sci 2010;36:307–26. https://doi.org/10.1016/j.pecs.2009.11.002.

[9] Ursúa A, Gandía LM, Sanchis P. Hydrogen production from water electrolysis: current status and future trends. Proc IEEE 2012;100:410–26. https://doi.org/10.1109/JPROC.2011.2156750.

[10] Brauns J, Turek T. Alkaline water electrolysis powered by renewable energy: a review. Processes 2020;8:248. https://doi.org/10.3390/pr8020248.

[11] Vincent I, Bessarabov D. Low cost hydrogen production by anion exchange membrane electrolysis: a review. Renew Sustain Energy Rev 2018;81:1690–704. https://doi.org/10.1016/j.rser.2017.05.258.

[12] Carmo M, Fritz DL, Mergel J, Stolten D. A comprehensive review on PEM water electrolysis. Int J Hydrogen Energy 2013;38:4901–34. https://doi.org/10.1016/j.ijhydene.2013.01.151.

[13] Ulleberg Ø. Modeling of advanced alkaline electrolyzers: a system simulation approach. Int J Hydrogen Energy 2003;28:21–33. https://doi.org/10.1016/S0360-3199(02)00033-2.

[14] Sánchez M, Amores E, Rodríguez L, Clemente-Jul C. Semi-empirical model and experimental validation for the performance evaluation of a 15 kW alkaline water electrolyzer. Int J Hydrogen Energy 2018;43:20332–45. https://doi.org/10.1016/j.ijhydene.2018.09.029.

[15] de Groot MT, Vreman AW. Ohmic resistance in zero gap alkaline electrolysis with a Zirfon diaphragm. Electrochim Acta 2021;369:137684. https://doi.org/10.1016/j.electacta.2020.137684.

[16] Haverkort JW, Rajaei H. Voltage losses in zero-gap alkaline water electrolysis. J Power Sources 2021;497:229864. https://doi.org/10.1016/j.jpowsour.2021.229864.

[17] Sánchez M, Amores E, Abad D, Rodríguez L, Clemente-Jul C. Aspen Plus model of an alkaline electrolysis system for hydrogen production. Int J Hydrogen Energy 2020;45:3916–29. https://doi.org/10.1016/j.ijhydene.2019.12.027.

[18] Zheng Y, You S, Bindner HW, Münster M. Optimal day-ahead dispatch of an alkaline electrolyser system concerning thermal–electric properties and state-transitional dynamics. Appl Energy 2022;307:118091. https://doi.org/10.1016/j.apenergy.2021.118091.

[19] Schmidt O, Gambhir A, Staffell I, Hawkes A, Nelson J, Few S. Future cost and performance of water electrolysis: an expert elicitation study. Int J Hydrogen Energy 2017;42:30470–92. https://doi.org/10.1016/j.ijhydene.2017.10.045.

[20] Terlouw T, Bauer C, McKenna R, Mazzotti M. Large-scale hydrogen production via water electrolysis: a techno-economic and environmental assessment. Energy Environ Sci 2022;15:3583–602. https://doi.org/10.1039/D2EE01023B.

[21] Parkinson B, Balcombe P, Speirs JF, Hawkes AD, Hellgardt K. Levelized cost of CO₂ mitigation from hydrogen production routes. Energy Environ Sci 2019;12:19–40. https://doi.org/10.1039/C8EE02079E.

[22] Dresp S, Dionigi F, Klingenhof M, Strasser P. Direct electrolytic splitting of seawater: opportunities and challenges. ACS Energy Lett 2019;4:933–42. https://doi.org/10.1021/acsenergylett.9b00220.

[23] Tong W, Forster M, Dionigi F, Dresp S, Sadeghi Erami R, Strasser P, et al. Electrolysis of low-grade and saline surface water. Nat Energy 2020;5:367–77. https://doi.org/10.1038/s41560-020-0550-8.

[24] Dionigi F, Reier T, Pawolek Z, Gliech M, Strasser P. Design criteria, operating conditions, and nickel–iron hydroxide catalyst materials for selective seawater electrolysis. ChemSusChem 2016;9:962–72. https://doi.org/10.1002/cssc.201501581.

[25] Xie H, Zhao Z, Liu T, Wu Y, Lan C, Jiang W, et al. A membrane-based seawater electrolyser for hydrogen generation. Nature 2022;612:673–8. https://doi.org/10.1038/s41586-022-05379-5.

[26] Guo J, Zheng Y, Hu Z, Zheng C, Mao J, Du K, et al. Direct seawater electrolysis by adjusting the local reaction environment of a catalyst. Nat Energy 2023;8:264–72. https://doi.org/10.1038/s41560-023-01195-x.

[27] Khan MA, Al-Attas T, Roy S, Rahman MM, Ghaffour N, Thangadurai V, et al. Seawater electrolysis for hydrogen production: a solution looking for a problem? Energy Environ Sci 2021;14:4831–9. https://doi.org/10.1039/D1EE00870F.

[28] Hausmann JN, Schlögl R, Menezes PW, Driess M. Is direct seawater splitting economically meaningful? Energy Environ Sci 2021;14:3679–85. https://doi.org/10.1039/D0EE03659E.

[29] Vogt H, Balzer RJ. The bubble coverage of gas-evolving electrodes in stagnant electrolytes. Electrochim Acta 2005;50:2073–9. https://doi.org/10.1016/j.electacta.2004.09.025.

[30] Angulo A, van der Linde P, Gardeniers H, Modestino M, Fernández Rivas D. Influence of bubbles on the energy conversion efficiency of electrochemical reactors. Joule 2020;4:555–79. https://doi.org/10.1016/j.joule.2020.01.005.

[31] Zhou D, Li P, Lin X, McKinley A, Kuang Y, Liu W, et al. Layered double hydroxide-based electrocatalysts for the oxygen evolution reaction: identification and tailoring of active sites, and superaerophobic nanoarray electrode assembly. Chem Soc Rev 2021;50:8790–817. https://doi.org/10.1039/D1CS00186H.

[32] Dong T, Duan X, Huang Y, Huang D, Luo Y, Liu Z, et al. Enhancement of hydrogen production via optimizing micro-structures of electrolyzer on a microfluidic platform. Appl Energy 2024;356:122376. https://doi.org/10.1016/j.apenergy.2023.122376.

[33] Karikkethu Prabhakaran P, Abidoye AK, Roy S, Krishnan VV. Layered double hydroxides for sustainable hydrogen production from seawater. Mater Today Sustain 2025;31:101130. https://doi.org/10.1016/j.mtsust.2025.101130.

[34] LeRoy RL, Bowen CT, LeRoy DJ. The thermodynamics of aqueous water electrolysis. J Electrochem Soc 1980;127:1954–62. https://doi.org/10.1149/1.2130044.

[35] Balej J. Water vapour partial pressures and water activities in potassium and sodium hydroxide solutions over wide concentration and temperature ranges. Int J Hydrogen Energy 1985;10:233–43. https://doi.org/10.1016/0360-3199(85)90093-X.

[36] MacMullin RB, Muccini GA. Characteristics of porous beds and structures. AIChE J 1956;2:393–403. https://doi.org/10.1002/aic.690020320.

[37] Gilliam RJ, Graydon JW, Kirk DW, Thorpe SJ. A review of specific conductivities of potassium hydroxide solutions for various concentrations and temperatures. Int J Hydrogen Energy 2007;32:359–64. https://doi.org/10.1016/j.ijhydene.2006.10.062.

[38] Tjaden B, Cooper SJ, Brett DJL, Kramer D, Shearing PR. On the origin and application of the Bruggeman correlation for analysing transport phenomena in electrochemical systems. Curr Opin Chem Eng 2016;12:44–51. https://doi.org/10.1016/j.coche.2016.02.006.

[39] Millero FJ, Feistel R, Wright DG, McDougall TJ. The composition of Standard Seawater and the definition of the Reference-Composition Salinity Scale. Deep Sea Res Part I Oceanogr Res Pap 2008;55:50–72. https://doi.org/10.1016/j.dsr.2007.10.001.

[40] Kuang Y, Kenney MJ, Meng Y, Hung W-H, Liu Y, Huang JE, et al. Solar-driven, highly sustained splitting of seawater into hydrogen and oxygen fuels. Proc Natl Acad Sci U S A 2019;116:6624–9. https://doi.org/10.1073/pnas.1900556116.

[41] McKay MD, Beckman RJ, Conover WJ. A comparison of three methods for selecting values of input variables in the analysis of output from a computer code. Technometrics 1979;21:239–45. https://doi.org/10.2307/1268522.

[42] Department for Energy Security and Net Zero. Hydrogen Production Business Model / Net Zero Hydrogen Fund: HAR1 successful projects. London: DESNZ; 2023. https://www.gov.uk/government/publications/hydrogen-production-business-model-net-zero-hydrogen-fund-shortlisted-projects/hydrogen-production-business-model-net-zero-hydrogen-fund-har1-successful-projects [accessed 6 October 2026].